Compound 1d was prepared as described2 and colorless crystals were obtained by evaporation from light petroleum. Single-crystal X-ray diffraction experiments were carried out with a SMART 1K CCD area detector mounted on a 3-circle diffractometer, using graphite-monochromated Mo-Kα radiation (λ = 0.71073 Å) and SMART software.17 The temperature of the experiments was controlled using an Oxford Cryosystems Cryostream open-flow N2 gas cryostat.18 The temperature measurement was calibrated against the phase transition in KH2PO4 at 122.5 K,19 the possible error not exceeding 2 K. Full data collections were performed at 210 K (α-1d) and 150 K (β-1d). In both cases, over a hemisphere of reciprocal space was nominally covered by four sets of ω scans (each scan 0.3° in ω), each set with different φ and/or 2θ angles. Reflection intensities were integrated using SAINT17 and corrected for Lorentz and polarization factors, absorption being negligible (μ = 0.6 cm–1). The structures were solved by direct methods20 and refined by full-matrix least squares against F2 of all reflections using SHELXTL.21 C and N atoms were refined with anisotropic displacement parameters. H atoms were treated as ‘riding’ (α-1) or refined isotropically (β-1d). Crystal data and experimental parameters are listed in Table 1.

17	SMART and SAINT, Release 4.05, Area detector control and integration software. Bruker AXS, Analytical X-Ray Instruments, Madison, WI, 1995.

18	J. Cosier and A. M. Glazer, J. Appl. Crystallogr., 1986, 19, 105.

19	R. J. Nelmes, G. M. Meyer and J. E. Tiballis, J. Phys. C, 1982, 15, 59.

20	G. M. Sheldrick, Acta Crystallogr., Sect. A, 1990, 46, 467.

21	G. M. Sheldrick, SHELXTL, Version 5/VMS, Bruker AXS, Analytical X-Ray Instruments, Madison, WI, 1995.