## Supplementary 1.

The calculated dehydrated C1 structure and a comparison with the experimental framework structure (Al highlighted in grey and pink).  Calculated Ca2+positions are shown in blue with the experimental positions shown as grey spheres.

## Supplementary 2.

The calculated hydrated C1 structure and a comparison with the experimental framework structure (Al highlighted in grey and pink).  Calculated Ca2+positions are shown as green spheres with the experimental positions shown as blue spheres.  Grey spheres show the experimental water oxygen positions.

## Supplementary 3.

The experimental structure of hydrated Goosecreekite highlighting the Ca2+ coordination sphere, which should be compared to our results given in Figure 2.