Supporting information to accompany ‘A Dense Coordination Polymer Bearing an Extensive and Highly Intricate Hydrogen Bonding Array’

T.J. Prior, M.J. Rosseinsky

Crystallographic data.

Table 1: Unit cell information for N3DAB

Lattice constants : 	a      	= 6.6480(18) Å

b      	= 8.5504(23) Å

c      	= 11.124(3)  Å

alpha  	= 70.280(6) °

beta   	= 79.594(6) °

gamma  	= 76.093(6) °

Volume 	= 574.4      Å3

Spacegroup          	P-1

Wavelength          	0.69410  Å

Formula             	C12 H11 N1 O7 Ni 0.50

Formula Weight      	310.6

Density             	1.796       Mg/m3

Absorpt. Coeff.     	0.932       mm-1

Table 2: Atomic coordinates and thermal parameters

Atom	x/a		y/b		z/c		Ueq / Å2

C1	0.89691	0.16321	1.18381	0.01402

O1	0.91013	0.17478	1.28759	0.02027

O2	0.94097	0.01806	1.15859	0.02388

C2	0.83240	0.31002	1.07087	0.01186

C3	0.76234	0.47067	1.08429	0.01163

C4	0.70170	0.60671	0.97771	0.01154

C5	0.62116	0.77763	0.99137	0.01344

O3	0.60275	0.80477	1.09528	0.01883

O4	0.56886	0.89456	0.88572	0.02238

C6	0.70370	0.58177	0.86017	0.01192

C7	0.77418	0.42057	0.84682	0.01200

C8	0.75644	0.39425	0.72228	0.01215

O5	0.87667	0.27183	0.69021	0.01878

O6	0.61569	0.49784	0.65851	0.01471

C9	0.84087	0.28556	0.95197	0.01266

NI1	0.50000	0.50000	0.50000	0.01101

O7	0.79263	0.37862	0.44326	0.01615

N1	0.38878	0.27264	0.60388	0.01508

C10	0.44353	0.13259	0.55290	0.01327

C11	0.31673	0.11639	0.47314	0.01513

C12	0.62773	0.01582	0.57940	0.01505

H2	0.98731	-0.06166	1.21835	0.03299

H3	0.75593	0.48743	1.16519	-1.20000

H4	0.51655	0.98682	0.89975	0.08537

H6	0.65695	0.67476	0.78887	-1.20000

H9	0.89254	0.17593	0.94300	-1.20000

H7B	0.83434	0.31936	0.51442	0.02439

H7A	0.80242	0.31006	0.40398	0.04713

H1A	0.42470	0.24325	0.68522	0.01228

H1B	0.24778	0.30839	0.61303	0.02834

H11	0.19097	0.19645	0.45441	-1.20000

H12	0.71569	0.02648	0.63352	-1.20000

Table 3: Anisotropic thermal parameters

Atom	U11		U22		U33		U12		U13		U23

C1	0.01695	0.01115	0.01258	0.00015	-0.00285	-0.00323

O1	0.03284	0.01512	0.01296	0.00204	-0.00699	-0.00679

O2	0.04305	0.01104	0.01609	0.00780	-0.01342	-0.00609

C2	0.01291	0.01077	0.01187	0.00009	-0.00368	-0.00389

C3	0.01172	0.01188	0.01172	-0.00104	-0.00100	-0.00518

C4	0.01308	0.00928	0.01306	-0.00084	-0.00142	-0.00537

C5	0.01540	0.01096	0.01476	-0.00126	-0.00199	-0.00570

O3	0.03131	0.01126	0.01455	0.00006	-0.00418	-0.00682

O4	0.03924	0.01037	0.01306	0.00339	-0.00465	-0.00263

C6	0.01350	0.01040	0.01179	-0.00181	-0.00270	-0.00299

C7	0.01339	0.01189	0.01127	-0.00083	-0.00195	-0.00509

C8	0.01614	0.00986	0.01081	-0.00144	-0.00202	-0.00409

O5	0.02593	0.01522	0.01464	0.00609	-0.00799	-0.00789

O6	0.01939	0.01254	0.01388	0.00102	-0.00670	-0.00654

C9	0.01385	0.01125	0.01361	0.00058	-0.00257	-0.00631

NI1	0.01451	0.00866	0.01019	0.00059	-0.00340	-0.00424

O7	0.02023	0.01377	0.01521	0.00170	-0.00485	-0.00739

N1	0.01944	0.01285	0.01400	-0.00145	-0.00114	-0.00700

C10	0.01781	0.00880	0.01305	-0.00242	0.00054	-0.00443

C11	0.01618	0.01182	0.01696	-0.00029	-0.00359	-0.00463

C12	0.01904	0.01229	0.01446	-0.00223	-0.00591	-0.00341

Table 4: Bond lengths

Atom1	Atom2	Distance / Å

C1	O1	1.2117(4)

C1	O2	1.3173(3)

C1	C2	1.4865(4)

C2	C3	1.3899(4)

C2	C9	1.3966(4)

C3	C4	1.3920(4)

C4	C5	1.4798(4)

C4	C6	1.3913(4)

C5	O3	1.2334(4)

C5	O4	1.2997(4)

C6	C7	1.3943(4)

C7	C8	1.5054(4)

C7	C9	1.3883(4)

C8	O5	1.2683(3)

C8	O6	1.2572(3)

O6	NI1	2.0401(6)

NI1	O7	2.0708(4)

NI1	N1	2.1278(5)

N1	C10	1.4361(3)

C10	C11	1.3879(3)

C10	C12	1.3883(3)

O2	H2	0.81775(23)

C3	H3	0.9500(3)

O4	H4	0.83618(20)

C6	H6	0.9500(3)

C9	H9	0.95005(24)

O7	H7B	0.8375(3)

O7	H7A	0.82648(16)

N1	H1A	0.9136(3)

N1	H1B	0.91173(24)

C11	H11	0.95003(20)

C12	H12	0.95002(19)

Table 5: Bond angles

Atom1	Atom2	Atom3	Angle / °

O1	C1	O2	123.30(3)

O1	C1	C2	124.10(5)

O2	C1	C2	112.59(3)

C1	C2	C3	119.88(3)

C1	C2	C9	119.80(4)

C3	C2	C9	120.31(3)

C2	C3	C4	119.18(3)

C3	C4	C5	119.77(3)

C3	C4	C6	120.59(4)

C5	C4	C6	119.51(3)

C4	C5	O3	122.26(3)

C4	C5	O4	114.37(3)

O3	C5	O4	123.36(5)

C4	C6	C7	120.13(3)

C6	C7	C8	118.95(3)

C6	C7	C9	119.37(3)

C8	C7	C9	121.41(4)

C7	C8	O5	119.70(3)

C7	C8	O6	115.29(3)

O5	C8	O6	125.00(3)

C8	O6	NI1	131.04(5)

C2	C9	C7	120.36(4)

O6	NI1	O7	88.368(16)

O6	NI1	N1	91.188(15)

O7	NI1	N1	94.883(17)

NI1	N1	C10	119.46(3)

N1	C10	C11	120.306(23)

N1	C10	C12	120.11(3)

C11	C10	C12	119.54(3)

# Table 6: Classical hydrogen bonds found in N3DAB

| # Donor - H | Acceptor | d (D-H) /Å | d (H···A) /Å | d (D···A) /Å |  (DHA) / ° |
| --- | --- | --- | --- | --- | --- |
| O7 – H7B | O5 | 0.838 (30) | 1.916 (32) | 2.704 (2) | 156 (3) |
| N1 - H1A | O3_$1 | 0.913 (24) | 2.316 (25) | 3.193 (3) | 161 (3) |
| N1 - H1B | O5_$2 | 0.912 (26) | 2.519 (29) | 3.367 (3) | 155 (3) |
| O2 - H2 | O5_$3 | 0.818 (25) | 1.844 (27) | 2.631 (2) | 161 (4) |
| O4 - H4 | O3_$4 | 0.836 (28) | 1.782 (30) | 2.613 (2) | 171 (6) |
| O7 - H7A | O1_$5 | 0.828 (35) | 1.951 (36) | 2.746 (2) | 162 (4) |

Symmetry operators for generating equivalent atom positions:

$1 : 1-x, -y, -z

$2 : 1+x, y, z

$3 : -x, 2-y, -z

$4 : 1-x, 1-y, -z

$5 : x, y, 1+z

Description of hydrogen bonded networks within N3DAB.

Infinite hydrogen bonded sheets are composed of chains made up from Z-shaped links as shown in Figure 4. These chains are held together by further hydrogen bonds. Using the Graph Set Analysis for the hydrogen bonding network, the chains can be described as C22(23).The links are held together by the very familiar R22(8)carboxylic acid dimer motifs (interaction 1), for which distances are 2.61(1) Å (O1···O8). Each link involves two btc units and two nickel atoms joined by one 1,4-DAB which is part of the 1-D coordination polymer. Further weaker R22(12) interactions (N1···O3 = 3.19(1) Å, O7···O1 = 2.75(1) Å) (interaction 2) also secure links together. These chains are joined together into an infinite layer by R22(16)hydrogen bonding motifs, for which distances are 2.63(1) Å (O2···O5) (interaction 3).

Additional hydrogen bonding networks run through the entire structure and are not constrained to run within the layers, reinforcing the remarkable extent of hydrogen bonding within the structure. Figure S1 shows one of the C22(16) sawtooth chains which extends through the structure (O3···O4 distances are 2.61 (1)Å), held together by R22(16)hydrogen bonding motifs to give an infinite sheet.

Figure S1. Infinite chains, held together by R22(16)motifs labelled 1.

Figure S2. X-ray powder diffraction data for N3DAB

Indexing of X-ray powder diffraction data for N3DAB

Wavelength : 1.540598 Å

Number of accepted peaks : 81

Refined cell parameters :

Cell_A     : 6.7246(15) Å

Cell_B     : 8.5855(11) Å

Cell_C     : 11.1893(14)Å

Cell_Alpha : 70.505(9)  °

Cell_Beta  : 80.186(12) °

Cell_Gamma : 75.739(12) °

Cell_Volume: 587.44     Å3

Number of single indexed lines : 52

Number of unindexed lines      : 0

2Theta zeropoint : 0.025(4)

Final 2Theta window : 0.0400

N   2Th[obs]    H   K   L  2Th[calc]  obs-calc   Int.   d[obs]   d[calc]

1    11.156     0   1   0    11.158   -0.0029    83.3   7.9251    7.9231

2    11.747     0   1   1    11.750   -0.0031    18.1   7.5274    7.5255

3    13.634     1   0   0    13.640   -0.0054    41.3   6.4894    6.4869

4    15.328     1   0   1    15.335   -0.0066    12.0   5.7759    5.7734

5    15.508     1   1   1    15.500    0.0072     2.1   5.7095    5.7121

6    15.778     1   1   0    15.780   -0.0020    20.0   5.6122    5.6115

7    15.914     0  -1   1    15.927   -0.0128     2.0   5.5645    5.5601

8    16.726    -1   0   1    16.731   -0.0054    32.7   5.2962    5.2945

9    16.876     0   0   2    16.877   -0.0002   100.0   5.2493    5.2492

10    17.167     0   1   2    17.165    0.0020    93.4   5.1612    5.1618

11    19.370    -1   1   0    19.356    0.0138     6.7   4.5787    4.5820

12    20.043    -1  -1   1    20.038    0.0048     5.6   4.4265    4.4276

13    20.267    -1   1   1    20.272   -0.0047    42.7   4.3781    4.3771

14    20.697     1   0   2    20.697    0.0003    91.5   4.2881    4.2881

15    21.400     0   2   1    21.401   -0.0007    78.3   4.1488    4.1486

16    21.975     1  -1   1    21.973    0.0018    14.9   4.0415    4.0418

17    22.331     1   2   1    22.324    0.0068     2.5   3.9780    3.9792

18    22.428     0   2   0    22.424    0.0038     2.4   3.9609    3.9616

19    22.778    -1   0   2    22.780   -0.0016    38.8   3.9008    3.9005

20    23.789     1   2   0    23.791   -0.0021    40.0   3.7373    3.7369

21    24.011     1   2   2    23.999    0.0113     1.7   3.7033    3.7050

22    25.432     0   0   3    25.432    0.0003     7.4   3.4995    3.4995

23    25.625     1   1   3    25.623    0.0016    33.3   3.4736    3.4738

24    26.484    -1  -1   2    26.481    0.0032    15.9   3.3627    3.3631

25    26.899     2   1   1    26.899    0.0004    22.9   3.3119    3.3119

26    27.483     2   0   0    27.477    0.0058    88.0   3.2428    3.2434

27    27.755     1   0   3    27.749    0.0062    14.6   3.2116    3.2123

28    27.940    -1  -2   1    27.938    0.0019    31.4   3.1908    3.1910

29    28.274    -1   2   1    28.280   -0.0061     7.2   3.1539    3.1532

30    28.373     0   2   3    28.384   -0.0110     5.7   3.1430    3.1418

31    29.574    -2   0   1    29.577   -0.0025     9.5   3.0181    3.0178

32    30.578    -2  -1   1    30.581   -0.0028    10.9   2.9212    2.9210

33    30.911     0  -1   3    30.902    0.0085     2.1   2.8906    2.8913

34    31.511     1  -2   1    31.514   -0.0036     3.9   2.8369    2.8366

35    31.857    -2   1   0    31.848    0.0086    14.9   2.8069    2.8076

36    32.240     1   3   2    32.234    0.0068     7.1   2.7743    2.7749

37    33.029     1   1   4    33.031   -0.0026    30.0   2.7099    2.7097

38    33.211     2  -1   1    33.207    0.0047    10.7   2.6954    2.6958

39    33.888     1  -1   3    33.848    0.0399    28.2   2.6431    2.6462

40    34.730     0   2   4    34.730   -0.0006     3.6   2.5809    2.5809

41    35.489    -2  -2   1    35.480    0.0089     3.1   2.5275    2.5281

42    35.817     2   0   3    35.856   -0.0396     8.4   2.5051    2.5024

43    36.274     1  -2   2    36.279   -0.0057     2.4   2.4746    2.4742

44    37.534     0  -3   1    37.538   -0.0039     5.9   2.3943    2.3941

45    38.225    -1   3   1    38.240   -0.0152     2.0   2.3526    2.3517

46    39.070     2   1   4    39.045    0.0248    28.4   2.3036    2.3051

47    39.159     1   3   4    39.131    0.0279    32.4   2.2986    2.3002

48    39.307     0  -1   4    39.289    0.0176    28.9   2.2903    2.2913

49    40.373     0   3   4    40.343    0.0300     6.2   2.2323    2.2339

50    41.109     1   1   5    41.101    0.0077    20.4   2.1940    2.1944

51    41.425     3   1   2    41.401    0.0235    25.8   2.1780    2.1792

52    41.720     2  -1   3    41.704    0.0168     5.6   2.1632    2.1640

53    42.232     1   4   2    42.234   -0.0025     5.0   2.1382    2.1381

54    42.401     1  -2   3    42.418   -0.0170     3.8   2.1300    2.1292

55    42.726     0  -3   2    42.735   -0.0096     9.8   2.1146    2.1142

56    42.853     2   3   4    42.876   -0.0236     7.2   2.1086    2.1075

57    43.034     0   0   5    43.044   -0.0107     6.7   2.1002    2.0997

58    43.551     1   4   3    43.548    0.0037     1.0   2.0764    2.0766

59    43.985     1   0   5    43.991   -0.0053     2.7   2.0569    2.0567

60    44.857    -2   2   3    44.838    0.0190     8.3   2.0190    2.0198

61    45.517    -1   1   5    45.489    0.0287     4.6   1.9912    1.9924

62    46.257     0   3   5    46.256    0.0008    10.2   1.9611    1.9611

63    46.563    -2   0   4    46.529    0.0341     2.8   1.9489    1.9503

64    48.011     2  -1   4    47.991    0.0191    10.6   1.8935    1.8942

65    50.101     0   2   6    50.106   -0.0048     3.8   1.8192    1.8191

66    50.987    -1   4   3    51.005   -0.0184     2.0   1.7897    1.7891

67    51.795    -3   0   3    51.758    0.0375     2.2   1.7636    1.7648

68    53.844     1   5   3    53.826    0.0178     2.7   1.7013    1.7018

69    55.137     0   5   2    55.146   -0.0083     2.7   1.6644    1.6642

70    55.473     4   2   2    55.442    0.0307     1.3   1.6551    1.6560

71    55.929     0   5   1    55.930   -0.0007     3.0   1.6427    1.6427

72    56.745     1   4   6    56.716    0.0290     4.2   1.6210    1.6217

73    57.768    -2  -4   2    57.736    0.0315     0.9   1.5947    1.5955

74    58.480    -2   4   2    58.495   -0.0145     3.1   1.5770    1.5766

75    59.400    -2   4   0    59.378    0.0222     3.3   1.5547    1.5552

76    62.114     1   0   7    62.110    0.0043     2.7   1.4931    1.4932

77    63.213     2  -2   5    63.178    0.0350     0.9   1.4698    1.4705

78    65.672     3  -2   4    65.642    0.0307     2.0   1.4206    1.4212

79    66.093     1  -2   6    66.088    0.0052     2.1   1.4126    1.4127

80    66.956    -4   2   1    66.983   -0.0270     1.6   1.3964    1.3959

81    69.067     1   6   5    69.089   -0.0222     0.7   1.3588    1.3584

Average delta(2Theta) = 0.009

Maximum delta(2Theta) = 0.040 ( peak 42 ) = 4.5 * average

Thermogravimetric data for N3DAB