Electronic Supplementary Information (ESI)

1. The theoretical expressions of the intra-/inter-molecular magnetic interactions

In 1, J and J´ are the intra- and inter-cluster coupling constants, respectively

S(1) = S(2) = S(3) = 5/2 and z =2.

H = -J[S(1)S(2) + S(2)S(3)]                                           	(1a)

m1 = (Ng22F1)/(4kTF2) + tip                                     		 (1b)

m = m1/(1- 2zJ´m1/Ng22)                                        		 (1c)

Where

F1 = 680P1 + 455P2 + 286P3 + 165P4 + 84P5 + 35P6 + 10P7+ P8 + 35

F2 = 8P1 + 7P2 + 6P3 + 5P4 + 4P5 + 3P6+ 2P7 + P8 + 3

P1 = e27.5x; P2 = e20x + e25x; P3 = e13.5x + e18.5x + e22.5x; P4 = e8x + e13x + e17x + e20x;

P5 = e3.5x + e8.5x + e12.5x + e15.5x + e17.5x; P6 = e15x + e5x + e9x + e12x + e14x;

P7 = e2.5x + e6.5x + e9.5x + e11.5x; P8 = e5x + e8x;

x = J/(kT)                                                     			 Eq. (1)

2. The two-dimensional skeleton in compound 1.

Fig. 1S  Perspective view of the two-dimensional skeleton in 1.

3.	Temperature dependence of ac magnetic susceptibility measured at different frequencies and field dependence of magnetization at 1.97 K

Fig. 2S Temperature dependence of ac magnetic susceptibility measured at zero applied dc field and 2 Oe ac field with different frequencies from 111-1111 Hz.

Fig. 3S  Field dependence of magnetization at 1.97 K for 1. Magnetization (0 to 70 kOe) is superposing with de-magnetization (70 to 0 kOe). No detected hysterestic loop was observed.