Electronic Supplementary Information

Communication Ref.: B200556P (E-Submission Web Password: 960518)

Title: 2-(1,3-Dithiolan-2-ylidene)-5-(1,3-dithian-2-ylidene)-1,3,4,6-tetrathiapentalene (DHDA-TTP), a hybrid of BDH-TTP and BDA-TTP, and its metallic cation-radical salts

Authors: Jun-ichi Yamada,* Maki Watanabe, Takashi Toita, Hiroki Akutsu, Shin'ichi Nakatsuji, Hiroyuki Nishikawa, Isao Ikemoto and Koichi Kikuchi*

Selected Crystallographic Data of (DHDA-TTP)4AuI2 and (DHDA-TTP)2X (X= ClO4, AsF6, SbF6)

(DHDA-TTP)4AuI2	(DHDA-TTP)2ClO4	(DHDA-TTP)2AsF6	(DHDA-TTP)2SbF6

Formula			C22S16H20Au0.5I1	C22H20S16Cl1O4	C22H20S16As1F6	C22H20S16Sb1F6

Temperature/K		298		295		295		295

Formula mass		1024.42		896.81		976.19		1033.10

Crystal system		Monoclinic	Triclinic		Triclinic		Monoclinic

a/Å			37.27(2)		7.839(4)		7.952(2)		37.26(1)

b/Å			7.953(4)		17.451(6)		17.591(5)		8.2646(8)

c/Å			11.448(8)		6.460(4)		6.455(2)		11.282(3)

/deg					96.82(4)		96.25(2)

/deg			100.18(5)		108.45(4)		108.32(2)		98.60(1)

/deg					91.38(4)		91.24(2)

V/Å3			3339(3)		830.6(7)		850.5(4)		3435(1)

Space group 		C2/c		P1		P1		C2/c

# Z			4		1		1		4

Dcalced/Mg m–3		2.04		1.793		1.906		1.998

Crystal dimensions/mm3	0.5  0.4  0.2	0.5 0.1 0.05	0.5 0.4 0.25	0.4 0.3 0.08

Crystal color		Black		Black		Black		Black

Radiation			Mo K		Mo K		Mo K		Mo K

µ(Mo K)/cm–1		7.211		11.534		20.339		18.28

Diffractometer		MacScience 	Rigaku AFC7R	Rigaku AFC7R	Rigaku RAXIS-IV IP

MXC18

Total no. of reflcns		5700		3927		4192		2822

No. of unique reflcns		4311		3801		3913		2745

No. of reflcns obsd		2936 (I > 3(I))	1578 (I > 2(I))	2983 (I > 3(I))	2199 (I > 3(I))

No. of parameters		200		205		235		205

R; RW			0.067; 0.089	0.070; 0.069	0.045; 0.064	0.092; 0.097

GOF			1.804		1.600		2.130		3.97

Max peak in

final diff. map (e/Å–3)	1.28/–0.81	0.699/–0.578	0.699/–0.578	1.026/–1.271