Supplementary Material (ESI) for Chemical Communications

This journal is © The Royal Society of Chemistry 2002

Synthesis and Characterisation of the New Oxyselenide Bi2YO4Cu2Se2

John S. O. Evans,*a Edward B. Brogdena, Amber L. Thompsona, and Richard L. Cordinera

a Department of Chemistry, University of Durham, Science Site, Durham, DH1 3LE. Fax: 44 191 384 4737 ; Tel: 44 191 374 3113; E-mail: john.evans@durham.ac.uk

Fractional atomic coordinates from Rietveld refinement of Bi2LnO4Cu2Se2 phases.

| Atom | x/a | y/b | z/c | Uiso (Å2) |
| --- | --- | --- | --- | --- |
| La | 0.500000 | 0.500000 | 0.500000 | 1.3(3) |
| Bi | 0.500000 | 0.500000 | 0.8928(2) | 1.0(2) |
| Se | 0.500000 | 0.500000 | 0.3080(4) | 0.92(3) |
| Cu | 0.000000 | 0.500000 | 0.250000 | 1.55(4) |
| O | 0.000000 | 0.500000 | 0.941(1) | 4.8(15) |
| 2=8.7 | R(F2)=23.8% |  |  |  |

| Atom | x/a | y/b | z/c | Uiso (Å2) |
| --- | --- | --- | --- | --- |
| Nd | 0.500000 | 0.500000 | 0.500000 | 0.16(8) |
| Bi | 0.500000 | 0.500000 | 0.89426(9) | 1.0(5) |
| Se | 0.500000 | 0.500000 | 0.3106(2) | 0.62(20) |
| Cu | 0.000000 | 0.500000 | 0.250000 | 0.8(14) |
| O | 0.000000 | 0.500000 | 0.940(14) | 4.0(6) |
| 2=2.8 | R(F2)=9.0% |  |  |  |

| Atom | x/a | y/b | z/c | Uiso (Å2) |
| --- | --- | --- | --- | --- |
| Sm | 0.500000 | 0.500000 | 0.500000 | -0.04(7) |
| Bi | 0.500000 | 0.500000 | 0.89511(8) | 0.44(18) |
| Se | 0.500000 | 0.500000 | 0.3109(2) | 0.64(14) |
| Cu | 0.000000 | 0.500000 | 0.250000 | 0.9(12) |
| O | 0.000000 | 0.500000 | 0.9401(7) | 1.1(5) |
| 2=2.7 | R(F2)=8.3% |  |  |  |

| Atom | x/a | y/b | z/c | Uiso (Å2) |
| --- | --- | --- | --- | --- |
| Gd | 0.500000 | 0.500000 | 0.500000 | 0.13(7) |
| Bi | 0.500000 | 0.500000 | 0.89593(8) | 0.72(4) |
| Se | 0.500000 | 0.500000 | 0.3114(2) | 0.59(10) |
| Cu | 0.000000 | 0.500000 | 0.250000 | 1.3(7) |
| O | 0.000000 | 0.500000 | 0.9415(7) | 2.0(5) |
| 2=2.7 | R(F2)=9.0% |  |  |  |