XRD identification.  The as-synthesized crystalline samples were identified on a Rigaku D/max rB diffractometer using Cu-K( radiation (0.15418 nm).  The range of scan angle was 5( to 35(/(2() with a scanning speed of 4(/(2() per min.

SEM. Scanning electron microscopy images of the synthesized samples were taken with a Philips XL 30 scanning electron microscope.

Element analysis.  The chemical compositions of the samples prepared were determined with inductively coupled plasma emission spectroscopy (ICP) on a HATACHI T-4010 spectrometer. Eu2O3 was chosen as a reference.  The samples analyzed were prepared by dissolution in concentrated nitric acid.

Mössbauer spectra.  The Mössbauer spectrum of Sample SEu was recorded at 77 K on a constant acceleration Mössbauer spectrometer with a source of 151Eu in Eu matrix.  The isomer shift of 151Eu of SEu was given relative to a reference sample of EuF3.  This spectrum was measured in Physics Department of Nanjing University.

27Al and 31P MAS NMR. 27Al, 31P magic angle spinning (MAS) NMR spectra of Sample SAP and Sample SEu were collected at room temperature (298 K) on a Brucker DSX-300 spectrometer. The detail experimental acquisition conditions are listed in Table .

Luminescent spectroscopy. The luminescence spectra of Sample SEu and a reference sample containing pure Eu2O3 were recorded on a HATACHI-MPE-4 with 150 W Xe lamp.

Table . MAS NMR One Pulse Acquisition Conditions On Bruker DSX-300 Spectrometer

|  | 27Al | 31P |
| --- | --- | --- |
| Pulse length | 0.5 ( sec | 2.5 ( sec |
| Dead time | 0.5 ( sec | 0.5 ( sec |
| Recycle time | 0.8 s | 60 s |
| Resonance frequency | 78.2 MHz | 121.5 MHz |
| Spectral width | 47 kHz | 72 kHz |
| MAS spinning speed | 10 K | 10 K |
| Number of scans | 4800 | 32 |
| Number of digitalized points | 1024 | 4096 |
| Referening 0 ppm | AlCl3 | H3PO4 85% |