Supporting Information:

Strategies Toward Improving the Performance of Fluorescence-Based Sensors for Inorganic Anions

Radek Pohl, Dmitry Aldakov, Pavel Kubát, Karolina Jursíková, Manuel Marquez, and Pavel Anzenbacher, Jr.*

Contents

General, photophysical measurements

Characterization of compounds 2 and 3

Optical Spectroscopic data

Examples of titration data

General. 1H and 13C NMR spectra were recorded using a Varian Unity 400 (400 MHz) spectrometer. The chemical shifts (δ, ppm) are referenced to a solvent. EI-DIP mass spectra were recorded using a Shimadzu QP5050A spectrometer. Melting points are uncorrected.

Photophysical Measurements. Absorption spectra were measured with a Hitachi U-3010 spectrophotometer, accurate to  0.3 nm. Steady-state and time-resolved fluorescence measurements were performed on a single photon counting spectrofluorimeter from Edinburgh Analytical Instruments (FL/FS 900). 	Optically dilute solutions (OD = 0.09-0.11) used for all photophysical experiments were prepared in spectroscopic grade solvents unless otherwise stated. The binding constant calculations were performed as a single reciprocal plot transformation of the Stern-Volmer equation according to Connors.1 The fitting errors were <15%. The 1:1 stoichiometry was confirmed by Job plots in selected examples. Likewise, the 1:1 stoichiometry for the complexes of the DPQ-derivatives with anions is in agreement with previously published data.2

Characterization of compounds 2 and 3

Compound 2: 5,8-Di[2-(1-pyrenyl)ethyl]-2,3-di(1H-2-pyrrolyl)quinoxaline

M.p. >260 oC. 1H NMR (DMSO-d6, ): 3.72 (m, 8H), 6.29 (ddd, 2H, J = 2.5, 3.6, 4.9 Hz), 6.33 (ddd, 2H, J = 1.4, 2.4, 3.6 Hz), 7.12 (ddd, 2H, J = 1.4, 2.5, 4.1 Hz), 7.42 (s, 2H), 7.95-8.15 (m, 16H), 8.58 (d, 2H, J = 9.3 Hz), 11.47 (brs, 2H). 13C APT NMR (DMSO-d6, ): 32.97 CH2, 34.74 CH2, 109.09 CH, 111.26 CH, 121.25 CH, 124.02 CH, 124.17 C, 124.20 C, 124.80 CH, 124.89 CH, 126.13 CH, 126.51 CH, 127.19 CH, 127.50 CH, 127.75 CH, 128.38 CH, 128.40 C, 129.20 C, 129.33 C, 130.49 C, 130.91 C, 136.70 C, 137.68 C, 138.27 C, 143.91 C. EI/MS (70 eV): 716 (100) [M+], 215 (100). Anal. calcd. (%) for C52H36N4 (716.87): C, 87.12; H, 5.06; N, 7.82. Found: C, 86.60; H, 4.91; N, 7.68.

# Compound 3: 5,8-Di(1-pyrenylethynyl)-2,3-di(1H-2-pyrrolyl)quinoxaline

M.p. >260 oC. 1H NMR (DMSO-d6, 80 oC, ): 6.38 (dd, 2H, J = 2.5, 3.6 Hz), 6.56 (d, 2H, J = 3.6 Hz), 7.22 (brs, 2H), 8.12-8.55 (m, 18H), 9.08 (d, 2H, J = 9.0 Hz), 11.21 (brs, 2H). 13C NMR was not measured due to very low solubility of the titled compound. EI/MS (70 eV): 709 (33) [MH+], 536 (45), 521 (100). Anal. calcd. (%) for C52H28N4 . ½ EtOH (731.85): C, 86.98; H, 4.27; N, 7.66. Found: C, 87.37; H, 4.05; N, 7.92.

Optical Spectroscopic Data

Fig. 1. Normalized absorption (full line) and emission (dashed) spectra of pyrene, 1 (DPQ), 2 and 3 in air-saturated dichloromethane

Fig. 2. Emission traces of pyrene (at 395 nm), 1 (DPQ), 2 (both at 495 nm) and 3 (at 550 nm) in air-saturated dichloromethane

|  | Fig. 3. Excitation (a, left axis, emission at 490 nm) and absorbance (b, right axis) spectra of 2 (2.3 M) |
| --- | --- |

## Examples of the titration data for the sensor 2

## Sensor 2 and Fluoride

Changes in absorption and photoluminescence intensity of the sensor 2 (2.35 and 2 M in CH2Cl2 respectively) upon the addition of fluoride (0-459 M).

The panel above shows Y-reciprocal transformation of the photoluminescence isotherm and fit. ex = 387 nm (isosbestic point in UV-Vis spectra).

## Sensor 2 and Pyrophosphate

Changes in absorption and photoluminescence intensity of the sensor 2 (10 and 2 M in CH2Cl2 respectively) upon the addition of pyrophosphate (0-357 M).

The panel above shows Y-reciprocal transformation of the photoluminescence isotherm and fit. ex = 385 nm (isosbestic point in UV-Vis spectra).

## Examples of the titration data for the sensor 3

## Sensor 3 and Fluoride

Changes in absorption and photoluminescence intensity of the sensor 3 (2.02 and 2 M respectively in CH2Cl2) upon the addition of fluoride (0-362 M). The results of titration and fit were apparently affected by the aggregation process.

The panel above shows Y-reciprocal transformation of the photoluminescence isotherm and fit. ex = 441 nm (isosbestic point in UV-Vis spectra).

## Sensor 3 and Pyrophosphate

Changes in absorption and photoluminescence intensity of the sensor 3 (10 and 2 M in CH2Cl2) upon the addition of pyrophosphate (0-296 M).

The panel above shows Y-reciprocal transformation of the photoluminescence isotherm and fit. ex = 434 nm (isosbestic point in UV-Vis spectra).

References (Supporting Information).

- Connors, A. K. Binding Constants: the Measurement of Molecular Complex Stability; Wiley: New York, 1987.

- (a) Black, C. B.; Andrioletti, B.; Try, A. C.; Ruiperez, C.; Sessler, J. L. J. Am. Chem. Soc. 1999, 121, 10438-10439. (b) Anzenbacher Jr., P.; Try, A. C.; Miyaji, H.; Jursíková, K.; Lynch, V. M.; Marquez, M.; Sessler, J. L. J. Am. Chem. Soc. 2000, 122, 10268-10272.