Table 1.  Crystal data and structure refinement for Compound 2.

Identification code 	um316s

Empirical formula 	C20 H22 N4 O2

Formula weight 	350.42

Temperature 	300(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P-1

Unit cell dimensions	a = 8.7863(6) Å	= 96.4150(10)°.

b = 8.9879(6) Å	= 90.7830(10)°.

c = 12.6434(9) Å	 = 108.9400(10)°.

Volume	937.16(11) Å3

Z	2

Density (calculated)	1.242 Mg/m3

Absorption coefficient	0.083 mm-1

F(000)	372

Crystal size	0.32 x 0.25 x 0.24 mm3

Theta range for data collection	2.41 to 25.00°.

Index ranges	-10<=h<=10, -10<=k<=9, -9<=l<=15

Reflections collected	5023

Independent reflections	3278 [R(int) = 0.0110]

Completeness to theta = 25.00°	99.1 %

Absorption correction	Empirical

Max. and min. transmission	1.000000 and 0.804350

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3278 / 0 / 235

Goodness-of-fit on F2	1.002

Final R indices [I>2sigma(I)]	R1 = 0.0510, wR2 = 0.1485

R indices (all data)	R1 = 0.0644, wR2 = 0.1556

Largest diff. peak and hole	0.199 and -0.228 e.Å-3

Table 2.  Atomic coordinates  ( x 104) and equivalent  isotropic displacement parameters (Å2x 103)

for um316s.  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

________________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________________

N(4)	2728(2)	1186(2)	6367(1)	53(1)

O(2)	878(2)	-1286(2)	6420(1)	73(1)

N(3)	2594(2)	69(2)	7855(1)	52(1)

N(1)	3673(2)	2567(2)	9000(1)	56(1)

C(15)	5324(2)	3363(2)	6670(1)	43(1)

C(1)	3935(2)	1551(2)	8103(1)	42(1)

C(2)	3742(2)	2464(2)	7126(1)	41(1)

C(9)	5556(2)	1289(2)	8194(1)	47(1)

N(2)	2913(2)	3506(2)	7609(1)	57(1)

C(7)	1951(2)	-122(2)	6843(2)	50(1)

O(1)	2465(2)	4487(2)	9294(2)	92(1)

C(20)	6007(2)	2645(2)	5875(2)	57(1)

C(4)	2959(2)	3602(2)	8688(2)	60(1)

C(10)	6860(2)	2452(3)	8761(2)	60(1)

C(16)	6191(2)	4889(2)	7115(2)	56(1)

C(17)	7701(3)	5662(2)	6775(2)	67(1)

C(14)	5805(3)	-4(3)	7624(2)	65(1)

C(18)	8360(3)	4949(3)	5993(2)	70(1)

C(19)	7524(3)	3434(3)	5542(2)	73(1)

C(6)	2104(3)	-1170(3)	8540(2)	78(1)

C(8)	2124(3)	1423(3)	5348(2)	88(1)

C(12)	8612(4)	1022(5)	8177(3)	98(1)

C(11)	8376(3)	2311(4)	8748(2)	82(1)

C(13)	7341(4)	-132(4)	7611(2)	88(1)

C(5)	2355(4)	4567(3)	7043(3)	100(1)

C(3)	3705(3)	2276(4)	10104(2)	89(1)

________________________________________________________________________________

Table 3.   Bond lengths [Å] and angles [°] for  um316s.

_____________________________________________________

N(4)-C(7) 	1.363(3)

N(4)-C(2) 	1.449(2)

N(4)-C(8) 	1.451(3)

O(2)-C(7) 	1.221(2)

N(3)-C(7) 	1.361(2)

N(3)-C(1) 	1.463(2)

N(3)-C(6) 	1.446(3)

N(1)-C(4) 	1.367(3)

N(1)-C(1) 	1.444(2)

N(1)-C(3) 	1.450(3)

C(15)-C(16) 	1.385(3)

C(15)-C(20) 	1.382(3)

C(15)-C(2) 	1.521(2)

C(1)-C(9) 	1.523(2)

C(1)-C(2) 	1.593(2)

C(2)-N(2) 	1.452(2)

C(9)-C(14) 	1.379(3)

C(9)-C(10) 	1.397(3)

N(2)-C(4) 	1.356(3)

N(2)-C(5) 	1.452(3)

O(1)-C(4) 	1.227(2)

C(20)-C(19) 	1.387(3)

C(10)-C(11) 	1.379(3)

C(16)-C(17) 	1.382(3)

C(17)-C(18) 	1.356(3)

C(14)-C(13) 	1.391(3)

C(18)-C(19) 	1.373(3)

C(12)-C(13) 	1.376(4)

C(12)-C(11) 	1.371(4)

C(7)-N(4)-C(2)	111.89(15)

C(7)-N(4)-C(8)	120.71(17)

C(2)-N(4)-C(8)	123.61(17)

C(7)-N(3)-C(1)	112.59(15)

C(7)-N(3)-C(6)	122.13(17)

C(1)-N(3)-C(6)	124.87(16)

C(4)-N(1)-C(1)	111.77(16)

C(4)-N(1)-C(3)	120.90(18)

C(1)-N(1)-C(3)	125.15(18)

C(16)-C(15)-C(20)	118.09(17)

C(16)-C(15)-C(2)	120.10(16)

C(20)-C(15)-C(2)	121.53(16)

N(1)-C(1)-N(3)	113.22(14)

N(1)-C(1)-C(9)	112.88(14)

N(3)-C(1)-C(9)	112.67(15)

N(1)-C(1)-C(2)	102.07(13)

N(3)-C(1)-C(2)	100.94(12)

C(9)-C(1)-C(2)	114.05(14)

N(4)-C(2)-N(2)	113.42(14)

N(4)-C(2)-C(15)	112.32(14)

N(2)-C(2)-C(15)	112.67(14)

N(4)-C(2)-C(1)	102.00(13)

N(2)-C(2)-C(1)	101.09(13)

C(15)-C(2)-C(1)	114.42(13)

C(14)-C(9)-C(10)	119.08(18)

C(14)-C(9)-C(1)	120.51(18)

C(10)-C(9)-C(1)	120.00(16)

C(4)-N(2)-C(2)	112.64(15)

C(4)-N(2)-C(5)	121.93(19)

C(2)-N(2)-C(5)	124.48(18)

O(2)-C(7)-N(3)	125.74(18)

O(2)-C(7)-N(4)	125.38(18)

N(3)-C(7)-N(4)	108.87(15)

C(19)-C(20)-C(15)	120.66(19)

O(1)-C(4)-N(2)	126.0(2)

O(1)-C(4)-N(1)	125.0(2)

N(2)-C(4)-N(1)	109.00(16)

C(11)-C(10)-C(9)	120.5(2)

C(17)-C(16)-C(15)	120.64(19)

C(16)-C(17)-C(18)	120.8(2)

C(9)-C(14)-C(13)	120.0(2)

C(19)-C(18)-C(17)	119.5(2)

C(18)-C(19)-C(20)	120.2(2)

C(13)-C(12)-C(11)	120.3(2)

C(12)-C(11)-C(10)	120.0(3)

C(12)-C(13)-C(14)	120.2(2)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

Table 4.   Anisotropic displacement parameters  (Å2x 103) for um316s.  The anisotropic

displacement factor exponent takes the form:  -22[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22 	U33	U23	U13	U12

______________________________________________________________________________

N(4)	48(1) 	53(1)	44(1) 	7(1)	-8(1) 	-4(1)

O(2)	62(1) 	58(1)	70(1) 	-4(1)	-4(1) 	-14(1)

N(3)	47(1) 	47(1)	54(1) 	13(1)	1(1) 	1(1)

N(1)	50(1) 	75(1)	41(1) 	-8(1)	3(1) 	23(1)

C(15)	41(1) 	39(1)	45(1) 	8(1)	1(1) 	10(1)

C(1)	37(1) 	45(1)	41(1) 	2(1)	2(1) 	9(1)

C(2)	37(1) 	39(1)	45(1) 	3(1)	0(1) 	8(1)

C(9)	45(1) 	56(1)	44(1) 	14(1)	9(1) 	19(1)

N(2)	48(1) 	54(1)	74(1) 	9(1)	10(1) 	24(1)

C(7)	44(1) 	47(1)	48(1) 	0(1)	3(1) 	2(1)

O(1)	70(1) 	88(1)	113(1) 	-35(1)	17(1) 	34(1)

C(20)	61(1) 	48(1)	56(1) 	4(1)	13(1) 	10(1)

C(4)	38(1) 	56(1)	77(2) 	-15(1)	4(1) 	11(1)

C(10)	41(1) 	77(1)	61(1) 	17(1)	-1(1) 	14(1)

C(16)	51(1) 	42(1)	69(1) 	2(1)	6(1) 	7(1)

C(17)	55(1) 	46(1)	90(2) 	11(1)	6(1) 	0(1)

C(14)	79(2) 	70(1)	60(1) 	17(1)	14(1) 	40(1)

C(18)	52(1) 	63(1)	93(2) 	27(1)	19(1) 	9(1)

C(19)	73(2) 	71(2)	76(2) 	15(1)	34(1) 	24(1)

C(6)	80(2) 	64(1)	82(2) 	32(1)	7(1) 	5(1)

C(8)	82(2) 	96(2)	63(2) 	23(1)	-26(1) 	-9(1)

C(12)	68(2) 	148(3)	109(2) 	61(2)	30(2) 	61(2)

C(11)	46(1) 	115(2)	91(2) 	37(2)	5(1) 	25(1)

C(13)	107(2) 	107(2)	84(2) 	34(2)	35(2) 	75(2)

C(5)	100(2) 	90(2)	137(3) 	35(2)	9(2) 	61(2)

C(3)	90(2) 	121(2)	45(1) 	-3(1)	12(1) 	22(2)

______________________________________________________________________________

Table 5.   Hydrogen coordinates ( x 104) and isotropic  displacement parameters (Å2x 10 3)

for um316s.

________________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________________

H(20A)	5445	1622	5561	69

H(10A)	6705	3328	9150	72

H(16A)	5754	5399	7649	68

H(17A)	8271	6684	7087	81

H(14A)	4946	-792	7248	78

H(18A)	9371	5483	5764	84

H(19A)	7976	2934	5012	87

H(6A)	1201	-2024	8205	117

H(6B)	1803	-754	9208	117

H(6C)	2983	-1554	8664	117

H(8A)	1488	418	4974	133

H(8B)	3014	1915	4933	133

H(8C)	1469	2093	5463	133

H(12A)	9634	926	8171	118

H(11A)	9240	3090	9126	99

H(13A)	7509	-999	7220	105

H(5A)	1849	5138	7526	150

H(5B)	1593	3961	6476	150

H(5C)	3256	5302	6751	150

H(3A)	3496	3118	10550	134

H(3B)	4745	2231	10305	134

H(3C)	2893	1287	10188	134

________________________________________________________________________________

Table 6.  Torsion angles [°] for um316s.

________________________________________________________________

C(4)-N(1)-C(1)-N(3)	-91.21(19)

C(3)-N(1)-C(1)-N(3)	72.0(2)

C(4)-N(1)-C(1)-C(9)	139.28(17)

C(3)-N(1)-C(1)-C(9)	-57.5(3)

C(4)-N(1)-C(1)-C(2)	16.42(19)

C(3)-N(1)-C(1)-C(2)	179.63(19)

C(7)-N(3)-C(1)-N(1)	121.37(17)

C(6)-N(3)-C(1)-N(1)	-65.9(2)

C(7)-N(3)-C(1)-C(9)	-109.01(17)

C(6)-N(3)-C(1)-C(9)	63.7(2)

C(7)-N(3)-C(1)-C(2)	13.03(18)

C(6)-N(3)-C(1)-C(2)	-174.21(19)

C(7)-N(4)-C(2)-N(2)	-89.48(19)

C(8)-N(4)-C(2)-N(2)	68.6(2)

C(7)-N(4)-C(2)-C(15)	141.33(16)

C(8)-N(4)-C(2)-C(15)	-60.6(2)

C(7)-N(4)-C(2)-C(1)	18.37(19)

C(8)-N(4)-C(2)-C(1)	176.49(19)

C(16)-C(15)-C(2)-N(4)	158.71(17)

C(20)-C(15)-C(2)-N(4)	-27.4(2)

C(16)-C(15)-C(2)-N(2)	29.1(2)

C(20)-C(15)-C(2)-N(2)	-156.99(16)

C(16)-C(15)-C(2)-C(1)	-85.6(2)

C(20)-C(15)-C(2)-C(1)	88.3(2)

N(1)-C(1)-C(2)-N(4)	-134.71(14)

N(3)-C(1)-C(2)-N(4)	-17.83(16)

C(9)-C(1)-C(2)-N(4)	103.24(16)

N(1)-C(1)-C(2)-N(2)	-17.59(15)

N(3)-C(1)-C(2)-N(2)	99.28(14)

C(9)-C(1)-C(2)-N(2)	-139.65(15)

N(1)-C(1)-C(2)-C(15)	103.77(15)

N(3)-C(1)-C(2)-C(15)	-139.36(14)

C(9)-C(1)-C(2)-C(15)	-18.29(19)

N(1)-C(1)-C(9)-C(14)	158.72(18)

N(3)-C(1)-C(9)-C(14)	28.9(2)

C(2)-C(1)-C(9)-C(14)	-85.4(2)

N(1)-C(1)-C(9)-C(10)	-28.6(2)

N(3)-C(1)-C(9)-C(10)	-158.43(16)

C(2)-C(1)-C(9)-C(10)	87.3(2)

N(4)-C(2)-N(2)-C(4)	122.82(17)

C(15)-C(2)-N(2)-C(4)	-108.17(17)

C(1)-C(2)-N(2)-C(4)	14.41(19)

N(4)-C(2)-N(2)-C(5)	-68.2(3)

C(15)-C(2)-N(2)-C(5)	60.8(2)

C(1)-C(2)-N(2)-C(5)	-176.6(2)

C(1)-N(3)-C(7)-O(2)	176.16(18)

C(6)-N(3)-C(7)-O(2)	3.2(3)

C(1)-N(3)-C(7)-N(4)	-2.4(2)

C(6)-N(3)-C(7)-N(4)	-175.39(19)

C(2)-N(4)-C(7)-O(2)	170.31(18)

C(8)-N(4)-C(7)-O(2)	11.5(3)

C(2)-N(4)-C(7)-N(3)	-11.1(2)

C(8)-N(4)-C(7)-N(3)	-169.97(19)

C(16)-C(15)-C(20)-C(19)	0.4(3)

C(2)-C(15)-C(20)-C(19)	-173.64(18)

C(2)-N(2)-C(4)-O(1)	174.03(19)

C(5)-N(2)-C(4)-O(1)	4.7(3)

C(2)-N(2)-C(4)-N(1)	-5.0(2)

C(5)-N(2)-C(4)-N(1)	-174.3(2)

C(1)-N(1)-C(4)-O(1)	172.62(19)

C(3)-N(1)-C(4)-O(1)	8.6(3)

C(1)-N(1)-C(4)-N(2)	-8.3(2)

C(3)-N(1)-C(4)-N(2)	-172.31(19)

C(14)-C(9)-C(10)-C(11)	0.2(3)

C(1)-C(9)-C(10)-C(11)	-172.55(19)

C(20)-C(15)-C(16)-C(17)	-0.3(3)

C(2)-C(15)-C(16)-C(17)	173.78(18)

C(15)-C(16)-C(17)-C(18)	0.5(3)

C(10)-C(9)-C(14)-C(13)	-0.5(3)

C(1)-C(9)-C(14)-C(13)	172.2(2)

C(16)-C(17)-C(18)-C(19)	-0.7(4)

C(17)-C(18)-C(19)-C(20)	0.8(4)

C(15)-C(20)-C(19)-C(18)	-0.6(4)

C(13)-C(12)-C(11)-C(10)	0.3(4)

C(9)-C(10)-C(11)-C(12)	-0.1(4)

C(11)-C(12)-C(13)-C(14)	-0.6(4)

C(9)-C(14)-C(13)-C(12)	0.8(4)

________________________________________________________________

Symmetry transformations used to generate equivalent atoms: