Supplementary material. Interferometric data for the system PEG6(6)-PEG2(2)-Water at four average compositions (a-d).  is the total number of Gouy interference fringes, : apparent diffusion coefficient,  is “area under the deviation function” (ref. 18). i is the refractive index fraction of the species i.

6=0.1000

|  | A1 | A2 | A3 | A4 |
| --- | --- | --- | --- | --- |
| (mol dm-3) | 0.02990 | 0.02991 | 0.02991 | 0.02991 |
| (mol dm-3) | 0.2692 | 0.2691 | 0.2691 | 0.2692 |
| (mol dm-3) | 0.0460 | 0.03671 | 0.00924 | 0.02302 |
| (mol dm-3) | -0.00022 | 0.02639 | 0.1051 | 0.06557 |
|  | -0.00153 | 0.1864 | 0.7837 | 0.4757 |
|  | 63.49 | 62.35 | 59.10 | 60.52 |
| x 105(cm2s-1) | 0.5369 | 0.5863 | 0.7935 | 0.6691 |
| x 104 | 15.9 | 44.2 | 41.0 | 49.3 |

6=0.3000

|  | B1 | B2 | B3 |
| --- | --- | --- | --- |
| (mol dm-3) | 0.08721 | 0.08728 | 0.08728 |
| (mol dm-3) | 0.2036 | 0.2035 | 0.2036 |
| (mol dm-3) | 0.03326 | 0.00841 | 0.0126 |
| (mol dm-3) | 0.02669 | 0.1164 | 0.1014 |
|  | 0.2170 | 0.8270 | 0.7355 |
|  | 57.05 | 65.44 | 63.73 |
| x 105(cm2s-1) | 0.5858 | 0.7897 | 0.7565 |
| x 104 | 34.1 | 18.1 | 24.8 |

6=0.7000

|  | C1 | C2 | C3 |
| --- | --- | --- | --- |
| (mol dm-3) | 0.21008 | 0.21003 | 0.21008 |
| (mol dm-3) | 0.09003 | 0.09002 | 0.09003 |
| (mol dm-3) | 0.04429 | 0.00003 | 0.00886 |
| (mol dm-3) | 0.00001 | 0.1505 | 0.1204 |
|  | 0.00007 | 0.9994 | 0.8146 |
|  | 62.12 | 68.31 | 66.93 |
| x 105(cm2s-1) | 0.5222 | 0.8633 | 0.7861 |
| x 104 | 6.9 | -30.8 | -8.7 |

6=0.90000

|  | D1 | D2 | D3 | D4 |
| --- | --- | --- | --- | --- |
| (mol dm-3) | 0.2704 | 0.2703 | 0.2703 | 0.2708 |
| (mol dm-3) | 0.03003 | 0.03006 | 0.03003 | 0.03014 |
| (mol dm-3) | 0.04569 | 0.00435 | 0.01182 | 0.0354 |
| (mol dm-3) | 0.00014 | 0.06011 | 0.06007 | 0.03033 |
|  | 0.00104 | 0.8259 | 0.6356 | 0.2272 |
|  | 61.41 | 33.57 | 43.47 | 61.32 |
| x 105(cm2s-1) | 0.5198 | 0.7727 | 0.7052 | 0.5507 |
| x 104 | 3.0 | -2.9 | 15.9 | 22.3 |