Table S1: Conditions and results of the diffraction experiments.

|  | NaY | Naphthalene in NaY | Anthracene in NaY a) | 2,3-Benz-anthracene in NaY |
| --- | --- | --- | --- | --- |
| Instrument | D1A | D1A | D2B | D2B |
| Wavelength [Å] | 1.909 | 1.909 | 2.3974 | 2.3974 |
| Step size | 0.05 | 0.05 | 0.05 | 0.05 |
| 2θ range / degrees | 10-142 | 10-150 | 10-157 | 5-158 |
| Rp [%] | 3.3 | 3.7 | 2.89 | 2.0 |
| Rwp[%] | 4.2 | 4.7 | 3.6 | 2.6 |
| Lattice constant [Å] | 24.8057(4) | 24.6919(9) | 24.71611(34) | 24.68262(33) |

a) only in 2,3-Benzanthracene in NaY the (111)-reflexion can be included in the Rietveld refinement despite of the asymmetry.

Table S2 : Results of the Rietveld refinement of NaY.

| Atom | x | y | z | Occupation factor | Biso [Å2] |
| --- | --- | --- | --- | --- | --- |
| Si | 0.12452(11) | 0.94612(10) | 0.03580(13) | 0.6999 | 0.0135(6) |
| Al | 0.12452(11) | 0.94612(10) | 0.03580(13) | 0.3001 | 0.0135(6) |
| O | 0.25244(7) | 0.25244(7) | 0.14267(12) | 0.930(11) | 0.0145(12) |
| O | 0.17758(8) | 0.17758(8) | 0.96616(12) | 0.971(11) | 0.0228(12) |
| O | 0.17715(10) | 0.17715(10) | 0.31809(12) | 0.989(10) | 0.0266(12) |
| O | 0.10607(7) | 0.89393(7) | 0.0 | 0.975(9) | 0.0155(11) |
| Na | 0.0 | 0.0 | 0.0 | 0.358(25) | 0.012(10) |
| Na | 0.0539(4) | 0.0539(4) | 0.0539(4) | 0.500(21) | 0.065(8) |
| Na | 0.23309(17) | 0.23309(17) | 0.23309(17) | 0.968(21) | 0.0225(26) |

Table S3 : Results of the Rietveld refinement of naphthalene in NaY.

| Atom | x | y | z | Occupation factor | Biso [Å2] |
| --- | --- | --- | --- | --- | --- |
| Si | 0.12324(19) | 0.94615(17) | 0.03595(21) | 0.7 | 0.0084(12) |
| Al | 0.12324(19) | 0.94615(17) | 0.03595(21) | 0.3 | 0.0089(10) |
| O | 0.25302(12) | 0.25302(12) | 0.14358(18) | 1.0 | 0.0119(5) |
| O | 0.10874(12) | 0.89126(12) | 0.0 | 1.0 | 0.0162(5) |
| O | 0.17422(14) | 0.17422(14) | 0.31839(19) | 1.0 | 0.0177(5) |
| O | 0.18061(12) | 0.18061(12) | 0.96532(17) | 1.0) | 0.0141(5) |
| Na | 0.0 | 0.0 | 0.0 | 0.845(32) | 0.0187(32) |
| Na | 0.0422(10) | 0.0422(10) | 0.0422(10) | 0.340(16) | 0.0379(32) |
| Na | 0.2344(4) | 0.2344(4) | 0.2344(4) | 0.877(9) | 0.0360(32) |
| Ca | 0.3113(8) | 0.3390(7) | 0.2392(4) | 0.0867(12) | 0.073(5) |
| Ca | 0.2697(8) | 0.3524(6) | 0.2751(6) | 0.0867(12) | 0.073(5) |
| Ca | 0.2642(6) | 0.3242(5) | 0.3239(5) | 0.0867(12) | 0.073(5) |
| Ca | 0.2226(8) | 0.3377(7) | 0.3598(7) | 0.0867(12) | 0.073(5) |
| Ca | 0.2172(7) | 0.3095(8) | 0.4085(6) | 0.0867(12) | 0.073(5) |
| Ca | 0.2534(7) | 0.2678(8) | 0.4214(4) | 0.0867(12) | 0.073(5) |
| Ca | 0.2951(6) | 0.2543(7) | 0.3855(5) | 0.0867(12) | 0.073(5) |
| Ca | 0.3005(5) | 0.2826(6) | 0.3367(4) | 0.0867(12) | 0.073(5) |
| Ca | 0.3421(6) | 0.2691(8) | 0.3008(6) | 0.0867(12) | 0.073(5) |
| Ca | 0.3475(7) | 0.2973(8) | 0.2520(5) | 0.0867(12) | 0.073(5) |
| Da | 0.3165(9) | 0.3596(8) | 0.2020(5) | 0.0867(12) | 0.183(12) |
| Da | 0.2438(10) | 0.3822(7) | 0.2659(8) | 0.0867(12) | 0.183(12) |
| Da | 0.1967(10) | 0.3674(9) | 0.3506(9) | 0.0867(12) | 0.183(12) |
| Da | 0.1861(9) | 0.3187(10) | 0.4365(8) | 0.0867(12) | 0.183(12) |
| Da | 0.2483(8) | 0.2472(9) | 0.4586(5) | 0.0867(12) | 0.183(12) |
| Da | 0.3209(8) | 0.2246(9) | 0.3947(7) | 0.0867(12) | 0.183(12) |
| Da | 0.3680(7) | 0.2394(10) | 0.3100(8) | 0.0867(12) | 0.183(12) |
| Da | 0.3786(8) | 0.2881(11) | 0.2241(6) | 0.0867(12) | 0.183(12) |

a) atoms are constrained by rigid body

Table S4 : Results of the Rietveld refinement of anthracene in NaY.

| Atom | x | y | z | Occupation factor | Biso [Å2] |
| --- | --- | --- | --- | --- | --- |
| Si | 0.12428(31) | 0.94551(27) | 0.03543(31) | 0.7 | 0.0023(10) |
| Al | 0.12428(31) | 0.94551(27) | 0.03543(31) | 0.3 | 0.0023(10) |
| O | 0.25236(23) | 0.25236(23) | 0.14401(29) | 1.0 | 0.0179(8) |
| O | 0.10679(20) | 0.89321(20) | 0.0 | 1.0 | 0.0179(8) |
| O | 0.17499(24) | 0.17499(24) | 0.31925(32) | 1.0 | 0.0179(8) |
| O | 0.17658(20) | 0.17658(20) | 0.96806(27) | 1.0 | 0.0179(8) |
| Na | 0.0 | 0.0 | 0.0 | 0.63(5) | 0.024(4) |
| Na | 0.0612(7) | 0.0612(7) | 0.0612(7) | 0.594(25) | 0.024(4) |
| Na | 0.2392(5) | 0.2392(5) | 0.2392(5) | 0.85726 | 0.024(4) |
| Ca | 0.3053(16) | 0.3599(17) | 0.2560(14) | 0.0353(7) | 0.04 |
| Ca | 0.2744(14) | 0.3693(14) | 0.2996(12) | 0.0353(7) | 0.04 |
| Ca | 0.2692(12) | 0.3311(11) | 0.3379(10) | 0.0353(7) | 0.04 |
| Ca | 0.2383(11) | 0.3405(10) | 0.3815(11) | 0.0353(7) | 0.04 |
| Ca | 0.2327(10) | 0.3020(10) | 0.4208(11) | 0.0353(7) | 0.04 |
| Ca | 0.2022(11) | 0.3118(13) | 0.4635(13) | 0.0353(7) | 0.04 |
| Ca | 0.1970(12) | 0.2736(15) | 0.5018(15) | 0.0353(7) | 0.04 |
| Ca | 0.2228(14) | 0.2260(15) | 0.4964(16) | 0.0353(7) | 0.04 |
| Ca | 0.2537(14) | 0.2166(13) | 0.4528(14) | 0.0353(7) | 0.04 |
| Ca | 0.2589(12) | 0.2548(10) | 0.4145(11) | 0.0353(7) | 0.04 |
| Ca | 0.2898(13) | 0.2453(11) | 0.3708(11) | 0.0353(7) | 0.04 |
| Ca | 0.2950(12) | 0.2835(11) | 0.3326(10) | 0.0353(7) | 0.04 |
| Ca | 0.3259(15) | 0.2741(15) | 0.2889(12) | 0.0353(7) | 0.04 |
| Ca | 0.3311(16) | 0.3123(17) | 0.2506(14) | 0.0353(7) | 0.04 |
| Da | 0.3100(18) | 0.3879(19) | 0.2264(16) | 0.0353(7) | 0.04 |
| Da | 0.2545(16) | 0.4060(15) | 0.3037(15) | 0.0353(7) | 0.04 |
| Da | 0.2184(13) | 0.3773(12) | 0.3857(13) | 0.0353(7) | 0.04 |
| Da | 0.1823(13) | 0.3485(14) | 0.4676(15) | 0.0353(7) | 0.04 |
| Da | 0.1740(14) | 0.2796(18) | 0.5351(17) | 0.0353(7) | 0.04 |
| Da | 0.2182(17) | 0.1980(18) | 0.5260(19) | 0.0353(7) | 0.04 |
| Da | 0.2736(18) | 0.1799(14) | 0.4486(17) | 0.0353(7) | 0.04 |
| Da | 0.3097(17) | 0.2086(13) | 0.3667(14) | 0.0353(7) | 0.04 |
| Da | 0.3458(18) | 0.2374(16) | 0.2848(15) | 0.0353(7) | 0.04 |
| Da | 0.3541(19) | 0.3063(20) | 0.2172(16) | 0.0353(7) | 0.04 |

a) atoms are constrained by rigid body

Table 5 : Results of the Rietveld refinement of 2,3-benzanthracene in NaY.

| Atom | x | y | z | Occupation factor | Biso [Å2] |
| --- | --- | --- | --- | --- | --- |
| Si | 0.12494(35) | 0.94813(31) | 0.0343(4) | 0.7 | 0.0110(12) |
| Al | 0.12494(35) | 0.94813(31) | 0.0343(4) | 0.3 | 0.0110(12) |
| O | 0.25321(27) | 0.25321(27) | 0.1444(4) | 1.0 | 0.0362(8) |
| O | 0.10559(22) | 0.89441(22) | 0.0 | 1.0 | 0.0249(8) |
| O | 0.17595(27) | 0.17595(27) | 0.3205(4) | 1.0 | 0.0259(8) |
| O | 0.17740(24) | 0.17740(24) | 0.9675(4) | 1.0 | 0.0257(8) |
| Na | 0.0 | 0.0 | 0.0 | 0.38(5) | 0.051(6) |
| Na | 0.0591(6) | 0.0591(6) | 0.0591(6) | 0.735(33) | 0.051(6) |
| Na | 0.2418(7) | 0.2418(7) | 0.2418(7) | 0.796(33) | 0.051(6) |
| Ca | 0.2924(14) | 0.4061(16) | 0.2145(15) | 0.0571(4) | 0.09 |
| Ca | 0.2645(15) | 0.4075(13) | 0.2670(14) | 0.0571(4) | 0.09 |
| Ca | 0.2722(10) | 0.3631(10) | 0.3058(10) | 0.0571(4) | 0.09 |
| Ca | 0.2443(13) | 0.3644(9) | 0.3583(10) | 0.0571(4) | 0.09 |
| Ca | 0.2520(10) | 0.3200(9) | 0.3971(7) | 0.0571(4) | 0.09 |
| Ca | 0.2242(14) | 0.3214(12) | 0.4496(9) | 0.0571(4) | 0.09 |
| Ca | 0.2319(12) | 0.2770(14) | 0.4884(9) | 0.0571(4) | 0.09 |
| Ca | 0.2040(17) | 0.2783(19) | 0.5409(12) | 0.0571(4) | 0.09 |
| Ca | 0.2117(17) | 0.2339(22) | 0.5797(14) | 0.0571(4) | 0.09 |
| Ca | 0.2473(17) | 0.1882(22) | 0.5660(17) | 0.0571(4) | 0.09 |
| Ca | 0.2752(16) | 0.1868(19) | 0.5135(17) | 0.0571(4) | 0.09 |
| Ca | 0.2675(12) | 0.2312(15) | 0.4747(12) | 0.0571(4) | 0.09 |
| Ca | 0.2954(12) | 0.2299(13) | 0.4222(12) | 0.0571(4) | 0.09 |
| Ca | 0.2877(8) | 0.2743(10) | 0.3834(9) | 0.0571(4) | 0.09 |
| Ca | 0.3156(11) | 0.2730(11) | 0.3309(11) | 0.0571(4) | 0.09 |
| Ca | 0.3078(8) | 0.3174(11) | 0.2921(9) | 0.0571(4) | 0.09 |
| Ca | 0.3357(12) | 0.3160(15) | 0.2396(12) | 0.0571(4) | 0.09 |
| Ca | 0.3280(12) | 0.3604(17) | 0.2008(13) | 0.0571(4) | 0.09 |
| Da | 0.2874(18) | 0.4390(19) | 0.1843(18) | 0.0571(4) | 0.09 |
| Da | 0.2390(21) | 0.4401(15) | 0.2768(18) | 0.0571(4) | 0.09 |
| Da | 0.2189(20) | 0.3971(12) | 0.3681(14) | 0.0571(4) | 0.09 |
| Da | 0.1987(20) | 0.3540(14) | 0.4594(12) | 0.0571(4) | 0.09 |
| Da | 0.1785(22) | 0.3110(20) | 0.5507(14) | 0.0571(4) | 0.09 |
| Da | 0.1912(20) | 0.2337(25) | 0.6197(16) | 0.0571(4) | 0.09 |
| Da | 0.2523(20) | 0.1553(26) | 0.5962(20) | 0.0571(4) | 0.09 |
| Da | 0.3007(21) | 0.1542(22) | 0.5038(21) | 0.0571(4) | 0.09 |
| Da | 0.3208(18) | 0.1972(17) | 0.4124(17) | 0.0571(4) | 0.09 |
| Da | 0.3410(17) | 0.2403(15) | 0.3211(15) | 0.0571(4) | 0.09 |
| Da | 0.3612(17) | 0.2834(18) | 0.2298(15) | 0.0571(4) | 0.09 |
| Da | 0.3485(15) | 0.3606(20) | 0.1608(15) | 0.0571(4) | 0.09 |

a) atoms are constrained by rigid body