Inverse Gas Chromatography study of the thermodynamic behaviour of thermotropic low molar mass and polymeric liquid crystals

Gareth J. Price* and Ian M. Shillcock

Department of Chemistry, University of Bath, Claverton Down, BATH, BA2 7AY, UK.

Fax.  01225 826231.     E-mail: g.j.price@bath.ac.uk

SUPPLEMENTARY DATA

Table S1 Partial molar excess enthalpies (kJ mol-1 ) and entropies (J mol-1 K-1) at infinite dilution for probes in OCB.  (Values in parentheses are the standard deviations)

Mesophase; I; N; SmA. #### PROBE; HE; SE; HE; SE; HE; SE. Pentane; 8.9 (1.8); 15.7 (1.5); 9.5 (3.2); 17.3 (2.3); 1.7 (3.6); -6.0 (1.9). Hexane; 9.7 (0.6); 17.4 (0.3); 11.5 (1.7); 22.1 (1.2); 4.4 (1.5); 1.1 (0.7). Heptane; 10.3 (1.3); 18.5 (0.2); 13.1 (1.4); 26.1 (1.0); 6.7 (1.5); 7.0 (0.7). Octane; 12.6 (0.2); 24.3 (0.2); 14.5 (1.1); 29.3 (0.8); 7.8 (1.5); 9.4 (0.7). Nonane; 10.6 (0.3); 18.4 (0.2); 16.0 (1.9); 35.5 (1.4); 8.9 (1.0); 14.9 (0.6). 2-Methylhexane; 9.2 (0.5); 17.1 (0.6); 14.8 (1.6); 32.3 (1.2); 7.3 (0.6); 10.2 (0.3). 3-Methylhexane; 10.8 (0.4); 21.7 (0.5); 15.2 (0.7); 33.8 (0.5); 8.4 (1.2); 13.8 (0.7). 2,3-Dimethylpentane; 11.5 (0.3); 23.9 (0.2); 15.1 (1.6); 33.7 (0.8); 8.2 (0.5); 13.4 (0.3). 2,4-Dimethylpentane; 11.3 (0.3); 22.5 (0.2); 13.2 (2.4); 27.3 (1.3); 7.0 (1.1); 9.2 (0.7). 2,2,3-Trimethylbutane; 9.0 (0.8); 17.1 (0.9); 13.9 (0.5); 30.3 (0.2); 6.6 (1.1); 8.5 (0.7). Cyclohexane; 10.6 (1.1); 23.8 (1.2); 15.1 (1.9); 36.3 (1.4); 7.0 (0.6); 12.3 (0.3). Benzene; 5.4 (0.5); 16.3 (0.5); 12.0 (1.8); 34.1 (1.6); 4.1 (1.8); 10.8 (1.8). Toluene; 5.4 (0.6); 15.6 (0.6); 12.3 (1.8); 34.4 (1.6); 4.8 (1.3); 12.4 (1.3). Ethylbenzene; 7.7 (0.5); 20.7 (0.6); 14.2 (2.0); 38.4 (1.7); 5.8 (1.3); 13.8 (1.3). o-Xylene; 6.2 (0.6); 17.6 (0.7); 13.7 (2.0); 38.0 (1.7); 5.4 (1.3); 13.6 (1.3). m-Xylene; 6.5 (1.0); 18.1 (1.2); 11.4 (1.7); 30.9 (1.4); 6.1 (1.2); 15.2 (0.5). p-Xylene; 5.9 (1.6); 16.7 (0.7); 12.0 (1.9); 33.2 (1.7); 4.5 (1.5); 11.1 (1.5).

Table S2 Partial molar enthalpies (kJ mol-1 ) and entropies (J mol-1 K-1) of solution at infinite dilution for probes in OCB.  (Values in parentheses are the standard deviations)

Mesophase; I; N; SmA. #### PROBE; -DHsol; -DSsol; -DHsol; -DSsol; -DHsol; -DSsol. Pentane; 14.9 (1.8); 61.5 (1.5); 15.0 (3.2); 62.0 (2.4); 21.5 (3.4); 81.5 (0.2). Hexane; 20.0 (0.9); 68.8 (0.7); 17.7 (1.8); 63.1 (0.1); 24.4 (1.7); 82.7 (1.4). Heptane; 23.0 (0.2); 70.7 (0.1); 20.7 (1.4); 64.9 (0.0); 26.9 (1.1); 83.1 (0.8). Octane; 24.9 (0.2); 69.6 (0.1); 23.9 (1.2); 67.3 (0.0); 31.2 (0.9); 88.8 (0.7). Nonane; 31.2 (0.2); 79.9 (0.2); 28.2 (1.8); 72.0 (1.7); 39.4 (1.0); 105.1 (0.7). 2-Methylhexane; 21.0 (1.0); 65.8 (0.4); 17.3 (1.6); 56.0 (1.2); 18.6 (3.2); 59.4 (2.5). 3-Methylhexane; 20.7 (0.5); 64.3 (0.7); 17.2 (0.7); 54.9 (0.5); 16.4 (3.5); 52.1 (2.0). 2,3-Dimethylpentane; 19.6 (0.2); 61.4 (0.1); 16.8 (1.7); 54.0 (0.9); 17.4 (3.6); 55.4 (2.7). 2,4-Dimethylpentane; 18.8 (1.4); 62.2 (1.2); 17.3 (2.5); 58.7 (1.3); 17.7 (3.2); 59.5 (2.6). 2,2,3-Trimethylbutane; 20.3 (0.8); 65.4 (0.9); 15.2 (0.8); 51.7 (0.6); 15.8 (3.7); 53.3 (3.1). Cyclohexane; 19.4 (1.1); 60.6 (1.2); 15.6 (1.9); 50.5 (0.1); 21.8 (1.3); 68.6 (1.1). Benzene; 25.6 (0.2); 71.4 (0.4); 18.2 (1.8); 51.2 (1.4); 31.4 (0.9); 90.2 (0.6). Toluene; 29.7 (0.2); 75.6 (0.5); 22.2 (2.0); 55.2 (0.2); 33.8 (0.7); 89.4 (0.6). Ethylbenzene; 31.3 (0.2); 74.6 (0.6); 24.1 (2.2); 55.1 (0.2); 36.9 (0.8); 92.8 (0.6). o-Xylene; 33.6 (0.2); 77.8 (0.7); 25.9 (2.2); 56.8 (0.2); 38.6 (0.8); 94.0 (0.6). m-Xylene; 34.2 (0.9); 81.1 (1.7); 28.9 (0.2); 67.3 (0.1); 35.7 (1.2); 87.6 (0.6). p-Xylene; 33.8 (0.2); 80.2 (0.6); 26.6 (2.0); 60.4 (0.2); 38.7 (0.9); 96.0 (0.6).

Table S3 Partial molar excess enthalpies (kJ mol-1 ) and entropies (J mol-1 K-1) at infinite dilution for probes in OBIB.  (Values in parentheses are the standard deviations)

Mesophase; I; N*; SmC. #### PROBE; HE; SE; HE; SE; HE; SE. Octane; 6.7 (0.7); 13.6 (0.7); 16.9 (1.0); 38.9 (0.9); 11.9 (0.7); 24.7 (0.8). Nonane; 8.2 (0.7); 17.0 (0.7); 17.5 (1.0); 39.7 (1.0); 13.7 (0.7); 28.9 (0.7). Decane; 8.8 (1.7); 18.1 (1.3); 18.5 (1.5); 42.0 (1.3); 16.3 (1.0); 35.2 (1.2). Benzene; 4.4 (0.7); 14.1 (0.6); 13.9 (0.4); 37.6 (0.3); 9.3 (0.7); 24.0 (0.7). Toluene; 6.1 (0.2); 18.0 (0.2); 15.0 (0.3); 40.1 (0.2); 11.4 (0.7); 29.2 (0.7). Ethylbenzene; 8.2 (0.5); 26.2 (0.5); 16.7 (0.5); 43.8 (0.5); 14.1 (0.5); 35.5 (0.7). o-Xylene; 9.5 (1.1); 26.7 (0.9); 17.4 (0.4); 46.3 (0.4); 14.9 (0.6); 38.0 (0.7). m-Xylene; 9.0 (0.8); 25.1 (0.7); 16.3 (0.7); 43.2 (0.6); 14.3 (0.6); 36.2 (0.7). p-Xylene; 8.9 (0.7); 25.1 (0.7); 15.8 (0.5); 42.2 (0.4); 15.1 (0.7); 38.9 (1.0).

Table S4 Partial molar enthalpies (kJ mol-1 ) and entropies (J mol-1 K-1) of solution at infinite dilution for probes in OBIB.  (Values in parentheses are the standard deviations)

Mesophase; I; N*; SmC. #### PROBE; -DHsol; -DSsol; -DHsol; -DSsol; -DHsol; -DSsol. Octane; 28.1 (0.6); 77.7 (0.6); 19.3 (1.0); 56.1 (1.5); 25.6 (0.7); 73.6 (0.8). Nonane; 30.7 (0.7); 79.0 (0.7); 23.1 (1.1); 60.3 (1.0); 28.2 (0.7); 74.9 (0.9). Decane; 32.0 (1.7); 76.9 (1.7); 26.4 (1.5); 63.3 (1.2); 30.2 (1.1); 74.4 (1.2). Benzene; 27.1 (1.9); 74.3 (1.7); 14.4 (2.0); 43.0 (2.0); 22.2 (0.5); 64.9 (0.4). Toluene; 28.3 (1.4); 71.1 (1.5); 17.6 (2.1); 44.7 (2.0); 24.0 (0.7); 63.0 (0.6). Ethylbenzene; 30.4 (1.0); 75.8 (1.5); 21.7 (1.3); 50.0 (1.2); 25.3 (0.8); 61.3 (0.9). o-Xylene; 33.1 (1.1); 79.9 (1.5); 23.1 (1.6); 51.0 (1.5); 25.8 (0.7); 59.9 (0.9). m-Xylene; 31.9 (1.0); 78.5 (1.4); 22.7 (1.6); 51.7 (1.5); 25.3 (1.1); 60.1 (1.1). p-Xylene; 31.6 (1.1); 77.6 (1.5); 23.5 (1.6); 53.5 (1.5); 24.1 (0.9); 56.5 (1.0).

Table S5 Partial molar enthalpies (kJ mol-1 ) and entropies (J mol-1 K-1) of solution at infinite dilution for probes in PDMS and PDCBBS.  (Values in parentheses are the standard deviations)

|  | PDMS |  | PDCBBS SmA |  | PDCBBS I |  |
| --- | --- | --- | --- | --- | --- | --- |
| #### PROBE | -DHsol | -DSsol | -DHsol | -DSsol | -DHsol | -DSsol |
| Pentane | 24.5 (0.4) | 42.2 (1.4) | 21.1 (1.1) | 58.6 (0.9) | 14.9 (2.5) | 38.0 (1.8) |
| Hexane | 28.8 (0.3) | 48.2 (1.3) | 25.1 (0.4) | 62.7 (0.7) | 19.9 (2.6) | 46.8 (1.7) |
| Heptane | 32.8 (0.3) | 53.2 (1.3) | 29.3 (0.4) | 67.1 (1.0) | 22.5 (1.0) | 47.9 (0.8) |
| Octane | 36.4 (0.6) | 57.3 (1.6) | 32.2 (0.7) | 68.8 (1.2) | 25.3 (0.5) | 44.3 (1.1) |
| Nonane | 40.3 (0.6) | 62.1 (1.7) | 31.7 (0.8) | 56.7 (1.4) | 29.6 (0.2) | 56.7 (0.2) |
| 2-Methylhexane | 31.5 (0.3) | 51.5 (0.6) | 24.9 (1.6) | 58.7 (1.5) | 17.8 (1.2) | 40.6 (1.0) |
| 3-Methylhexane | 31.8 (0.3) | 51.7 (0.7) | 26.8 (2.3) | 63.3 (1.6) | 19.4 (0.6) | 42.1 (0.4) |
| 2,3-Dimethylpentane | 31.4 (0.2) | 51.0 (0.3) | 24.9 (1.9) | 59.9 (1.8) | 20.2 (2.5) | 50.8 (2.2) |
| 2,4-Dimethylpentane | 30.2 (0.1) | 50.1 (0.3) | 23.5 (1.8) | 58.3 (1.7) | 18.3 (1.4) | 45.9 (1.2) |
| 2,2,3-Trimethylbutane | 29.8 (0.2) | 48.3 (0.3) | 23.4 (1.6) | 52.8 (2.3) | 17.6 (4.3) | 51.8 (1.2) |
| Cyclohexane | 29.1 (0.2) | 44.6 (0.3) | 22.8 (0.9) | 53.4 (0.9) | 29.0 (0.0) | 63.0 (1.1) |
| Benzene | 29.4 (0.3) | 45.3 (0.8) | 28.8 (0.7) | 61.7 (0.9) | 25.3 (0.7) | 56.3 (1.0) |
| Toluene | 33.5 (0.3) | 50.4 (0.8) | 32.2 (0.7) | 64.1 (1.0) | 28.5 (0.4) | 58.2 (0.8) |
| Ethylbenzene | 37.9 (0.5) | 57.5 (1.3) | 34.5 (0.7) | 64.1 (1.4) | 30.2 (0.5) | 58.9 (1.2) |
| o-Xylene | 35.8 (0.8) | 49.9 (3.2) | 36.3 (0.8) | 65.3 (1.6) | 32.2 (0.5) | 60.1 (0.9) |
| m-Xylene | 35.3 (0.6) | 49.9 (2.4) | 31.4 (0.3) | 57.6 (0.3) | 31.8 (0.4) | 57.5 (0.4) |
| p-Xylene | 35.5 (0.7) | 50.2 (2.5) | 35.2 (0.8) | 67.8 (0.7) | 31.5 (0.6) | 54.9 (0.5) |