Supplementary Information for

Strong and Reciprocal Magneto-Phonon Effects in a 2D Antiferromagnetic Semiconductor FePSe3

Yue Sun, ‡a Bo Liu, ‡a Chee Kwan Gan, b Shian Xia, a Haoyun Lina, Sheng Liu*a, Ting Yu*ac

*Corresponding authors

a School of Physics and Technology, Wuhan University, Wuhan 430072, China;

E-mail: yu.ting@whu.edu.cn and liu.sheng@whu.edu.cn

b Institute of High Performance Computing (IHPC), Agency for Science, Technology and Research (A*STAR), 1 Fusionopolis Way, #16-16 Connexis, Singapore 138632, Republic of Singapore

c Wuhan Institute of Quantum Technology, Wuhan 430206, China

‡ These authors contributed equally to this work.

Figure S1.  The optical image of the sample

The Fig. S1 is an image of the few-layer FePSe3. The cross in the figure is the location of the sample tested, which is about 20μm. The Raman scattering of the features in FePSe3 from monolayer to bulk only changes in intensity, do not offer any detectable difference on the phonon frequency, line width, and shape. The diameter of gaussian spot of the laser beam (~0.8μm), calculated from the objective numerical aperture (NA=0.84) and laser wavelength(532nm), is significantly smaller than the sample size (~20μm). This spatial scale ensures minimal global thermal perturbation, regarding the preserved global magnetic order.

Figure S2. Magnetic-field-dependent peak position of MP1, MP2, M1, M2, P1, P2. The solid lines are fits to the Zeeman splitting of M1 and M2.

As shown in Fig. S2, with the magnetic field increase, the two MP (MP+, MP-) modes split to four peaks(M+、P+、P-、M+). The M+、M- show the Zeeman splitting with a g-factor of -0.71 and 0.66 cm-1/T, respectively, so they are more magnon-like , while the inner ones are more phonon-like and approach each other as the field increases and finally degenerate into one phonon.

Figure S3.  Power dependence of Raman spectra at high frequency at 0T of bulk FePSe3.

Fig. S3 The energy of high-frequency phonons exhibits negligible variation with increasing laser power when the power is below 4mW. This observation indicates that these three phonon modes are relatively insensitive to temperature changes and suggests that it is more challenging to modulate these phonons through localized laser heating than modulate the phonons coupled with magnon.

Figure S4. (a) Temperature dependence Raman spectra of phonon and magnons in few-layer FePSe3, measured from 2 K to 65 K at 6T.(b) The peak position of Raman as a function of laser power and temperature at 6T. Symbols denote Raman peaks: circles (M-), squares (P), triangles (M+). Colors indicate experimental conditions: black (temperature-dependent), red (power-dependent).

Fig. S4(a) displays the temperature-dependent Raman spectra under a 6 T magnetic field. A distinct red-shift is observed in both M+ and M- magnon branches when the temperature exceeds 30 K, whereas the P branch exhibits no variation, that correlates well with the power-dependent measurements.

The temperature- and power-dependent peak energy of M+, M- and P are plotted in Fig. S4(b), with red traces representing laser power dependence and black traces corresponding to temperature evolution. As demonstrated in the figure, the energy variations caused by temperature and power vibration exhibit identical trends, indicating a unified modulation mechanism governing these correlated responses.

Figure S5. Circular polarized Raman of FePSe3 at 0T with the laser power 0.5mW

Fig. S5 presents the circularly-polarized Raman spectra, revealing that the MP+ and MP- branches exhibit chiral characteristics with a measured degree of circular polarization (DCP) of ~14%. While the observed chirality cannot be unambiguously attributed solely to magnons, phonons, or their coupling through our experiment data. However, previous study of magnon-phonon coupling in FePSe3[1] prove the left- and right-handed chiral phonon modes selectively couple to spin-up and spin-down magnons via spin-locked selection rules.

Figure S6. linear polarization Raman spectra of FePSe3 and Si at 0T.

Fig. S6 provides a detailed illustration of the polarization-dependent Raman intensity spectra of high-frequency phonons. It is evident that the phonon modes at 148 cm⁻¹ and 216 cm⁻¹ exhibit Ag symmetry, with their Raman intensities varying significantly with changes in the polarization direction. This behavior reflects a pronounced anisotropic characteristic, and these phonon modes demonstrate a clear twofold rotational symmetry. In contrast, the phonon mode at 170 cm⁻¹, which exhibits Eg symmetry, shows no sensitivity to the polarization direction of the incident light in its Raman scattering intensity. This indicates that the in-plane vibrational mode of the Eg phonon is isotropic, meaning its vibrational direction is uniformly distributed within the crystal plane and does not change with the polarization direction of the light.

Figure S7. The linear polarization Raman of Eg mode of FePSe3 with magnetic field from -6T to 6T.

It shows that the intensity of Eg mode remains almost constant and the polarization direction show no dependence with magnetic field.

Figure S8. (a) The parallel and perpendicular polarization Raman of Si with magnetic flied from -6T to 6T. (b) The linear polarization Raman of Si with magnetic field from -6T to 6T.

The relative Raman intensities measured under XX and XY polarization configurations for silicon (Si) exhibit no dependence on the applied magnetic field. Figure S6b illustrates the angle-dependent linear polarization Raman scattering of Si as the magnetic field varies from -6 T to 6 T. The results indicate that the polarization direction of Si remains constant despite the presence of a twofold anisotropic pattern. This invariance under varying magnetic fields suggests robust polarization characteristics in Si, unaffected by magnetic field variations.

Reference

1. 	J. Cui, E. V. Boström, M. Ozerov, F. Wu, Q. Jiang, J.-H. Chu, C. Li, F. Liu, X. Xu, A. Rubio and Q. Zhang, Nature Communications, 2023, 14, 3396.