Supporting Information

Star Copolymers with Tunable Clusteroluminescence

Zixuan Zhou,1 Xiang Chen,1 Yang Wang,*1 Ting Li,1 Xuhui Zhang,1 Bihua Xia,1 Shibo Wang,1 Weifu Dong,*1 Jinliang Qiao*2

*Corresponding Authors:

Yang Wang: ywang@jiangnan.edu.cn

Weifu Dong: wfdong@jiangnan.edu.cn

Jinliang Qiao: qiaojl.bjhy@sinopec.com

Tel.: +86-510-8532-6290.

1The Key Laboratory of Synthetic and Biological Colloids, Ministry of Education, School of Chemical and Material Engineering, Jiangnan University, 1800 Lihu Road, Wuxi 214122, China;

2SINOPEC, Beijing Research Institute of Chemical Industry, Beijing, 100013, China.

Table of contents

EXPERIMENTAL SECTION	S-3

Figure S1. 1H NMR spectra of RAFT-4.	S-6

Figure S2. FTIR spectra of PMV and SPMV.	S-6

Figure S3. 1H NMR spectra of PMV and SPMV.	S-7

Figure S4. The GPC curve of PMV and SPMV.	S-8

Figure S5. TGA curves of PMV and SPMV.	S-8

Figure S6. DSC curves of PMV and SPMV.	S-9

Figure S7. GPC, DSC curve, an 3D emission spectra of PMV39..	S-9

Figure S8. Decay times of PMV and SPMV.	S-9

Figure S9. The UV-Vis diffuse reflection spectra of PMV and SPMV.	S-10

Figure S10. UV-Vis absorption spectra of PMV and SPMV solutions in THF .	S-10

Figure S11. Plots of PL intensity versus concentration of PMV and SPMV solutions.	S-11

Figure S12. The size distribution of PMV and SPMV solutions in THF (l mg/mL).	S-11

Figure S13. The 3D emission spectra of SPMAh and SPVAc..	S-12

Figure S14. XRD patterns of PMV and SPMV.	S-12

Figure S15. Photographs of SPMV49/PVA film and its 3D photoluminescence spectra.	S-13

Table S1. Photophysical properties, molecular weight, and polydispersity of samples	S-13

- EXPERIMENTAL SECTION

Materials. Maleic anhydride (MAh, 99% purity), chloroform (anhydrous, 99%), 2-bromopropionyl bromide (97%), pentaerythritol (99%), pyridine (99%), hydrochloric acid (HCl, 37% solution in water), sodium bicarbonate (NaHCO3, anhydrous, 99.5%), magnesium sulfate (MgSO4, anhydrous, 98%), potassium O-ethylcarbonodithioate (95%) and other solvents were all supplied by Aladdin-reagent Inc. Vinyl acetate (VAc, 99%), 2,2’-azobisiso-butyronitrile (AIBN, 99%), and 1,4-dioxane (99.5%) were purchased from Sinopharm Chemical Reagent Co. All chemicals and solvents were used as received without further purification.

Synthesis of RAFT agent. The synthetic procedures of RAFT agent RAFT-4 are according to the previous report. Pentaerythritol (1.4 g, 10.0 mmol) was dissolved in 50 mL of chloroform and pyridine (2.5 mL, 31.0 mmol) under the ice bath solution conditions. A solution of 2-bromopropionyl bromide (15 mL, 143.2 mmol) in anhydrous chloroform (25 mL) was added slowly to this stirred, cooled solution for 1 h. The ice bath was then removed and the solution was stirred for 24 h at room temperature (25 °C). Dilute hydrochloric acid (10 %) was slowly added to the mixture. The organic phase was then washed with aqueous NaHCO3 (5%) and dried with MgSO4. A viscous yellow liquid intermediate bromo-compound (4.01 g, 59.4%) was obtained after evaporation of the solvent under reduced pressure.

A solution of the intermediate bromo-compound (3.38 g, 5 mmol) in 50 mL of chloroform was added to a 10-fold excess of potassium O-ethylcarbonodithioate (8.0 g, 50 mmol) in chloroform (25 mL) over 30 min at room temperature, then the mixture was reacted for 48 h. The mixture of remaining sodium (O-ethyl) xanthate was filtered and washed several times with chloroform. The chloroform was evaporated from the solution under reduced pressure. Last, the remaining residue was redissolved in 50 mL of dichloromethane, washed with H2O (2 × 50 mL), and dried using MgSO4. After evaporation of the solvent, the product was obtained as a yellow compound (3.4 g, 75.7%).

Synthesis of PMV. PMV with different molecular weights was synthesized by solution polymerization reported previously.

Synthesis of Star PMV (SPMV). RAFT polymerizations of MAh and VAc were carried out in a 100 mL three-necked flask. At first, MAh (4.9 g, 50 mmol) and VAc monomer (4.6 mL, 50 mmol) were dissolved in 50 mL of 1,4-dioxane in the three-necked flask. Then, RAFT agent RAFT-4 (0.225 g, 0.25 mmol or 0.45 g, 0.50 mmol or 0.9 g, 1 mmol) was dissolved in the solution, followed by AIBN (0.20 n (RAFT agent)) was added into the mixture. The reaction mixture was degassed with N2 for 30 min and then the reactor was immersed in a preheated oil bath at 70 °C for 24 h with magnetic stirring. After that, the reaction was stopped by cooling. The reaction mixture was precipitated and diluted three times with petroleum ether. Finally, the polymers were dried in a vacuum oven at 65 °C to constant weights. The star PMV derivatives were named SPMV (degree of polymerization), resulting in three products named SPMV55, SPMV49, and SPMV31.

Synthesis of tetra-armed MAh (SPMAh) and VAc (SPVAc) homopolymers. At first, MAh (4.9 g, 50 mmol) or VAc monomer (4.6 mL, 50 mmol) were dissolved in 50 mL of 1,4-dioxane in the three-necked flask. Then, RAFT agent RAFT-4 (0.9 g, 1 mmol) was dissolved in the solution, followed by AIBN (0.20 n (RAFT agent)) was added into the mixture. The reaction mixture was degassed with N2 for 30 min and then the reactor was immersed in a preheated oil bath at 70 °C for 24 h with magnetic stirring. After that, the reaction was stopped by cooling. The reaction mixture was dried in a vacuum oven at 80 °C to constant weights.

Characterization. 1H NMR spectra of chemicals were performed on Bruker AVANCE 400 NMR Spectrometer with DMSO-d6. The Fourier transform infrared (FT-IR) spectra were recorded on an FT-IR spectrometer (Nicolet 6700, USA). Polymer molecular weight and molar mass dispersity were determined by gel permeation chromatography (GPC) using THF as eluent, and polystyrene samples were used as standards. Particle sizes were conducted on a zeta potential analyzer (Brookhaven, ZetaPALS). Thermogravimetric analysis was conducted with a heating rate of 10 °C/min. Differential scanning calorimetry tests (DSC-8000, Germany) were conducted under a nitrogen atmosphere and the temperature from 30 °C to 150 °C with a heating and cooling rate of 20 °C/min, and the glass transition temperature (Tg) was determined from the second heating cure at the middle of the step transition. UV absorption spectra were conducted on a UV-vis spectrophotometer (TU-1950, China). UV-vis diffuse reflection spectra were conducted on a UV/vis/NIR spectrophotometer (UV-3600 plus, Japan). Decay times were measured on Lifespec II (Edinburgh, UK). Photoluminescence spectra were taken on a fluorescence spectrometer (FS5, UK). The absolute quantum yields were measured on FLS-1000 (Edinburgh, UK). The TEM images were obtained on JEM-2100plus. XRD patterns were recorded by an XRD analyzer (Bruker-D8, Germany). A two-dimensional multifunctional small angle X-ray scatterer (Xeuss 3.0HR, France) was applied to get the SAXS.

- Figure S1. 1H NMR spectra of RAFT-4.

The peaks at δ = 1.42 and 1.59 are attributed to -CH3, while the signals at 4.41 ppm belongs to -CH. The peaks observed at 4.12 and 4.63 are associated with the RAFT central and terminal methylene protons, respectively. These results indicated the successful synthesis of RAFT-4.

- Figure S2. FTIR spectra of PMV67, SPMV55, SPMV49, and SPMV31.

- For PMV67, the absorption peaks at 1860 cm-1 and 1780 cm-1 correspond to the C=O group in MAh, while the stretching vibration peak at 1735 cm-1 is attributed to the C=O group in VAc. The absorption band at 1215 cm-1 is associated with the C-O stretching vibration of MAh, and the peak at 1029 cm-1 represents the C-O in VAc. The presence of absorption peaks at 1435 cm-1 and 1376 cm-1 indicates the stretching vibration of -CH2 and -CH3 in VAc, respectively.

- Figure S3. 1H NMR spectra of (a) PMV67, (b) SPMV55, (c) SPMV49, and (d) SPMV31.

- The characteristic -CH=CH- peaks of MAh (δ = 7.5) and VAc (δ = 4.9) disappeared, which supported the successful polymerization of monomers. The peaks in the region at δ = 5.2-5.7 are attributed to the -CH of VAc, while the peaks at δ = 1.9-2.3 are associated with the -CH2 and -CH3 on VAc. Furthermore, the δ in the 3.0-3.7 range is assigned to the -CH protons of MAh. In comparison to PMV67, the 1H NMR spectra of the SPMV show new chemical shifts at δ=4.6-4.7 and δ=4.1-4.2 ppm, which are attributed to the -CH2 protons of RAFT-4 (Figure S3b-d). The shift of the -CH proton at δ = 4.41 ppm reveals the complete transfer of the growing macroradical to the thiocarbonylthio group, followed by the leaving group reinitiating the polymerization. Notably, the peak at δ = 4.6-4.7 ppm becomes more visible as the amount of RAFT-4 increases.

- Figure S4. The GPC curve of PMV67, SPMV55, SPMV49, and SPMV31.

- In comparison, SPMV achieves good control of the polymerization kinetics and reduced dispersity with the addition of RAFT-4. As the amount of RAFT agents increased, the peak of each SPMV shifts to a large retention time.

- Figure S5. TGA curves of PMV67, SPMV55, SPMV49, and SPMV31.

- Figure S6. DSC curves of PMV67, SPMV55, SPMV49, and SPMV31.

Figure S7. (a) GPC, (b) DSC curve, and (c) the normalized 3D emission spectra of PMV39.

- Figure S8. Decay times of PMV67, SPMV55, SPMV49, and SPMV31.

- Figure S9. The UV-Vis diffuse reflection spectra of PMV67, SPMV55, SPMV49, and SPMV31.

- The broader absorption observed for PMV and SPMV between 250 and 350 nm are attributed to n-π* transitions of C=O in numerous states. With the increase of RAFT agents, the emergence of new absorption peaks at 370 nm and 500-600 nm indicates the formation of new clusters in the star polymers, which corresponded to the 3D emission spectra.

- Figure S10. UV-Vis absorption spectra of PMV67, SPMV55, SPMV49, and SPMV31 solutions in THF (1 mg/mL).

- Figure S11. Plots of PL intensity versus concentration of PMV67, SPMV55, SPMV49, and SPMV31 solutions in THF.

- Figure S12. The size of PMV67, SPMV55, SPMV49, and SPMV31 solutions in THF (1 mg/mL).

Figure S13. 3D emission spectra of (a) SPMAh, and (b) SPVAc.

- Figure S14. XRD patterns of PMV67, SPMV55, SPMV49, and SPMV31.

- Figure S15. a) Photographs of SPMV49/PVA film under natural light and b) its 3D photoluminescence spectra (inset: the photographs of SPMV49/PVA film under 365 nm UV light.

- Table S1. Photophysical properties, Molecular Weight, and polydispersity of PMV67, SPMV55, SPMV49, and SPMV31.

| Sample | λex(nm) | λem(nm) | QY(%) | (ns) | Mw | Mn | Mn,NMR | Mw/Mn |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| PMV67 | 370 | 450 | 14.86 | 7.84 | 23800 | 12000 | - | 1.99 |
| SPMV55 | 330 | 435 | 13.34 | 6.36 | 12560 | 10810 | 11300 | 1.16 |
| SPMV49 | 510 | 590 | 12.36 | 5.54 | 10940 | 9740 | 9000 | 1.12 |
| SPMV31 | 530 | 605 | 12.37 | 4.82 | 7270 | 6530 | 4500 | 1.11 |