Supplemental information

Three-Dimensional Porphyrin-Based Covalent Organic Frameworks as Bifunctional Electrocatalysts for Oxygen Reduction and Evolution Reactions

Li Liao,‡a,b Rui Wang,‡c Zerong Zhang,c Jianfeng Zhang,c Shibin Huang,c Wenhao Xie,c Yiji Wang,c Ming Xue,a* Qianrong Fang,c* and Shilun Qiuc*

a School of Chemical Engineering and Technology, School of Chemistry, GBRCE for Functional Molecular Engineering, IGCME, Sun Yat-sen University, Guangzhou, 510275, P. R. China

E-mail: xueming5@mail.sysu.edu.cn

b Northeast Guangdong Key Laboratory of New Functional Materials， School of Chemistry and Environment, Jiaying University, Meizhou, 514015, P.R. China.

c State Key Laboratory of Inorganic Synthesis and Preparative Chemistry, Jilin University,

Changchun 130012, P. R. China

E-mail: sqiu@jlu.edu.cn

Table of contents

| Section S1 | Materials and characterization | S3-S11 |
| --- | --- | --- |
| Section S2 | SEM image | S12 |
| Section S3 | TEM image & Mapping | S13-14 |
| Section S4 | FT-IR spectra | S14-15 |
| Section S5 | Solid-state 13C NMR spectra | S16 |
| Section S6 | TGA curves | S16 |
| Section S7 | Nitrogen adsorption | S17-18 |
| Section S8 | XPS spectra | S18-19 |
| Section S9 | PXRD patterns and structures | S19-21 |
| Section S10 | Electrochemistry measurements | S21-23 |
| Section S11 | UV-vis DRS patterns | S24 |
| Section S12 | Unit cell parameters and fractional atomic coordinates | S25-32 |
| Section S13 | Reference | S32 |

Section S1. Materials and characterization

S1.1 Materials

All starting materials and solvents, unless otherwise noted, were obtained from J&K scientific LTD and used without further purification. All products were isolated and handled under nitrogen using either glovebox or Schlenk line techniques.

S1.2 Instruments

Solid-state 13C NMR spectra were recorded on an AVIII 500 MHz solid-state NMR spectrometer. The FTIR spectra (KBr) were obtained using a SHIMADZU IRAffinity-1 Fourier transform infrared spectrophotometer. A SHIMADZU UV-2450 spectrophotometer was used for all absorbance measurements. Thermogravimetric analysis (TGA) was recorded on a SHIMADZU DTG-60 thermal analyzer under N2. The operational range of the instrument was from 30 °C to 800 °C at a heating rate of 10 °C min-1 with N2 flow rate of 30 mL min-1. PXRD data were collected on a PANalytical B.V. Empyrean powder diﬀractometer using a Cu Kα source (λ = 1.5418 Å) over the range of 2θ = 2.0−40.0° with a step size of 0.02° and 2 s per step. The sorption isotherm for N2 was measured by using a Quantachrome Autosorb-IQ analyzer with ultra-high-purity gas (99.999% purity). To estimate pore size distributions for SUZ-101-H, SUZ-101-Co, and SUZ-101-Ni, nonlocal density functional theory (NLDFT) was applied to analyze the N2 isotherm on the basis of the model of N2@77K on carbon with slit pores and the method of non-negative regularization. For scanning electron microscopy (SEM) image, JEOL JSM-6700 scanning electron microscope was applied. Transmission electron microscopy (TEM) image was obtained on JEM-2100 transmission electron microscopy.

S1.3 Electrochemistry measurements

All electrocatalytic measurements were carried out in a three-electrode cell (counter electrode: graphite rod, reference electrode: Hg/HgO electrode in 0.1 M KOH solution, working electrode: different catalytic ink distributed onto the glass carbon electrode). Before formulating the catalyst ink, the three types of COF were ball-milled and ultrasonically exfoliated into nanosheets to allow for full exposure of the active sites of the catalyst. To prepare catalytic ink, SUZ-101-H, SUZ-101-Ni or SUZ-101-Co (6.0 mg) mixed with Carbon Black (a common electrochemical conductive agent) 6.0 mg were dispersed in a mixed solution of isopropanol: DMF = 3:1 at a dispersion concentration of 10 mg∙mL-1 which contain 5 wt.% Nafion solution. Then 7.5 μL of homogeneous ink was pipetted onto the polished rotating disc electrode (RDE) or rotating ring disc electrode (RRDE). The ORR LSV polarization curves were recorded at a scan rate of 10 mV∙s-1 in 0.1 M O2-saturated KOH. Besides, all LSV curves were measured with iR compensation at 100%. The experimental potential values were calibrated by using the following equation: E vs. RHE = E vs. Hg/HgO + 0.098 + 0.059 pH. Before electrochemical modifications and measurements, the reference electrodes were all calibrated by CV tests using glassy carbon electrode as standard work electrode. H2O2 selectivity (H2O2%) and the transfer number electron (n) were determined by RRDE results according to the following equations:

H2O2(%) = 200*(Ir/N)/ (Ir/N+Id)

n = 4* Id/(Ir/N+Id); Ir and Id are the ring current and disk current, respectively, and N is the collection efficiency of the RRDE. Tafel plots were converted from the LSV data at low overpotential fitted to the Tafel equation (η = blog j + a, where η is overpotential, j is the current density, a is the intercept of the y-axis, and b is the Tafel slope). The Electrochemical Impedance spectroscopic (EIS) analysis was carried out by applying an AC voltage with an amplitude of 5 mV and a frequency range of 105-10-1 Hz. The EIS measurement carried at the potential of 0.8 V (vs. RHE) in 0.1 M O2-saturated KOH solution. The electrochemically active surface area (ECSA) of different catalysts was determined based on the double-layer capacitance (Cdl) using a simple cyclic voltammetry method in a non-Faradic potential range of 0.90-1.10 V vs RHE. By plotting the capacitive density at 1.00 V vs RHE against the scan rate (10, 20, 40, 60, 80 and 100 mV∙s-1), a linear trend was observed. The current density was normalized to the geometrical area.

S1.4 Computational Details

All fragment structures were optimized using Gaussian09 software package under B3LYP-D3BJ/6-31+g (d,p) level. The frequencies of the structures were calculated under the same calculation level. High quality single-point energies were calculated using ORCA software package under PWPB95-D3/def2-TZVPP level. All of the quantum chemistry calculations have utilized the SMD solvation module to simulate aqueous environment. The Gibbs free energies were calculated using Shermo software package. Oxygen evolution reaction (OER) is considered to comprise the following four elementary steps in alkaline condition and each step involved transfer of an electron until OH is oxidized to water: Only intermediate states as well as reactants and products were considered. The additional kinetic energy barriers between the intermediates have been neglected with the justification through the Bronsted-Evans Polanyi postulate which states that the activation energy and reaction free energy are linearly correlated.

First-principles calculations in the framework DFT are performed by using the Vienna Ab Initio Simulation Package (VASP) with the projector-augmented wave method (PAW). The cutoff energy for plane wave expansion of the system was set to 600 eV. The exchange-correlation energy was calculated by using the generalized gradient approximation (GGA) of Perdew-Burke-Ernzerhof (PBE). To correct the van der Waals interactions, the DFT-D3 method proposed by Grimme et al. was adopted. The convergence thresholds for electronic self-consistent field and forces acting on the atoms are 1.0×10-7 eV and 1.0×10-4 eV/Å within the current numerical parameters, respectively.

S1.5 Synthesis of meso-tetrakis(4-aminophenyl) porphyrin（TAPP）

TNPP and TAPP were synthesized following the similar method as described in the literature.[1]

Synthesis of TNPP: In a 1000 ml three-neck round-bottom flask equipped with a magnetic stir bar and reflux condenser, 4-nitrobenzaldehyde (22 g, 145.6 mmol) was mixed with propionic acid (600 ml). The mixture was heated to reflux, and pyrrole (10 ml, 145.6 mmol) was then added dropwise, with the reaction mixture kept under reflux for 1.5 hours. The reaction was allowed to cool to room temperature, and the precipitate was collected by filtration. The resulting black precipitate was washed with methanol and dried at 80 °C for 12 hours. The dried precipitate was suspended in 200 ml of pyridine and refluxed with stirring for an additional 1.5 hours. After cooling to room temperature, the suspension was filtered to yield approximately 8.6 g of crude product. The solid product was then repeatedly washed with acetone until the rinses were clear, indicating the absence of dark impurities. Finally, the product was dried at 80 °C for 12 hours to yield TNPP as a reddish-purple solid (6.4 g, 23%).

Synthesis of TAPP: In the obtained product TNPP (2 g, 2.5 mmol), concentrated HCl (100 ml) was added and the solution was bubbled with N₂ for 30 minutes. A solution of SnCl₂·2H₂O (9 g, 40 mmol) in concentrated HCl (150 ml) was then added to the porphyrin solution. The mixture was stirred at 80 °C for 3 hours, then cooled to 0 °C, and subsequently neutralized with aqueous NH₃. Filtration yielded the crude product, a greenish solid. This solid was stirred vigorously with 5% NaOH (200 ml), then filtered, washed with H₂O, and dried at 40 °C for 18 hours to obtain TAPP as a purple solid (1.1 g, 65%). 1H NMR (400 MHz, DMSO, δ/ppm) δ 8.88 (s, 8H), 7.85 (d, J = 7.9 Hz, 8H), 7.00 (d, J = 7.9 Hz, 8H), 5.57 (s, 8H), -2.75 (s, 2H). 13C NMR (101 MHz, DMSO, δ ppm): 148.98, 135.92, 129.20, 121.04, 112.98; MS (EI) m/z: 674 M+.

S1.4 Synthesis of 5,10,15,20-tetrayl(tetrakis(([1,1′:3′,1″-terphenyl]-4,4″-dicarbaldehyde)))-porphyrin（TTEP）

TDBP and TTEP were synthesized following the similar method as described in the literature.[2]

Synthesis of TDBP: In a 250 mL dry round-bottom flask, 3,5-dibromobenzaldehyde (2.64 g, 10 mmol) was added, followed by 120 mL of propionic acid to dissolve the sample. Pyrrole (0.7 mL, 10 mmol) was added dropwise once the reaction mixture was heated to reflux. The system was then maintained at 140 °C for 4 hours. After this period, hot water was poured in, and the mixture was filtered. The residue was washed with hot water and ethanol, then transferred to a vacuum chamber and evacuated to 20 mTorr at 80 °C for 12 hours, yielding 5,10,15,20-tetrakis(3,5-dibromophenyl)-21H,23H-porphyrin (TDBP) as an atropurpureus solid (2.33 g, 75%). This product was used in the next step without further purification.

Synthesis of TTEP: In a 100 mL dry Schlenk flask, TDBP (500 mg, 0.4 mmol), 4-formylphenylboronic acid (880 mg, 4.0 mmol), Pd (PPh₃)₄ (120 mg, 0.10 mmol), and anhydrous K₂CO₃ (1.33 g, 9.6 mmol) were added. The reaction system was then vacuumed for 30 minutes, with argon gas introduced three times. Under argon protection, 30 mL of anoxic tetrahydrofuran and 10 mL of anoxic water were added. The mixture was heated to 100 °C and stirred for 72 hours. Afterward, the mixture was extracted into DCM (3×50 mL), and the solvent was removed under reduced pressure. The crude product was washed with MeOH and purified by flash column chromatography [C18, 40–63 µm, 60 Å, H₂O/MeOH], yielding TTEP as a purple solid (464 mg, 80%). 1H NMR (500 MHz, CDCl3, δ/ppm) δ 10.10 (s, 8H), 9.06 (s, 8H), 8.60 (s, 8H), 8.35 (s, 4H), 8.09 (m, 32H), -2.61 (s, 2H). 13C NMR (125 MHz, CDCl3): δ 191.73, 146.23, 143.58, 139.24, 135.82, 133.45, 130.54, 128.22, 126.02, 119.64.

S1.5 Synthesis of TAPP-M (M= Co and Ni)

TAPP-Co and TAPP-Ni were synthesized following the similar method as described in the literature.[3]

In a 250 mL round-bottom flask, TAPP-Co synthesis was initiated by charging TAPP (400 mg, 0.59 mmol, 1 equiv.), Na OAc (210 mg, 4.3 mmol, 7.28 equiv.), and Co (OAc)₂·4H₂O (1.41 mmol, 2.3 equiv.) in a 1:3 mixture of DMF and C₆H₅Cl (total 76 mL). The reaction mixture was sonicated for 5 minutes, then stirred under nitrogen at 180 °C (reflux) for 24 hours. After natural cooling, the reaction solvents were removed first by rotary evaporation, then by CH₂Cl₂ to eliminate residual DMF. The resulting solid was suspended in CH₂Cl₂ (100 mL), transferred to a Buchner funnel with a glass frit, and filtered under vacuum. The crude product was thoroughly washed with saturated NaHCO₃ solution (3 × 20 mL) and water (3 × 20 mL). The resulting dark purple microcrystalline powder was dried under high vacuum at 80 °C for 12 hours (yield: 85-95%) before further use in COF synthesis. TAPP-Ni (dark purple) was prepared using a similar procedure, substituting Ni (OAc)₂·4H₂O for cobalt salt.

S1.6 Synthesis of TTEP-M (M= Co and Ni)

TTEP-Co and TTEP-Ni were synthesized following the similar method as described in the literature.[4]

In a 250 mL round-bottom flask, TTEP-Co synthesis was carried out by charging TTEP (400 mg, 0.276 mmol, 1 equiv.) and Co (OAc)₂·4H₂O (1.41 mmol, 2.3 equiv.) in DMF (80 mL). The reaction mixture was sonicated for 5 minutes, then stirred under nitrogen at 180 °C (reflux) for 24 hours. After cooling naturally, the mixture was poured into 500 mL of water. The residue was collected by filtration and subsequently purified by flash column chromatography [C18, 40–63 µm, 60 Å, H₂O/MeOH], yielding the product as a brown solid (158.1 mg, 38% yield). TTEP-Ni (dark purple) was prepared using a similar procedure, substituting Ni (OAc)₂·4H₂O for the cobalt salt.

S1.7 Synthesis of COFs

Synthesis of SUZ-101-H: In a Pyrex tube (volume: approximately 20.0 mL, body length: 18.0 cm, neck length: 9.0 cm), TAPP (0.02 mmol, 13.5 mg) and TTEP (0.01 mmol, 14.7 mg) were weighed and added with 0.5 mL of NMP, 0.5 mL of mesitylene, and 0.2 mL of acetic acid (6 M). The Pyrex tube was flash frozen in a liquid nitrogen bath, evacuated to an internal pressure of approximately 19.0 mbar, and flame-sealed, reducing the total length by about 10.0 cm. Once warmed to room temperature, the tube was placed in an oven at 120 °C for 7 days. The resulting precipitate was filtered and exhaustively washed by Soxhlet extraction with acetone for 48 hours. The obtained powder was then immersed in anhydrous acetone, with the solvent exchanged multiple times with fresh acetone. The wet sample was transferred to a supercritical dryer (Samdri-PTV-3D), where it was washed six times with liquid CO₂ and exchanged with fresh CO₂ six times at intervals of half an hour. The system was heated to 45 °C to reach the supercritical state of CO₂, which was then bled off at a very slow rate to ambient pressure. Finally, the sample was transferred to a vacuum chamber and evacuated to 20 mTorr at room temperature, resulting in the formation of approximately 20 mg of a blackish-purple powder suitable for N₂ adsorption measurements.

Synthesis of SUZ-101-Co: In a Pyrex tube (volume: approximately 20.0 mL, body length: 18.0 cm, neck length: 9.0 cm), TAPP-Co (0.02 mmol, 14.6 mg) and TTEP-Co (0.01 mmol, 15.1 mg) were weighed and combined with 0.5 mL of NMP, 0.5 mL of mesitylene, and 0.2 mL of acetic acid (6 M). The Pyrex tube was flash frozen in a liquid nitrogen bath, evacuated to an internal pressure of approximately 19.0 mbar, and flame-sealed, reducing the total length by about 10.0 cm. After warming to room temperature, the tube was placed in an oven at 120 °C for 7 days. The resulting precipitate was filtered and thoroughly washed by Soxhlet extraction with acetone for 48 hours. The obtained powder was then immersed in anhydrous acetone, with multiple solvent exchanges using fresh acetone. The wet sample was transferred to a supercritical dryer (Samdri-PTV-3D), where it was washed six times with liquid CO₂, followed by six exchanges with fresh CO₂ at half-hour intervals. The system was heated to 45 °C to achieve the supercritical state of CO₂, which was then bled off very slowly to ambient pressure. Finally, the sample was transferred to a vacuum chamber and evacuated to 20 mTorr at room temperature, resulting in the formation of approximately 18 mg of a blackish-purple powder suitable for N₂ adsorption measurements.

Synthesis of SUZ-101-Ni: In a Pyrex tube (volume: approximately 20.0 mL, body length: 18.0 cm, neck length: 9.0 cm), TAPP-Ni (0.02 mmol, 14.6 mg) and TTEP-Ni (0.01 mmol, 15.1 mg) were weighed and combined with 0.5 mL of NMP, 0.5 mL of mesitylene, and 0.2 mL of acetic acid (6 M). The Pyrex tube was flash frozen in a liquid nitrogen bath, evacuated to an internal pressure of approximately 19.0 mbar, and flame-sealed, reducing the total length by about 10.0 cm. Once warmed to room temperature, the tube was placed in an oven at 120 °C for 7 days. The resulting precipitate was filtered and exhaustively washed by Soxhlet extraction with acetone for 48 hours. The obtained powder was then immersed in anhydrous acetone, with multiple exchanges using fresh acetone. The wet sample was transferred to a supercritical dryer (Samdri-PTV-3D), where it was washed six times with liquid CO₂ and subsequently exchanged with fresh CO₂ six times at half-hour intervals. The system was heated to 45 °C to achieve the supercritical state of CO₂, which was then bled off very slowly to ambient pressure. Finally, the sample was transferred to a vacuum chamber and evacuated to 20 mTorr at room temperature, resulting in the formation of approximately 16 mg of a blackish-purple powder suitable for N₂ adsorption measurements.

Section S2. SEM image

Figure S1. SEM image of SUZ-101-H.

Figure S2. SEM image of SUZ-101-Co.

Figure S3. SEM image of SUZ-101-Ni.

Section S3. TEM image ＆ Mapping

Figure S4. TEM image of SUZ-101-H.

Figure S5. TEM image of SUZ-101-Co.

Figure S6 TEM image of SUZ-101-Ni.

Figure S7. Mapping of SUZ-101-Ni.

Section S4. FT-IR spectra

Figure S8. FT-IR spectra of SUZ-101-H (orange) and TAPP (purple), TTEP (green).

Figure S9. FT-IR spectra of SUZ-101-Co (orange) and TAPP (purple), TTEP (green).

Figure S10. FT-IR spectra of SUZ-101-Ni (orange) and TAPP (purple), TTEP (green).

Section S5. Solid-state 13C NMR spectra

Figure S11. Solid state 13C NMR of SUZ-101-H.

Section S6. TGA curves

Figure S12. TGA curve of SUZ-101-H (bule) and SUZ-101-Co (red) and SUZ-101-Ni (green).

Section S7. Nitrogen adsorption

Figure S13. BET plot of SUZ-101-H calculated from N2 adsorption isotherm at 77 K.

Figure S14. BET plot of SUZ-101-Co calculated from N2 adsorption isotherm at 77 K.

Figure S15. BET plot of SUZ-101-Ni calculated from N2 adsorption isotherm at 77 K.

Section S8.  XPS spectra

Figure S16. High resolution N 1s XPS profiles of a) TAPP; b) TTEP; c) SUZ-101-H.

Figure S17. High resolution Co 2p XPS profiles of a) TTAP-Co, b) TTEP-Co.

Figure S18. High resolution Ni 2p XPS profiles of a) TAPP-Ni, b) TTEP-Ni.

Section S9. PXRD patterns and structures

Figure S19. a) The structure of SUZ-101-H based on the scu net viewed along a axis. b) The structure of SUZ-101-H based on the scu net viewed along b axis. c) PXRD pattern of SUZ-101-H based on the scu net.

Figure S20. a) The structure of SUZ-101-Co based on the scu net viewed along a axis. b) The structure of SUZ-101-Co based on the scu net viewed along b axis. c) PXRD pattern of SUZ-101-Co based on the scu net.

Figure S21. a) The structure of SUZ-101-Ni based on the scu net viewed along a axis. b) The structure of SUZ-101-Ni based on the scu net viewed along b axis. c) PXRD pattern of SUZ-101-Ni based on the scu net.

Figure S22. a) The structure of SUZ-101-H based on the csq net viewed along a axis. b) The structure of SUZ-101-H based on the csq net viewed along b axis. c) PXRD pattern of SUZ-101-H based on the csq net.

Figure S23. a) The structure of SUZ-101-H based on the sqc net viewed along a axis. b) The structure of SUZ-101-H based on the sqc net viewed along c axis. c) PXRD pattern of SUZ-101-H based on the sqc net.

Section S10. Electrochemistry measurements

Figure S24. The corresponding Tafel slopes of SUZ-101-H (orange), SUZ-101-Co (pink), SUZ-101-Ni (blue) and CB (purple) in O2-saturated 0.1 M KOH for ORR.

Figure S25. CV curves of a) SUZ-101-H, b) SUZ-101-Co, c) SUZ-101-Ni, d) CB in 0.1 M KOH solution at different scan rates (10, 20, 40, 60, and 80 mV s-1).

Figure S26. a) Chronopotentiometry curves of SUZ-101-Co during ORR and OER (at current density corresponding to wave potential and current density of 10 mA cm-2, respectively). b) Stability of SUZ-101-Co and commercial catalyst RuO2 at 1.5 V. c) Stability of SUZ-101-Co and commercial catalyst Pt/C at 0.76 V.

Figure S27. Current−time curve of SUZ-101-H at 0.78 V vs RHE.

Figure S28. Optimized structures of a) SUZ-101-Co and b) SUZ-101-Ni molecular fragment.

Section S11. UV-vis DRS patterns

Figure S29. Optical band gap by Tauc plot of SUZ-101-H.

Figure S30. Optical band gap by Tauc plot of SUZ-101-Co.

Figure S31. Optical band gap by Tauc plot of SUZ-101-Ni.

Supplementary Table

Table S1 Performance statistics of COF-based bifunctional electrocatalysts reported in the literatures.

| Catalyst | Overpotential at 10 mA cm−2 [RHE] | Half-wave potential | ΔE | Ref. |
| --- | --- | --- | --- | --- |
| 3D COF |  |  |  |  |
| SUZ-101-Co | 240 mV | 0.78 V | 0.69 V | This Work |
| 2D COF |  |  |  |  |
| Ag/Ag2O@MCOF(Co) | 260 mV | 0.76 V | 0.73 V | ACS Sustainable Chem. Eng. 2021, 9, 5872−5883 |
| C-Fe,Co-COF | 280 mV | 0.81 V | 0.7 V | Chem. Eur. J. 2019, 25, 3105 – 3111 |
| Ni/Fe-COF@CNT900 | 320 mV | 0.87 V | 0.68 V | Adv. Sustainable Syst. 2020, 4, 2000115. |
| CNFs/CoZn-MOF@COF | 320 mV | 0.82 V | 0.73 V | J. Colloid Interf. Sci. 2024, 666, 35–46. |
| Nb2CO2@COF | 373 mV | 0.81 V | 0.79 V | ACS Appl. Mater. Interfaces 2022, 14, 10738−10746 |
| CoTAPP-PATA-COF | 420 mV | 0.80 V | 0.85 V | Angew. Chem. Int. Ed. 2022, 61, e202213522. |
| CoFe-COFbpda/CNT-700 | 440 mV | 0.862 V | 0.808 V | ChemNanoMat 2022, 8, e202200330. |
| FeCo@NC | 440 mV | 0.86 V | 0.81 V | Carbon Neutralization. 2024; 3:689–699. |
| CoNP-PTCOF | 450 mV | 0.85 V | 0.83 V | Adv. Funct. Mater. 2021, 31, 2101727. |
| Co-COFs/CNT-700 | 470 mV | 0.83 V | 0.87 V | ChemNanoMat 2024, 10, e202400068 |
| CoNP-s-IMCOF | 500 mV | 0.83 V | 0.9 V | ACS Appl. Mater. Interfaces 2022, 14, 24404−24414. |
| Co-CTF/KB | 550 mV | 0.83 V | 0.95 V | Sci. China Mater. 2021, 64(9): 2221–2229 |
| Porphyrin |  |  |  |  |
| CoIITP[CoIIIC]2 | 412 mV | 0.72 V | 0.922 V | Angew. Chem. Int. Ed. 2023, 62, e202302208 |
| Fe porphyrin 1 | 500 mV | 0.84 V | 0.89 V | Angew. Chem. 2021, 133, 7654 –7659 |
| Other |  |  |  |  |
| NCNTs | 370 mV | 0.84 V | 0.76 V | Nat. Energy 2016, 1, 15006 |
| NCMT | 290 mV | 0.89 V | 0.63 V | Energy Environ. Sci. 2016, 9, 3079 |
| P, N Co-doped graphene | 320 mV | 0.845 V | 0.705 V | Sci. Adv. 2016, 2, e1501122 |
| Co-N-C | 310 mV | 0.80 V | 0.74 V | J. Am. Chem. Soc. 2016, 138, 10226 |
| NiCo2O4/NCNTs/NiCo | 350 mV | 0.83 V | 0.75 V | Chem. Eng. J. 2021, 408, 127814 |
| Ni/NiO | 260 mV | 0.76 V | 0.73 V | Nano-Micro Lett. 2020, 12, 68 |
| ODAC-CoO | 364 mV | 0.849 V | 0.745 V | Adv. Funct. Mater. 2021, 31, 2101239 |
| Co@Co3O4/PNC | 350 mV | 0.89 V | 0.69 V | Small 2023, 19, 2300621 |
| Mn/Co-450 | 380 mV | 0.78 V | 0.83 V | Appl. Catal., B 2022, 319, 121909 |
| P-CoO@PWC | 290 mV | 0.84 V | 0.68 V | Adv. Sci. 2021, 8, 2101314 |

Section S12: Unit cell parameters and fractional atomic coordinates

Table S2. Unit cell parameters and fractional atomic coordinates for SUZ-101-H calculated based on the scu net.

| Space group |  | CMCM |  |  |
| --- | --- | --- | --- | --- |
| Calculated unit cell |  | a = 52.2607 Å, b = 13.0996 Å, c = 52.2607 Å, α = β = γ = 90° |  |  |
| Measured unit cell |  | a = 52.2592 Å, b = 13.0951 Å, c = 52.2688 Å, α = β = γ = 90° |  |  |
| Pawley refinement |  | RP = 2.61%, RWP = 2.83% |  |  |
| atoms | x |  | y | z |
| C1 | 0.90324 |  | 0.54955 | 0.59837 |
| C2 | 0.83865 |  | 0.33008 | 1.07525 |
| C3 | 0.17863 |  | 0.33494 | 1.09737 |
| N4 | 0.17426 |  | 0.28016 | 1.11742 |
| C5 | 0.44627 |  | 0.5817 | 0.99924 |
| C6 | 0.43282 |  | 0.23775 | 1.0036 |
| C7 | 0.63245 |  | 0.97431 | 0.8521 |
| C8 | 0.64849 |  | 0.91907 | 0.83555 |
| C9 | 0.31013 |  | 0.22095 | 0.63981 |
| C10 | 0.27928 |  | 0.23418 | 0.68362 |
| C11 | 0.31551 |  | 0.29277 | 0.65869 |
| C12 | 0.30019 |  | 0.29977 | 0.68033 |
| C13 | 0.77403 |  | 0.66094 | 0.66488 |
| C14 | 0.71058 |  | 0.84615 | 1.35681 |
| C15 | 0.90343 |  | 0.62908 | 0.61799 |
| N16 | 0.89001 |  | 0.63962 | 0.63854 |
| C17 | 0.35983 |  | 0.12655 | 0.67247 |
| C18 | 0.33985 |  | 0.9681 | 0.6852 |
| C19 | 0.656 |  | 0.92756 | 1.31124 |
| C20 | 0.12834 |  | 0.57904 | 0.65196 |
| C21 | 0.26026 |  | 0.7441 | 1.29599 |
| C22 | 0.26695 |  | 0.76216 | 1.27041 |
| C23 | 0.28968 |  | 0.80768 | 1.26304 |
| C24 | 0.23703 |  | 0.69787 | 1.30354 |
| C25 | 0.23183 |  | 0.67115 | 1.32837 |
| C26 | 0.1762 |  | 0.58715 | 1.20418 |
| C27 | 0.1682 |  | 0.58474 | 1.2297 |
| C28 | 0.14426 |  | 0.55063 | 1.23705 |
| C29 | 0.19984 |  | 0.62818 | 1.19644 |
| C30 | 0.20811 |  | 0.62653 | 1.17162 |
| N31 | 0.21745 |  | 0.67168 | 1.28815 |
| C32 | 0.33397 |  | 0.89039 | 1.0538 |
| C33 | 0.36028 |  | 0.76705 | 1.07559 |
| C34 | 0.41437 |  | 0.7682 | 1.01551 |
| C35 | 0.42888 |  | 0.81601 | 0.974 |
| C36 | 0.38147 |  | 0.99526 | 0.9095 |
| C37 | 0.42538 |  | 0.04557 | 0.91635 |
| C38 | 0.38225 |  | 0.93736 | 0.93198 |
| C39 | 0.42625 |  | 0.98801 | 0.9384 |
| C40 | 0.40679 |  | 0.87499 | 0.97037 |
| C41 | 0.35096 |  | 0.88891 | 1.03316 |
| C42 | 0.39196 |  | 0.82608 | 1.01263 |
| C43 | 0.38817 |  | 0.87934 | 0.98969 |
| C44 | 0.40468 |  | 0.93462 | 0.94673 |
| C45 | 0.37717 |  | 0.76586 | 1.05514 |
| C46 | 0.37297 |  | 0.8272 | 1.03371 |
| C47 | 0.54629 |  | 0.68515 | 0.99802 |
| C48 | 0.42087 |  | 0.55191 | 0.99942 |
| C49 | 0.47944 |  | 0.71745 | 0.99738 |
| C50 | 0.48682 |  | 0.81887 | 0.99622 |
| H51 | 0.19598 |  | 0.38763 | 1.09667 |
| H52 | 0.62288 |  | 0.93394 | 0.86869 |
| H53 | 0.65207 |  | 0.83431 | 0.83892 |
| H54 | 0.33255 |  | 0.34644 | 0.65654 |
| H55 | 0.30484 |  | 0.35939 | 0.69534 |
| H56 | 0.7571 |  | 0.60703 | 0.66742 |
| H57 | 0.71486 |  | 0.90649 | 1.37175 |
| H58 | 0.91845 |  | 0.68859 | 0.6128 |
| H59 | 0.36308 |  | 0.21134 | 0.67611 |
| H60 | 0.66564 |  | 0.88613 | 1.29485 |
| H61 | 0.30378 |  | 0.83593 | 1.27791 |
| H62 | 0.24291 |  | 0.67943 | 1.34682 |
| H63 | 0.12941 |  | 0.52947 | 1.22216 |
| H64 | 0.19948 |  | 0.59751 | 1.15318 |
| H65 | 0.31627 |  | 0.94117 | 1.053 |
| H66 | 0.3642 |  | 0.71621 | 1.09265 |
| H67 | 0.41734 |  | 0.72533 | 1.03403 |
| H68 | 0.44374 |  | 0.81247 | 0.95826 |
| H69 | 0.36322 |  | 0.998 | 0.89773 |
| H70 | 0.44312 |  | 0.08999 | 0.91034 |
| H71 | 0.36468 |  | 0.89254 | 0.93829 |
| H72 | 0.44468 |  | 0.984 | 0.94988 |
| H73 | 0.34692 |  | 0.93799 | 1.01581 |
| H74 | 0.36998 |  | 0.92597 | 0.98682 |
| H75 | 0.39478 |  | 0.7145 | 1.05561 |
| H76 | 0.40198 |  | 0.59536 | 0.99881 |
| H77 | 0.47172 |  | 0.88159 | 0.9955 |
| N78 | 0 |  | 0.15493 | 0.99817 |
| N79 | 0.25285 |  | 0.73458 | 1.25 |
| N80 | 0.18294 |  | 0.60727 | 1.25 |
| N81 | 0.46212 |  | 0.5 | 1 |

Table S3. Unit cell parameters and fractional atomic coordinates for SUZ-101-Co calculated based on the scu net.

| Space group |  | CMCM |  |  |
| --- | --- | --- | --- | --- |
| Calculated unit cell |  | a = 52.2186 Å, b = 13.9009 Å, c = 52.2852 Å, α = β = γ = 90° |  |  |
| Measured unit cell |  | a = 52.2199 Å, b = 13.8991 Å, c = 52.2798 Å, α = β = γ = 90° |  |  |
| Pawley refinement |  | RP = 2.97%, RWP = 3.88% |  |  |
| atoms | x |  | y | z |
| C1 | 0.92079 |  | 0.62641 | 0.58421 |
| C2 | 0.83127 |  | 0.27999 | 1.07287 |
| C3 | 0.1886 |  | 0.27277 | 1.09504 |
| N4 | 0.19132 |  | 0.19334 | 1.10947 |
| C5 | 0.44761 |  | 0.57734 | 0.99973 |
| C6 | 0.43506 |  | 0.24996 | 1.0011 |
| C7 | 0.60408 |  | 1.11895 | 0.85096 |
| C8 | 0.62095 |  | 1.07679 | 0.83157 |
| C9 | 0.29082 |  | 0.32747 | 0.63183 |
| C10 | 0.25656 |  | 0.37892 | 0.67542 |
| C11 | 0.28959 |  | 0.42232 | 0.64188 |
| C12 | 0.27259 |  | 0.4481 | 0.66344 |
| C13 | 0.75787 |  | 0.78329 | 0.66582 |
| C14 | 0.72505 |  | 0.74263 | 1.35583 |
| C15 | 0.9223 |  | 0.72342 | 0.59767 |
| N16 | 0.90793 |  | 0.75685 | 0.61813 |
| C17 | 0.36763 |  | 0.2541 | 0.64311 |
| C18 | 0.35651 |  | 1.12371 | 0.67545 |
| C19 | 0.64918 |  | 0.7877 | 1.33743 |
| C20 | 0.10988 |  | 0.7075 | 0.636 |
| C21 | 0.2383 |  | 0.59182 | 1.30196 |
| C22 | 0.24413 |  | 0.60895 | 1.27316 |
| C23 | 0.26568 |  | 0.65707 | 1.26465 |
| C24 | 0.2166 |  | 0.54364 | 1.31034 |
| C25 | 0.21033 |  | 0.52848 | 1.33903 |
| C26 | 0.16036 |  | 0.41646 | 1.19801 |
| C27 | 0.15423 |  | 0.40169 | 1.22685 |
| C28 | 0.13312 |  | 0.35083 | 1.23537 |
| C29 | 0.18186 |  | 0.46563 | 1.18963 |
| C30 | 0.18833 |  | 0.47923 | 1.16095 |
| N31 | 0.19909 |  | 0.50558 | 1.29234 |
| C32 | 0.33458 |  | 0.86566 | 1.0574 |
| C33 | 0.34721 |  | 0.70188 | 1.0671 |
| C34 | 0.41535 |  | 0.75322 | 1.01891 |
| C35 | 0.43522 |  | 0.81546 | 0.9759 |
| C36 | 0.39841 |  | 1.0726 | 0.91729 |
| C37 | 0.44178 |  | 0.09404 | 0.93136 |
| C38 | 0.39708 |  | 0.98949 | 0.93427 |
| C39 | 0.44031 |  | 1.01213 | 0.94873 |
| C40 | 0.41551 |  | 0.88132 | 0.97236 |
| C41 | 0.35412 |  | 0.8744 | 1.03731 |
| C42 | 0.39381 |  | 0.80937 | 1.01377 |
| C43 | 0.3943 |  | 0.87449 | 0.99045 |
| C44 | 0.41776 |  | 0.96016 | 0.95088 |
| C45 | 0.36667 |  | 0.71054 | 1.04714 |
| C46 | 0.37113 |  | 0.79814 | 1.03268 |
| C47 | 0.54518 |  | 0.67382 | 1.00102 |
| C48 | 0.42272 |  | 0.54834 | 0.99908 |
| C49 | 0.47986 |  | 0.70079 | 1.00394 |
| C50 | 0.48727 |  | 0.79542 | 1.00779 |
| H51 | 0.20066 |  | 0.33404 | 1.09887 |
| H52 | 0.58635 |  | 1.08374 | 0.85535 |
| H53 | 0.61617 |  | 1.00908 | 0.82138 |
| H54 | 0.30181 |  | 0.4767 | 0.63275 |
| H55 | 0.27181 |  | 0.5221 | 0.67073 |
| H56 | 0.74567 |  | 0.72908 | 0.67509 |
| H57 | 0.72438 |  | 0.81698 | 1.36256 |
| H58 | 0.93582 |  | 0.77293 | 0.58846 |
| H59 | 0.36328 |  | 0.32353 | 0.63376 |
| H60 | 0.66634 |  | 0.75016 | 1.33184 |
| H61 | 0.28019 |  | 0.68802 | 1.27815 |
| H62 | 0.22054 |  | 0.55077 | 1.35812 |
| H63 | 0.11911 |  | 0.31661 | 1.22189 |
| H64 | 0.17828 |  | 0.45571 | 1.14188 |
| H65 | 0.32236 |  | 0.92661 | 1.06125 |
| H66 | 0.34484 |  | 0.63392 | 1.0782 |
| H67 | 0.4164 |  | 0.70653 | 1.03755 |
| H68 | 0.45077 |  | 0.81518 | 0.96078 |
| H69 | 0.38136 |  | 1.09714 | 0.90707 |
| H70 | 0.45912 |  | 0.1349 | 0.93115 |
| H71 | 0.37949 |  | 0.95054 | 0.9354 |
| H72 | 0.4565 |  | 0.99217 | 0.96159 |
| H73 | 0.35639 |  | 0.94266 | 1.02658 |
| H74 | 0.37842 |  | 0.92064 | 0.98645 |
| H75 | 0.37822 |  | 0.64788 | 1.04321 |
| H76 | 0.40584 |  | 0.59111 | 0.99777 |
| H77 | 0.47558 |  | 0.85857 | 1.0102 |
| N78 | 0 |  | 0.14085 | 1.00269 |
| N79 | 0.23051 |  | 0.57928 | 1.25 |
| N80 | 0.16759 |  | 0.43305 | 1.25 |
| N81 | 0.46326 |  | 0.5 | 1 |
| Co82 | 0.5 |  | 0.5 | 0.5 |
| Co83 | 0.30093 |  | 0.00592 | 0.25 |

Table S4. Unit cell parameters and fractional atomic coordinates for SUZ-101-Ni calculated based on the scu net.

| Space group |  | CMCM |  |  |
| --- | --- | --- | --- | --- |
| Calculated unit cell |  | a = 51.2941 Å, b = 13.8791 Å, c = 52.2124 Å, α = β = γ = 90° |  |  |
| Measured unit cell |  | a = 51.2984 Å, b = 13.8802 Å, c = 52.2109 Å, α = β = γ = 90° |  |  |
| Pawley refinement |  | RP = 2.76%, RWP = 3.20% |  |  |
| atoms | x |  | y | z |
| C1 | 0.90531 |  | 0.55386 | 0.59351 |
| C2 | 0.83507 |  | 0.32567 | 1.07607 |
| C3 | 0.1827 |  | 0.33452 | 1.09838 |
| N4 | 0.18207 |  | 0.27101 | 1.11671 |
| C5 | 0.44613 |  | 0.57679 | 0.99941 |
| C6 | 0.43242 |  | 0.25222 | 1.00279 |
| C7 | 0.62112 |  | 0.99211 | 0.85011 |
| C8 | 0.63551 |  | 0.94064 | 0.83167 |
| C9 | 0.30224 |  | 0.23216 | 0.63958 |
| C10 | 0.27099 |  | 0.25197 | 0.68379 |
| C11 | 0.30393 |  | 0.3148 | 0.6549 |
| C12 | 0.28846 |  | 0.32488 | 0.67673 |
| C13 | 0.76995 |  | 0.66694 | 0.66922 |
| C14 | 0.71447 |  | 0.84327 | 1.35272 |
| C15 | 0.90488 |  | 0.63915 | 0.61061 |
| N16 | 0.89122 |  | 0.65223 | 0.63134 |
| C17 | 0.35698 |  | 0.13857 | 0.66277 |
| C18 | 0.34637 |  | 0.98864 | 0.68407 |
| C19 | 0.65735 |  | 0.91222 | 1.31903 |
| C20 | 0.12513 |  | 0.59175 | 0.64682 |
| C21 | 0.25124 |  | 0.72775 | 1.2959 |
| C22 | 0.25708 |  | 0.7446 | 1.27045 |
| C23 | 0.27982 |  | 0.79014 | 1.26296 |
| C24 | 0.2281 |  | 0.68416 | 1.30297 |
| C25 | 0.22183 |  | 0.66737 | 1.32838 |
| C26 | 0.1691 |  | 0.56316 | 1.20405 |
| C27 | 0.16224 |  | 0.55399 | 1.22956 |
| C28 | 0.13954 |  | 0.50824 | 1.23706 |
| C29 | 0.19157 |  | 0.61101 | 1.19699 |
| C30 | 0.19877 |  | 0.62093 | 1.17161 |
| N31 | 0.20944 |  | 0.65032 | 1.28674 |
| C32 | 0.33498 |  | 0.89621 | 1.05684 |
| C33 | 0.35241 |  | 0.74795 | 1.07381 |
| C34 | 0.41464 |  | 0.76074 | 1.01731 |
| C35 | 0.4289 |  | 0.79821 | 0.97432 |
| C36 | 0.38306 |  | 0.99902 | 0.91249 |
| C37 | 0.42805 |  | 0.04003 | 0.92094 |
| C38 | 0.38356 |  | 0.93364 | 0.93312 |
| C39 | 0.4286 |  | 0.97511 | 0.94126 |
| C40 | 0.40732 |  | 0.85888 | 0.97092 |
| C41 | 0.35277 |  | 0.89188 | 1.03647 |
| C42 | 0.39144 |  | 0.81389 | 1.01378 |
| C43 | 0.38808 |  | 0.86296 | 0.9902 |
| C44 | 0.40629 |  | 0.92233 | 0.94795 |
| C45 | 0.36984 |  | 0.74265 | 1.05327 |
| C46 | 0.37107 |  | 0.81632 | 1.03462 |
| C47 | 0.54672 |  | 0.67289 | 0.9991 |
| C48 | 0.42027 |  | 0.54829 | 0.99932 |
| C49 | 0.47921 |  | 0.69971 | 0.99974 |
| C50 | 0.48683 |  | 0.7953 | 1.00031 |
| H51 | 0.19621 |  | 0.39425 | 1.09899 |
| H52 | 0.60636 |  | 0.95494 | 0.8611 |
| H53 | 0.63225 |  | 0.86407 | 0.82934 |
| H54 | 0.3169 |  | 0.37289 | 0.64946 |
| H55 | 0.28932 |  | 0.3913 | 0.6876 |
| H56 | 0.75644 |  | 0.61015 | 0.67436 |
| H57 | 0.71589 |  | 0.90935 | 1.36356 |
| H58 | 0.91679 |  | 0.69943 | 0.60456 |
| H59 | 0.35458 |  | 0.21589 | 0.66142 |
| H60 | 0.67109 |  | 0.87388 | 1.30703 |
| H61 | 0.29504 |  | 0.81954 | 1.275 |
| H62 | 0.23294 |  | 0.68552 | 1.34534 |
| H63 | 0.12453 |  | 0.47715 | 1.22506 |
| H64 | 0.1886 |  | 0.59603 | 1.15469 |
| H65 | 0.32164 |  | 0.95657 | 1.05797 |
| H66 | 0.35263 |  | 0.69099 | 1.08798 |
| H67 | 0.41871 |  | 0.72483 | 1.03523 |
| H68 | 0.443 |  | 0.78962 | 0.95902 |
| H69 | 0.36498 |  | 1.0103 | 0.90228 |
| H70 | 0.4453 |  | 0.08277 | 0.91712 |
| H71 | 0.36607 |  | 0.89383 | 0.93789 |
| H72 | 0.4463 |  | 0.96902 | 0.95247 |
| H73 | 0.35243 |  | 0.9497 | 1.02272 |
| H74 | 0.3708 |  | 0.90495 | 0.9867 |
| H75 | 0.38219 |  | 0.67974 | 1.05219 |
| H76 | 0.40286 |  | 0.59207 | 0.99847 |
| H77 | 0.47463 |  | 0.85893 | 1.00074 |
| N78 | 0 |  | 0.13848 | 0.99982 |
| N79 | 0.24232 |  | 0.7169 | 1.25 |
| N80 | 0.17656 |  | 0.58464 | 1.25 |
| N81 | 0.46267 |  | 0.5 | 1 |
| Ni82 | 0.5 |  | 0.5 | 0.5 |
| Ni83 | 0.29055 |  | 0.1505 | 0.25 |

# Section S13. Reference

[1] a) Y. Qian, D. Li, Y. Han, H. Jiang, H. Han, Photocatalytic Molecular Oxygen Activation by Regulating Excitonic Effects in Covalent Organic Frameworks, J. Am. Chem. Soc, 2020, 142, 20763-20771. b) Y. Gong, W. Zhong, Y. Li, Y. Qiu, L. Zheng, J. Jiang, H. Jiang, Regulating Photocatalysis by Spin-State Manipulation of Cobalt in Covalent Organic Frameworks, J. Am. Chem. Soc, 2020, 142, 16723-16731.

[2] Z. Shan, M. Wu, D. Zhu, X. Wu, K. Zhang, R. Verduzco, G. Zhang, 3D Covalent Organic Frameworks with Interpenetrated pcb Topology Based on 8-Connected Cubic Nodes, J. Am. Chem. Soc, 2022, 144, 5728-5733.

[3] D. Fa, Y. Tao, X. Pan, D. Wang, G. Feng, J. Yuan, Q. Luo, Y. Song, X. J. Gao, L. Yang, S. Lei, W. Hu, Spatial Well-defined Bimetallic Two-Dimensional Polymers with Single-Layer Thickness for Electrocatalytic Oxygen Evolution Reaction, Angew. Chem. Int. Ed, 2022, 61, e202207845.

[4] R. Chen, Y. Wang, Y. Ma, M. Arindam, X. Gao, L. Gao, L. Qiao, X. Li, L. Wu, C. Wang, Rational design of isostructural 2D porphyrin-based covalent organic frameworks for tunable photocatalytic hydrogen evolution, Nat. Commun, 2021, 12, 1354.