Supplementary Materials

A Facile Approach Towards Recycling of Polyurethane coated PET Fabrics

Vaishali Meenakshisundaram a,b, Sathyaraj Gopal a and Kalarical Janardhanan Sreeram*a

a Centre for Analysis, Testing, Evaluation and Reporting Services (CATERS), CSIR – Central Leather Research Institute, Adyar, Chennai 600 020, India.

bAcademy of Scientific and Innovative Research (AcSIR), Ghaziabad 201002, India

Table S1: Water contact angle values recorded on the surface of PET on adding NaOH solution at various concentrations

| Entry | Concentration of NaOH (wt.%) | Contact angle made by NaOH on PET surface | Time taken to remove the PU coating (Minutes) |
| --- | --- | --- | --- |
| 1 | 1 | 133±2˚ | 720 |
| 2 | 4 | 121±3.5˚ | 190 |
| 3 | 5 | 119±2.5˚ | 180 |
| 4 | 10 | 105±2˚ | 60 |

Fig S1: (a) FT-IR spectrum of the PU adhesive (b) PU adhesive scratched from PUCF upon soaking in 5 wt.% NaOH (c) Optical microscopy image of the PU adhesive

The detachment of Polyurethane (PU) coatings from various surfaces, such as metals, has been documented1, 2. However, the separation of PU coatings from fabric surfaces has not been thoroughly studied previously. A series of experiments were conducted to demonstrate the effectiveness of alkaline treatment in separating PU coatings across a broad spectrum of surfaces. Initially, PU adhesive was spread onto a glass slide and allowed to dry at room temperature. Subsequently, a PU film was placed on top of the adhesive and cured in an oven at 60˚ C for more than 24 hours. Following this, the PU-coated glass slide was immersed in a NaOH/SDS mixture (10:20 wt.%) for 10 minutes. Upon removal from the solution, the PU coating readily peeled off from the slide. This observation indicates that the alkaline treatment is indeed efficient in facilitating the separation of PU coatings from various surfaces.

Fig S2: (1) PU film placed on a glass slide for curing in an oven at 60˚ C (2) PU coated glass slide soaked in NaOH/SDS (10:20 wt.%) solution (3) Image showing the peeling of PU coating from the glass slide after soaking

Fig S3: Image showing (on left) three different coloured PET fabrics labelled PET 1, 2, and 3; (on right) the three dye-stripped fabrics labelled PET 1(S), 2(S), and 3(S).

Fig S4: FTIR-ATR spectra of the three PET fabrics (PET 1, 2, and 3) before and after the dye stripping process

Fig S5: SEM – EDX analysis of PET 1 fabric at two different spots (a) Spot 1 on the dye molecule (b) Spot 2 on the clean surface of the PET fabric (c) FTIR spectrum of the extracted dye molecule (scale bar – 1 µm)

Fig S6: Changes in Molecular weights of the PET fabrics before and after the extraction of the dye molecule

References

1.	H. A. Goldsmith, Torrance and L. Salavarrieta, Reseda., Calif pat., 3,410,805, 1964.

2.	E. J. Belack, F. Corcoran.,US pat., 3,954,648, 1976.