(Supporting Information)

RNA-binding peptide and edosomal escape-assisting peptide (L2) improved siRNA delivery by the hexahistidine-metal assembly

Yan Zhanga,c†, Li-Miao Qina,c†, Meng-fan Fenga,c , Xianghui Yub, Yuqing Wua,c*

*Corresponding author: Prof. Yuqing Wu, E-mail: yqwu@jlu.edu.cn.

Fig. S1 The verification of the stability of siBCL-2+L2NTD digested by 2% agarose electrophoresis. Lane 1 is naked siBCL-2 (0.5 nmol/mL) without RNase A; Lines 2-4 for free siBCL-2, Lines 5-7 for siBCL-2+L2NTD in different molar ratios, after co-incubation with RNase A (3 mg mL-1) at 37 °C for 30 min. The results indicated that, after RNase A treatment, different amounts of siBCL-2 in Lanes 2-4 were completely digested; while the complex of siBCL-2+L2NTD with different proportions of L2-NTD in Lanes 5-7 still showed large amounts of siBCL-2. Meanwhile, the remained siBCL-2 increased with the increase of the L2-NTD proportion, indicating the well protective effects of L2-NTD the vulnerable siBCL-2.

Fig. S2. DLS histograms of HmA being assembled at pH 5.0, 7.0, 8.0, 9.0, and 10.0, respectively.

Fig. S3. SEM image and the corresponding EDS mapping for the element of Zn, C, N, O, and P in siGFP+L2-NTD@HmA, respectively.

Fig. S4. SEM image and the corresponding EDS mapping for the element of Zn, C, N, O, and P in siBCL-2+L2-NTD@HmA, respectively.

Fig. S5 Electrophoresis mobility shift assay (EMSA) of siBCL-2+L2-NTD@HmA after dis-assembled in acidic buffer of pH = 4.0, 4.5, 5.5, and 6.5 for 6 h, respectively.