Supporting Information for

Hydroxyl-Modified Chitosan Nanofiber Beads for Sustainable Boron Removal and Environmental Applications

Ho Hong Quyen,*a Hoang M.Nguyen,*a Vu Chi Mai Tran,a Phuoc-Cuong Le,a Masashi Kurashina,b Mikito Yasuzawa,b and Yuki Hiragac

a The University of Da Nang - University of Science and Technology, 54 Nguyen Luong Bang Street, Lien Chieu District, Da Nang City 550000, Vietnam.

b Department of Applied Chemistry, Graduate School of Science and Technology, Tokushima University, 2-1 Minamijosanjima-cho, Tokushima-shi, Tokushima 770-8506, Japan.

c Department of Chemical and Biological Technologies, Shikoku Research Institute, Inc., 2109

Yashima-Nishimachi, Takamatsu-shi, Kagawa 761-0192, Japan.

*Corresponding authors:

Email addresses:

hhquyen@dut.udn.vn (Dr. Ho Hong Quyen).

nmhoang@dut.udn.vn (Dr. Hoang M. Nguyen).

Fig. S1. Illustration of CGCNF beads (a) before and (b) after freeze-drying.

| a b |  |
| --- | --- |

Fig. S2. Experiment of colloidal titration (a) before and (b) after adding indicator of toluidine blue.

Fig. S3. DA%, DD%, and DG% of chitosan nanofibers and GCNF beads.

Calculation details of degree of deacetylation (DD)

DD1% of bare chitosan nanofibers was calculated according to Eq. (S1):

DD1% = d1W1 - 161d1204 + d1100  						(S1)

Where d1 is the mole of deacetylated unit (mol), W1 is the dry mass of bare chitosan nanofibers (g), and 161 and 204 are the molar weight of deacetylated unit and acetylated unit (g/mol), respectively.

DD2% of GC particles and GCNF beads was calculated based on Eq. (S2):

DD2% = d2W2 - 204a-161d1340 +a+d2100    					(S2)

Where d2 is the mole of deacetylated unit (mol), a is the mole of acetylated unit (mol), 340 is the molar weight of gluconated unit (g/mol), and W2 is the dry mass of GC particles or GCNF beads (g).

The degree of gluconated units (DG%) is therefore given as follows:

DG(%) = DD1(%) – DD2(%) 						(S3)

The level of grafted gluconted units (LGG%) is written as follows:

LGG% = DGDD1100       						(S4)

Table S1. The solubility of various adsorbents.

| Sample | Mili-Q water | 0.1M NaOH | 6M NaOH | 0.1M HCl | 6M HCl |
| --- | --- | --- | --- | --- | --- |
| GC particles | + | + | + | - | - |
| GCNF beads | + | + | + | - | - |
| CGC particles | + | + | + | + | + |
| CGCNF beads | + | + | + | + | + |

“+”: insoluble.

“-”: soluble.

Fig. S4. CGCNF beads in 6M HCl solution after (a) 1 min; and (b) 1 month.

Fig. S5. N2 adsorption-desorption isotherm curves of CGCNF beads and CGC particles samples.

Fig. S6. Pore size distribution of CGCNF sample.

Fig. S7. TGA analysis for the prepared chitosan-based samples.

Fig. S8. Effect of initial pH solution on boron removal efficiency by using CGCNF beads and CGC particles (Initial concentration of boron: 400 mg/L, mass of adsorbent: 0.8 g, initial pH solution: 2.03-12.03, solution volume: 20 mL, contact time: 24 h and temperature: 25 ºC).

Table S2. Langmuir, Freundlich, and Temkin isotherm constants and correlation coefficients of various adsorbents for boron adsorption.

| Isotherm | Parameters | CGCNF beads | CGC particles | Amberlite IRA-743 |
| --- | --- | --- | --- | --- |
| Langmuir | qexp (mg/g) | 5.53 | 3.96 | 5.42 |
|  | qmax (mg/g) | 6.05 | 4.13 | 5.73 |
|  | b (L/mg) | 0.094 | 0.090 | 0.151 |
|  | R2 | 0.9976 | 0.9991 | 0.9997 |
|  | RL range | 0.027 - 0.513 | 0.028 - 0.524 | 0.016 - 0.385 |
| Freundlich | KF | 1.793 | 0.886 | 1.827 |
|  | n | 4.454 | 3.441 | 4.522 |
|  | R2 | 0.9441 | 0.8418 | 0.7764 |
| Temkin | B (J/mol) | 0.589 | 0.716 | 0.963 |
|  | AT (L/g) | 44.003 | 1.478 | 2.617 |
|  | R2 | 0.9687 | 0.9866 | 0.9111 |

c

Fig. S9. Experimental data of boron adsorption onto CGCNF beads fitted to linearized forms of (a) Langmuir, (b) Freundlich, and (c) Temkin isotherms (Initial concentration of boron: 10 - 400 mg/L, mass of adsorbent: 0.8 g, initial pH solution: 5.45, solution volume: 20 mL and contact time: 24h).

c

Fig. S10. Experimental data of boron adsorption onto CGC particles fitted to linearized forms of (a) Langmuir, (b) Freundlich, and (c) Temkin isotherms (Initial concentration of boron: 10 - 400 mg/L, mass of adsorbent: 0.8 g, initial pH solution: 5.45, solution volume: 20 mL and contact time: 24 h).

Table S3. Kinetics parameters for adsorption of boron by using various adsorbents.

| Kinetic models | Parameters | CGCNF beads | CGC particles |
| --- | --- | --- | --- |
| Pseudo-first order model | k1 (min-1) | 0.0648 | 0.0037 |
|  | qe (mg/g) | 5.47 | 4.06 |
|  | R2 | 0.9958 | 0.9137 |
| Pseudo-second order | k2 (g mg-1 min-1) | 0.0221 | 0.0007 |
|  | qe (mg/g) | 5.67 | 5.04 |
|  | R2 | 1.000 | 0.9901 |
| Intra-particle diffusion | Kdiff (mg g-1 min-1/2) | 0.0370 | 0.1231 |
|  | C (mg g-1) | 4.5003 | 0.0359 |
|  | R2 | 0.3860 | 0.9137 |

a

Fig. S11. Experimental data of boron adsorption onto CGCNF beads fitted to linearized forms of (a) Pseudo-first order, (b) Pseudo-second order, and (c) Intra-particle diffusion (Initial concentration of boron: 400 mg/L, mass of adsorbent: 0.8 g, initial pH solution: 5.56, solution volume: 20 mL, contact time: 0-24 h and temperature: 25 oC).

Fig. S12. Experimental data of boron adsorption onto CGC particles fitted to linearized forms of (a) Pseudo-first order, (b) Pseudo-second order, and (c) Intra-particle diffusion (Initial concentration of boron: 400 mg/L, mass of adsorbent: 0.8 g, initial pH solution: 5.56, solution volume: 20 mL, contact time: 0-24 h and temperature: 25 oC).

Fig. S13. Effect of ions Na+, K+, Ca2+ and Mg2+ on boron removal efficiency by using (a) CGCNF beads and (b) CGC particles.

Fig. S14. Adsorption performance of Se(VI), As(III), As(V), Cr(III) and Cr(VI) on CGCNF beads and CGC particles.

Fig. S15. Desorption and reusability of CGCNF beads and CGC particles (Initial concentration of boron: 400 mg/L, mass of adsorbent: 0.8 g, initial pH solution: 5.56, solution volume: 20 mL, contact time: 24h and temperature: 25 oC).

Table S4. Comparison of boron desorption efficiency by various adsorbents.

| Adsorbent | Desorption condition | Regeneration condition | Desorption efficiency | Ref. |
| --- | --- | --- | --- | --- |
| Functional magnetic mesoporous silica hybrid nanoparticles | Ci = 100 mg/L, dose = 0.1 g/50 mL, 0.1 M HCl, 12h, room temperature | 3% NH3.H2O then dried at 60oC | 65% after 7 cycles | [51] |
| Magnetic multi-hydroxyl microbeads | Ci = 150 mg/L, m = 0.1 g, 0.1 M HCl, 8h, 25 oC | Water at pH 9 then dried at 80 oC | 44.5% after 6 cycles | [51] |
| Zeolitic imidazolate framework | dose = 0.1 g/80 mL, water, 12h | 80 oC, overnight | 74.4% after 4 cycles | [52] |
| CGC particles | Ci = 400 mg/L, dose = 0.8 g/50 mL, 0.1 M HCl, 24h, 25 oC | 0.1 M NaOH, 12 h, 25oC then freeze drying | 51.8% after 5 cycles | This work |
| CGCNF beads | Ci = 400 mg/L, dose = 0.8 g/50 mL, 0.1 M HCl, 24h, 25 oC | 0.1 M NaOH, 12 h, 25oC then freeze drying | 65.1% after 20 cycles | This work |

Table S5. Characteristics of FGD wastewater (concentrations in mg/L).

| Parameters | FGD wastewater |
| --- | --- |
| pH | 6.6 |
| Na+ | 1261.40 |
| Ca2+ | 3627.85 |
| Mg2+ | 1392.50 |
| B3+ | 133.29 |
| Se6+ | 850.38 |
| As3+ | 0.02 |
| Cr5+ | 0.04 |
| Zn2+ | 1.49 |
| Cu2+ | 0.44 |
| Cd2+ | 0.03 |
| Ni2+ | 0.15 |