Fig. S1. Negative ion ESMS of 1. Solvent: H2O; mobile phase 1/1 CH3CN/H2O

Fig.S2. Negative ion ESMS of 1. Magnification of the peaks at m/z range 534-559 and calculated isotope pattern.

Fig.S3. Negative ion ESMS of 2. Solvent: H2O; mobile phase 1/1 CH3CN/H2O.

Table S1.  Atomic coordinates ( x 104) and equivalent isotropic

displacement parameters (Å2 x 103) for 1.    U(eq) is defined

as one third of the trace of the orthogonalized Uij tensor.

________________________________________________________________

x             y             z      U(eq)* or U

________________________________________________________________

Cu           1485(1)       1002(1)       1184(1)       21(1)*

P(1)         2980(2)        412(1)       -124(1)       21(1)*

P(2)         2886(2)        225(1)       2372(1)       23(1)*

P(3)         2329(2)       2777(1)       1088(1)       20(1)*

N            3350(6)       1211(4)       1195(3)       18(2)*

O(1)         1651(5)        546(4)         74(3)       26(2)*

O(2)         3382(5)       -488(3)        143(3)       29(2)*

O(3)         3308(6)        560(4)       -901(3)       38(2)*

O(4)         1683(5)        197(4)       1968(3)       34(2)*

O(5)         2884(6)        909(4)       2979(3)       36(2)*

O(6)         3284(5)       -611(4)       2668(3)       31(2)*

O(7)         1305(5)       2196(3)        856(3)       26(2)*

O(8)         1842(5)       3326(4)       1735(3)       29(2)*

O(9)         2871(5)       3306(4)        494(3)       28(2)*

OW           -256(5)        786(4)       1185(3)       34(2)*

C(1)         3836(8)       1144(5)        429(4)       19(2)

C(2)         3936(8)        586(5)       1693(5)       22(2)

C(3)         3484(8)       2082(5)       1487(4)       19(2)

C(4)         -535(6)       6347(3)       6070(4)       47(3)

C(5)        -1115(5)       6845(4)       6591(4)       66(4)

C(6)         -676(6)       7648(4)       6746(4)       59(3)

C(7)          343(7)       7953(3)       6380(4)       62(4)

C(8)          924(5)       7455(4)       5859(3)       51(3)

N(1)          485(6)       6652(4)       5704(3)       41(2)

________________________________________________________________

Table S4.   Bond lengths [Å] and angles [deg] for 1.

_____________________________________________________________

Cu-O(4)                       1.928(6)

Cu-OW                         1.943(6)

Cu-O(7)                       1.994(6)

Cu-N                          2.074(7)

Cu-O(1)                       2.156(6)

P(1)-O(3)                     1.481(6)

P(1)-O(1)                     1.519(6)

P(1)-O(2)                     1.570(6)

P(1)-C(1)                     1.802(8)

P(2)-O(6)                     1.497(6)

P(2)-O(4)                     1.513(6)

P(2)-O(5)                     1.551(6)

P(2)-C(2)                     1.786(8)

P(3)-O(9)                     1.493(6)

P(3)-O(7)                     1.515(6)

P(3)-O(8)                     1.560(6)

P(3)-C(3)                     1.831(8)

N-C(3)                        1.487(10)

N-C(2)                        1.490(10)

N-C(1)                        1.500(10)

C(4)-C(5)                     1.39

C(4)-N(1)                     1.39

C(5)-C(6)                     1.39

C(6)-C(7)                     1.39

C(7)-C(8)                     1.39

C(8)-N(1)                     1.39

O(4)-Cu-OW                   89.6(3)

O(4)-Cu-O(7)                149.5(3)

OW-Cu-O(7)                   94.0(3)

O(4)-Cu-N                    89.3(2)

OW-Cu-N                     178.9(3)

O(7)-Cu-N                    87.1(2)

O(4)-Cu-O(1)                117.7(3)

OW-Cu-O(1)                   91.4(2)

O(7)-Cu-O(1)                 92.5(2)

N-Cu-O(1)                    88.8(2)

O(3)-P(1)-O(1)              116.0(4)

O(3)-P(1)-O(2)              111.9(4)

O(1)-P(1)-O(2)              108.9(3)

O(3)-P(1)-C(1)              107.8(4)

O(1)-P(1)-C(1)              106.2(4)

O(2)-P(1)-C(1)              105.3(4)

O(6)-P(2)-O(4)              113.9(4)

O(6)-P(2)-O(5)              111.2(4)

O(4)-P(2)-O(5)              111.6(4)

O(6)-P(2)-C(2)              110.2(4)

O(4)-P(2)-C(2)              103.7(4)

O(5)-P(2)-C(2)              105.8(4)

O(9)-P(3)-O(7)              115.8(3)

O(9)-P(3)-O(8)              111.9(3)

O(7)-P(3)-O(8)              107.2(3)

O(9)-P(3)-C(3)              110.5(4)

O(7)-P(3)-C(3)              105.1(3)

O(8)-P(3)-C(3)              105.8(4)

C(3)-N-C(2)                 110.9(6)

C(3)-N-C(1)                 111.3(6)

C(2)-N-C(1)                 111.4(6)

C(3)-N-Cu                   104.5(5)

C(2)-N-Cu                   109.1(5)

C(1)-N-Cu                   109.3(5)

P(1)-O(1)-Cu                110.6(3)

P(2)-O(4)-Cu                116.1(3)

P(3)-O(7)-Cu                114.8(3)

N-C(1)-P(1)                 112.4(5)

N-C(2)-P(2)                 110.8(6)

N-C(3)-P(3)                 110.3(5)

C(5)-C(4)-N(1)              120.0

C(6)-C(5)-C(4)              120.0

C(5)-C(6)-C(7)              120.0

C(8)-C(7)-C(6)              120.0

C(7)-C(8)-N(1)              120.0

C(8)-N(1)-C(4)              120.0

_____________________________________________________________

Table S2.   Anisotropic displacement parameters (Å2 x 103) for 1.

The anisotropic displacement factor exponent takes the form:

-2 2 [ h2 a*2 U11 + ... + 2 h k a* b* U12 ]

_______________________________________________________________________

U11        U22        U33        U23        U13        U12

_______________________________________________________________________

Cu       19(1)      22(1)      22(1)       3(1)      -1(1)      -1(1)

P(1)     24(1)      23(1)      16(1)      -4(1)      -2(1)       2(1)

P(2)     23(1)      25(1)      20(1)       7(1)      -2(1)      -2(1)

P(3)     23(1)      15(1)      24(1)      -1(1)      -2(1)      -1(1)

N        22(4)      18(4)      12(4)       1(3)       2(3)       4(3)

O(1)     25(4)      27(3)      25(3)      -6(3)      -6(3)       5(3)

O(2)     35(4)      21(3)      32(4)      -3(3)      -6(3)       9(3)

O(3)     44(4)      52(4)      17(3)       0(3)       2(3)      -6(4)

O(4)     23(4)      37(4)      41(4)      20(3)      -7(3)      -8(3)

O(5)     53(5)      25(4)      30(4)      -5(3)       4(3)      -8(3)

O(6)     36(4)      26(3)      31(4)      14(3)      -1(3)       1(3)

O(7)     24(3)      14(3)      39(4)      -2(3)      -9(3)       3(3)

O(8)     28(4)      29(4)      31(4)     -11(3)      10(3)       3(3)

O(9)     33(4)      20(3)      31(4)       8(3)       2(3)      -1(3)

OW       20(3)      44(4)      37(4)      13(4)       2(3)      -4(3)

_______________________________________________________________________

Table S3.   Hydrogen coordinates ( x 104) and isotropic

displacement parameters (Å2 x 103) for 1.

________________________________________________________________

x             y             z           U(eq)

________________________________________________________________

H(11)        4679(8)        962(5)        448(4)       23

H(12)        3815(8)       1696(5)        200(4)       23

H(21)        4633(8)        843(5)       1931(5)       26

H(22)        4226(8)        109(5)       1408(5)       26

H(31)        4289(8)       2295(5)       1371(4)       23

H(32)        3398(8)       2075(5)       2016(4)       23

H(4)         -828(6)       5809(3)       5967(4)       56

H(5)        -1797(7)       6641(6)       6836(5)       79

H(6)        -1064(9)       7982(6)       7095(5)       71

H(7)          637(9)       8491(4)       6483(6)       74

H(8)         1605(7)       7659(6)       5614(5)       62

H(N)          838(7)       6346(5)       5385(4)       51

________________________________________________________________

Table S5.   Bond lengths [Å] and angles [deg]for 2.

_____________________________________________________________

Cu-O(3)                       1.982(8)

Cu-O(1)                       1.979(8)

Cu-N(2)                       1.983(10)

Cu-N(1)                       2.093(10)

Cu-O(2)#1                     2.336(9)

Cu-O(5)                       2.450(9)

P(1)-O(2)                     1.487(8)

P(1)-O(1)                     1.511(8)

P(1)-C(1,1)                   1.795(7)

P(1)-C(1)                     1.858(12)

P(2)-O(4)                     1.516(9)

P(2)-O(3)                     1.515(9)

P(2)-C(1,2)                   1.765(8)

P(2)-C(2)                     1.813(11)

P(3)-O(5)                     1.466(9)

P(3)-O(6)                     1.562(10)

P(3)-C(1,3)                   1.779(8)

P(3)-C(3)                     1.836(12)

N(1)-C(2)                     1.434(14)

N(1)-C(1)                     1.508(14)

N(1)-C(3)                     1.538(14)

N(2)-C(4)                     1.30(2)

N(2)-C(8)                     1.36(2)

C(4)-C(5)                     1.39(2)

C(5)-C(6)                     1.33(2)

C(6)-C(7)                     1.28(2)

C(7)-C(8)                     1.42(2)

C(2,1)-C(3,1)                 1.39

C(2,1)-C(1,1)                 1.39

C(3,1)-C(4,1)                 1.39

C(4,1)-C(5,1)                 1.39

C(5,1)-C(6,1)                 1.39

C(6,1)-C(1,1)                 1.39

C(2,2)-C(3,2)                 1.39

C(2,2)-C(1,2)                 1.39

C(3,2)-C(4,2)                 1.39

C(4,2)-C(5,2)                 1.39

C(5,2)-C(6,2)                 1.39

C(6,2)-C(1,2)                 1.39

C(2,3)-C(3,3)                 1.39

C(2,3)-C(1,3)                 1.39

C(3,3)-C(4,3)                 1.39

C(4,3)-C(5,3)                 1.39

C(5,3)-C(6,3)                 1.39

C(6,3)-C(1,3)                 1.39

O(7)-C(9)                     1.26(4)

C(9)-C(11)                    1.31(5)

C(9)-C(10)                    1.50(5)

O(3)-Cu-O(1)                173.8(4)

O(3)-Cu-N(2)                 92.9(4)

O(1)-Cu-N(2)                 93.2(4)

O(3)-Cu-N(1)                 87.0(4)

O(1)-Cu-N(1)                 86.9(4)

N(2)-Cu-N(1)                178.9(4)

O(3)-Cu-O(2)#1               87.0(3)

O(1)-Cu-O(2)#1               92.0(3)

N(2)-Cu-O(2)#1               93.4(4)

N(1)-Cu-O(2)#1               87.7(3)

O(3)-Cu-O(5)                 87.6(3)

O(1)-Cu-O(5)                 92.6(3)

N(2)-Cu-O(5)                 94.2(4)

N(1)-Cu-O(5)                 84.8(3)

O(2)#1-Cu-O(5)              170.9(3)

O(2)-P(1)-O(1)              118.1(5)

O(2)-P(1)-C(1,1)            107.8(5)

O(1)-P(1)-C(1,1)            107.9(5)

O(2)-P(1)-C(1)              109.4(5)

O(1)-P(1)-C(1)              104.0(5)

C(1,1)-P(1)-C(1)            109.4(5)

O(4)-P(2)-O(3)              116.1(5)

O(4)-P(2)-C(1,2)            109.2(5)

O(3)-P(2)-C(1,2)            110.0(5)

O(4)-P(2)-C(2)              111.1(6)

O(3)-P(2)-C(2)              103.6(5)

C(1,2)-P(2)-C(2)            106.3(5)

O(5)-P(3)-O(6)              119.4(6)

O(5)-P(3)-C(1,3)            111.8(5)

O(6)-P(3)-C(1,3)            103.7(5)

O(5)-P(3)-C(3)              108.0(6)

O(6)-P(3)-C(3)              108.3(6)

C(1,3)-P(3)-C(3)            104.6(5)

P(1)-O(1)-Cu                117.7(5)

P(1)-O(2)-Cu#1              147.3(5)

P(2)-O(3)-Cu                118.1(4)

P(3)-O(5)-Cu                108.0(5)

C(2)-N(1)-C(1)              111.6(9)

C(2)-N(1)-C(3)              111.4(10)

C(1)-N(1)-C(3)              106.4(9)

C(2)-N(1)-Cu                108.9(7)

C(1)-N(1)-Cu                106.2(7)

C(3)-N(1)-Cu                112.2(7)

N(1)-C(1)-P(1)              111.1(8)

N(1)-C(2)-P(2)              111.7(8)

N(1)-C(3)-P(3)              113.4(8)

C(4)-N(2)-C(8)              118.1(12)

C(4)-N(2)-Cu                123.5(10)

C(8)-N(2)-Cu                118.4(10)

N(2)-C(4)-C(5)              122.7(14)

C(6)-C(5)-C(4)              119.4(16)

C(7)-C(6)-C(5)              118.9(17)

C(6)-C(7)-C(8)              122.9(17)

N(2)-C(8)-C(7)              117.5(15)

C(3,1)-C(2,1)-C(1,1)        120.0

C(2,1)-C(3,1)-C(4,1)        120.0

C(5,1)-C(4,1)-C(3,1)        120.0

C(4,1)-C(5,1)-C(6,1)        120.0

C(1,1)-C(6,1)-C(5,1)        120.0

C(6,1)-C(1,1)-C(2,1)        120.0

C(6,1)-C(1,1)-P(1)          120.2(5)

C(2,1)-C(1,1)-P(1)          119.6(5)

C(3,2)-C(2,2)-C(1,2)        120.0

C(4,2)-C(3,2)-C(2,2)        120.0

C(3,2)-C(4,2)-C(5,2)        120.0

C(4,2)-C(5,2)-C(6,2)        120.0

C(1,2)-C(6,2)-C(5,2)        120.0

C(6,2)-C(1,2)-C(2,2)        120.0

C(6,2)-C(1,2)-P(2)          118.7(7)

C(2,2)-C(1,2)-P(2)          121.2(7)

C(3,3)-C(2,3)-C(1,3)        120.0

C(4,3)-C(3,3)-C(2,3)        120.0

C(3,3)-C(4,3)-C(5,3)        120.0

C(4,3)-C(5,3)-C(6,3)        120.0

C(1,3)-C(6,3)-C(5,3)        120.0

C(6,3)-C(1,3)-C(2,3)        120.0

C(6,3)-C(1,3)-P(3)          123.4(6)

C(2,3)-C(1,3)-P(3)          116.7(7)

O(7)-C(9)-C(11)             121(5)

O(7)-C(9)-C(10)             115(4)

C(11)-C(9)-C(10)            110(5)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 -x+1,-y+2,-z+2

Table  S6 . Atomic coordinates ( x 104) and equivalent isotropic

displacement parameters (Å2 x 103) for 2.    U(eq) is defined

as one third of the trace of the orthogonalized Uij tensor.

________________________________________________________________

x             y             z        U(eq)* or U

________________________________________________________________

Cu           7090(2)       8532(2)       9268(1)       37(1)*

P(1)         6048(4)      11000(3)       9570(3)       37(1)*

P(2)         6158(4)       8549(4)       7292(3)       43(1)*

P(3)         8735(4)       9568(4)       7359(4)       53(1)*

O(1)         7123(8)       9586(7)       9984(7)       44(3)*

O(2)         5012(8)      11302(8)      10266(7)       48(3)*

O(3)         6933(8)       7664(7)       8417(7)       43(3)*

O(4)         6968(10)      8566(9)       6370(7)       60(3)*

O(5)         9126(8)       8536(8)       8483(8)       55(3)*

O(6)         8694(9)       9176(10)      6447(8)       70(3)*

N(1)         6112(10)     10353(9)       7891(8)       32(3)

C(1)         5240(12)     11343(12)      8286(10)      39(4)

C(2)         5339(12)     10191(11)      7234(10)      37(4)

C(3)         7089(12)     10888(12)      7255(11)      48(4)

N(2)         8047(10)      6804(10)     10561(8)       41(3)

C(4)         8312(14)      6705(14)     11496(12)      58(4)

C(5)         8987(14)      5483(15)     12397(13)      73(5)

C(6)         9459(15)      4365(16)     12295(13)      72(5)

C(7)         9245(15)      4440(16)     11376(13)      77(5)

C(8)         8469(15)      5661(15)     10465(13)      74(5)

C(1,1)       6848(8)      12074(8)       9290(7)       31(3)

C(2,1)       8232(8)      11545(7)       9394(7)       54(4)

C(3,1)       8863(7)      12349(10)      9259(8)       79(5)

C(4,1)       8110(10)     13680(10)      9020(8)       83(5)

C(5,1)       6726(10)     14209(7)       8916(8)       97(6)

C(6,1)       6095(7)      13406(9)       9051(8)       84(5)

C(1,2)       4876(8)       8121(9)       7172(9)       49(4)

C(2,2)       4230(10)      7661(10)      8045(7)       71(5)

C(3,2)       3198(10)      7368(10)      7919(8)       84(5)

C(4,2)       2811(9)       7534(11)      6920(11)     102(6)

C(5,2)       3457(12)      7994(12)      6048(8)      126(7)

C(6,2)       4489(11)      8288(10)      6174(7)       99(6)

C(1,3)       9804(8)      10379(9)       6960(8)       52(4)

C(2,3)      10485(10)     10340(9)       7777(6)       77(5)

C(3,3)      11339(9)      10950(10)      7529(8)       84(5)

C(4,3)      11512(9)      11601(9)       6462(9)       82(5)

C(5,3)      10831(10)     11640(9)       5645(6)       79(5)

C(6,3)       9977(9)      11029(10)      5894(7)       73(5)

O(7)         3643(20)      3680(20)      5535(17)     193(8)

C(9)         2876(45)      4708(45)      4731(37)     241(18)

C(10)        2110(35)      4469(33)      4069(29)     238(15)

C(11)        3248(47)      5636(50)      4104(40)     343(26)

________________________________________________________________

Table S7.   Anisotropic displacement parameters (Å2 x 103) for 2.

The anisotropic displacement factor exponent takes the form:

-2 2 [ h2 a*2 U11 + ... + 2 h k a* b* U12 ]

_______________________________________________________________________

U11        U22        U33        U23        U13        U12

_______________________________________________________________________

Cu       44(1)      26(1)      36(1)     -14(1)       1(1)     -11(1)

P(1)     37(2)      32(2)      40(3)     -16(2)       5(2)     -13(2)

P(2)     52(3)      39(2)      43(3)     -22(2)       2(2)     -20(2)

P(3)     44(3)      46(3)      64(3)     -28(3)       8(2)     -13(2)

O(1)     49(6)      27(5)      45(6)     -11(5)      -3(5)     -11(5)

O(2)     53(6)      58(6)      54(6)     -35(5)      26(5)     -34(5)

O(3)     50(6)      26(5)      46(7)     -17(5)      -1(5)      -9(5)

O(4)     89(8)      94(8)      40(6)     -51(6)      32(6)     -58(6)

O(5)     48(6)      40(6)      55(7)     -11(6)      -4(5)      -9(5)

O(6)     70(7)      82(8)      75(8)     -54(7)      21(6)     -30(6)

_______________________________________________________________________

Table S8.   Hydrogen coordinates ( x 104) and isotropic

displacement parameters (Å2 x 103) for 2.

________________________________________________________________

x             y             z           U(eq)

________________________________________________________________

H(11)        4391(12)     11295(12)      8395(10)      47

H(12)        5066(12)     12238(12)      7745(10)      47

H(21)        5196(12)     10863(11)      6493(10)      45

H(22)        4473(12)     10325(11)      7476(10)      45

H(31)        7200(12)     11449(12)      7519(11)      57

H(32)        6706(12)     11441(12)      6502(11)      57

H(4)         8040(14)      7483(14)     11565(12)      70

H(5)         9106(14)      5449(15)     13063(13)      88

H(6)         9938(15)      3543(16)     12883(13)      87

H(7)         9613(15)      3660(16)     11302(13)      93

H(8)         8256(15)      5678(15)      9825(13)      89

H(2,1)       8736(8)      10654(7)       9554(7)       65

H(3,1)       9789(7)      11995(14)      9328(12)      95

H(4,1)       8532(14)     14218(13)      8929(12)      99

H(5,1)       6222(14)     15100(8)       8756(12)     117

H(6,1)       5169(7)      13760(13)      8981(12)     101

H(2,2)       4489(10)      7550(10)      8713(7)       86

H(3,2)       2766(14)      7060(14)      8502(11)     101

H(4,2)       2120(12)      7338(15)      6836(15)     122

H(5,2)       3198(17)      8106(17)      5380(9)      152

H(6,2)       4921(15)      8595(14)      5590(9)      119

H(2,3)      10369(10)      9905(9)       8491(6)       92

H(3,3)      11794(13)     10924(15)      8076(10)     100

H(4,3)      12083(12)     12009(13)      6296(13)      98

H(5,3)      10946(14)     12075(13)      4931(7)       95

H(6,3)       9521(13)     11055(14)      5347(9)       88

________________________________________________________________