Electronic Supplementary Information

Preparations of M4As2W18

K8Na2As2W18Cu4(H2O)2O68·32H2O, Cu4As2W18. Solid CuCl2·2H2O (0.26 g, 1.5 mmol) was dissolved in 15 mL of water. To this solution was added with stirring 2.0 g ( 0.75 mmol ) of solid Na8HAsW9O34 (1atm, 140 oC,1-2 h). The solution was stirred at room temperature until all the B-AsW9 was dissolved. Excess solid KCl (4.5 g) was added to the light green solution, resulting in the precipitation of a pale green solid. This solid was collected on a sintered-glass frit and dried under aspiration. The slightly damp solid was redissolved in about 5-10 mL of hot water and allowed to recrystallize overnight at 5 oC. A crystalline pale-green solid was collected and dried at 80 oC under vacuum for 2 h. The yield was 1.54 g (77%) of a pale-green solid. Slow crystallization at room temperature will result in large well-formed pale-green to clear crystals.  Anal. Calcd for K4NaAsW9Cu2(H2O)O34 ·10H2O: K, 5.62; Na, 0.83; As, 2.70; W, 59.57; Cu, 4.57; H2O, 7.13. Found: K, 5.75; Na, 0.71; As, 2.63; W, 59.45; Cu, 4.69; H2O, 7.18.

K8.2Na1.8As2W18Zn4(H2O)2O68 ·20H2O, Zn4As2W18.  Solid ZnCl2 (0.21 g, 1.5 mmol) was dissolved in 15 mL of water. To this solution was added with stirring 2.0 g ( 0.75 mmol ) of solid Na8HAsW9O34 (1atm, 140 oC,1-2 h). The solution was heated until nearly homogeneous and then filtered hot by gravity filtration through paper. Excess solid KCl (4.5 g) was added to the clear filtrate, resulting in the immediate precipitation of a white solid. After the mixture was cooled to room temperature, this solid was collected on a sintered-glass frit and dried under aspiration. The slightly damp solid was redissolved in about 5-10 mL of hot water and allowed to recrystallize overnight at 5 oC. A crystalline white solid was collected and dried at 80 oC under vacuum for 2 h. The yield was 1.60 g (80%) of a white solid. Anal. Calcd for K4.1Na0.9AsW9Zn2(H2O)O34 ·10H2O: K, 5.75; Na, 0.74; As, 2.69; W, 59.46; Zn, 4.70; H2O, 7.11. Found: K, 5.69; Na, 0.75; As, 2.71; W, 59.51; Zn, 4.68; H2O, 7.22 .

K8Na2As2W18Cd4(H2O)2O68 ·20H2O, Cd4As2W18. Solid CdCl2·2.5 H2O (0.35 g, 1.5 mmol) was dissolved in 15 mL of water. To this solution was added with stirring 2.0 g ( 0.75 mmol ) of solid Na8HAsW9O34 (1atm, 140 oC,1-2 h). The solution was heated until nearly homogeneous and then filtered hot by gravity filtration through paper. Excess solid KCl (4.5 g) was added to the clear filtrate, resulting in the immediate precipitation of a white solid. After the mixture was cooled to room temperature, this solid was collected on a sintered-glass frit and dried under aspiration. The slightly damp solid was redissolved in about 5-10 mL of hot water and allowed to recrystallize overnight at 5 oC. A crystalline white solid was collected and dried at 80℃ under vacuum for 2 h. The yield was 1.58 g (79%) of a white solid. Anal. Calcd for K4NaAsW9Cd2(H2O)O34 ·10H2O: K, 5.42; Na, 0.80; As, 2.61; W, 57.54; Cd, 7.82; H2O, 6.89 . Found: K, 5.52 ; Na, 0.75; As, 2.56 ; W, 57.42; Cd, 7.79; H2O, 6.93 .

K8Na2As2W18Co4(H2O)2O68·18H2O, Co4As2W18.  Solid Co(NO3 )2· 6H2O (0.45g, 1.5 mmol) was dissolved in 15 mL of water. To this light pink solution was added with stirring 2.0 g ( 0.75 mmol ) of solid Na8HAsW9O34 (1atm, 140 oC,1-2 h). The solution was heated until a homogeneous purple to burgundy solution resulted. Excess solid KCl (5.0 g) was added , and a blue-purple precipitate formed. After the mixture was cooled to room temperature, this solid was collected on a sintered-glass frit and dried under aspiration. The slightly damp solid was redissolved in about 5-10 mL of hot water and allowed to recrystallize overnight at 5 oC.A crystalline blue-purple solid was collected and dried at 80 oC under vacuum for 2 h. The yield was 1.74 g (87%) of a blue-purple solid. Slow crystallization at room temperature will result in large well-formed blue-purple to clear crystals. Anal. Calcd for K4NaAsW9Co2(H2O)O34 ·9H2O: K, 5.67; Na, 0.84; As, 2.73; W, 60.16; Co, 4.28; H2O, 6.54 . Found: K, 5.65; Na, 0.82; As, 2.66; W, 60.25; Co, 4.33; H2O, 6.62 .

K10As2W18Ni4(H2O)2O68·20H2O, Ni4As2W18. Solid NiCl2·6H2O (0.37 g, 1.5 mmol) was dissolved in 15 mL of water. To this solution was added with stirring 2.0 g ( 0.75 mmol ) of solid Na8HAsW9O34 (1atm, 140 oC,1-2 h). The solution was stirred at room temperature until all the B-AsW9 was dissolved. Excess solid KCl (4.5 g) was added to the yellow-green solution, resulting in the immediate precipitation of a yellow solid. This solid was collected on a sintered-glass frit and dried under aspiration. The slightly damp solid was redissolved in about 5-10 mL of hot water and allowed to recrystallize overnight at 5 oC. A crystalline yellow solid was collected and dried at 80 oC under vacuum for 2 h. The yield was 1.50 g (75%) of a yellow solid. Anal. Calcd for K5AsW9Ni2(H2O)O34 ·10H2O: K, 7.00; As, 2.69; W, 59.43; Ni, 4.22; H2O, 7.11. Found: K, 6.92; As, 2.95; W, 59.55; Ni, 4.18; H2O,7.28 .

K10As2W18Mn4(H2O)2O68·18H2O, Mn4As2W18. Solid MnCl2·4H2O (0.30 g, 1.5 mmol) was dissolved in 15 mL of water. To this solution was added with stirring 2.0 g ( 0.75 mmol ) of solid Na8HAsW9O34 (1atm, 140 oC,1-2 h). The solution was heated until nearly homogeneous and then filtered hot by gravity filtration through paper. Excess solid KCl (4.5 g) was added to the clear filtrate, resulting in the immediate precipitation of a orange solid. After the mixture was cooled to room temperature, this solid was collected on a sintered-glass frit and dried under aspiration. The slightly damp solid was redissolved in about 5-10 mL of hot water and allowed to recrystallize overnight at 5 oC. A crystalline orange solid was collected and dried at 80 oC under vacuum for 2 h. The yield was 1.58 g (79%) of a orange solid. Slow crystallization at room temperature will result in large well-formed orange to clear crystals. Anal. Calcd for K5AsW9Mn2(H2O)O34·9H2O: K, 7.07; As, 2.72; W, 59.98; Mn, 3.98; H2O, 6.52 . Found: K, 6.98; As,2.70; W, 60.15; Mn, 3.89; H2O, 6.66 .

K7Na3As2W18Fe4(H2O)2O68·18H2O, Fe4As2W18. Solid FeSO4·7H2O (0.42 g, 1.5 mmol) was dissolved in 15 mL of water. To this solution was added with stirring 2.0 g ( 0.75 mmol ) of solid Na8HAsW9O34 (1atm, 140 oC,1-2 h). The solution was heated until nearly homogeneous and then filtered hot by gravity filtration through paper. Excess solid KCl (4.5 g) was added to the clear filtrate, resulting in the immediate precipitation of a brown solid. After the mixture was cooled to room temperature, this solid was collected on a sintered-glass frit and dried under aspiration. The slightly damp solid was redissolved in about 5-10 mL of hot water and allowed to recrystallize overnight at 5 oC. A crystalline brown solid was collected and dried at 80 oC under vacuum for 2 h. The yield was 1.74 g (87%) of a brown solid. Anal. Calcd for K3.5Na1.5AsW9Fe2(H2O)O34·9 H2O: K, 5.00; Na, 1.26; As, 2.74; W, 60.47; Fe, 4.08; H2O, 6.58. Found: K, 5.11; Na, 1.23; As, 2.69; W, 60.42; Fe, 3.98; H2O, 6.62.

K10 [Zn4(H2O)2(AsW9O34)2 ]·23H2O Prepared after the Method Suggested by Weakley. A boiling solution containing ZnSO4 ∙7H2O (5.75 g, 0.021 mol) and 6.4 mol ·dm-3 HNO3 (17.2 cm3 , 0.110 mol) in water (110 cm3 ) was treated slowly with a solution of Na2WO4 ·2H2O (29.7 g, 0.090 mol) and Na2HAsO4 ·7H2O (3.15 g, 0.011 mol ) in water (110 cm3 ). The mixture was refluxed for 3 h and filtered while hot. The crude crystalline product was precipitated by the addition of KNO3 (40 g) and cooling; it was twice redissolved and reprecipitated with KNO3 , and was finally recrystallised twice from hot water (Found: As, 2.60; H2O, 8.05; K, 7.10; W, 58.5; Zn, 4.70. Calc. for H50As2K10O93W18Zn4 : As, 2.65; H2O, 7.95; K, 6.90; W, 58.6; Zn, 4.65% ).

Replacement Reaction of the Water Molecules Coordinated to the M4As2W18 Anion in Aqueous Solutions.

K16[Mn4(L1)2(AsW9O34)2], Mn4As2W18-L1. The preparation procedure was the same as that for Cu4As2W18-L1 described above except that Mn4As2W18 was used and the product was a yellow powder (0.40 g). Elemental analyses gave a ratio K:Mn:Fe:W = 16.0:3.8:2.1:17.8, consistent with the formula. IR (KBr, cm-1): 2109 (v (CN)), 954, 880, 840, 728.

K16[Co4(L1)2(AsW9O34)2], Co4As2W18-L1. The preparation procedure was the same as that for Cu4As2W18-L1 described above except that Co4As2W18 was used and the product was a brown black powder (0.33 g). Elemental analyses gave a ratio K:Co:Fe:W = 16.0:4.1:1.7:18.4, consistent with the formula. IR (KBr, cm-1): 2116 (v (CN)), 966, 881, 819, 763, 712.

K16[Ni4(L1)2(AsW9O34)2], Ni4As2W18-L1. The preparation procedure was the same as that for Cu4As2W18-L1 described above except that Ni4As2W18 was used and the product was a yellow-green powder (0.43 g). Elemental analyses gave a ratio K:Ni:Fe:W = 16.0:4.1:1.8:18.3, consistent with the formula. IR (KBr, cm-1): 2112 (v (CN)), 954, 881, 763, 701.

K16[Fe4(L1)2(AsW9O34)2], Fe4As2W18-L1. The preparation procedure was the same as that for Cu4As2W18-L1 described above except that Fe4As2W18 was used and the product was a dark-green powder (0.43 g). Elemental analyses gave a ratio K:Fe:As:W = 16.0:3.8:2.0:17.7, consistent with the formula. IR (KBr, cm-1): 2114 (v (CN)), 958, 880, 819, 733.

K18[Mn4(L2)2(AsW9O34)2], Mn4As2W18-L2. The preparation procedure was the same as that for Cu4As2W18-L2 described above except that Mn4As2W18 was used and the product was a pale-yellow powder (0.38 g). Elemental analyses gave a ratio K:Mn:Fe:W = 18.0:4.1:1.7:18.2, consistent with the formula.IR (KBr, cm-1): 2094 (v (CN)), 953, 881, 840, 765, 729.

K18[Co4(L2)2(AsW9O34)2], Co4As2W18-L2. The preparation procedure was the same as that for Cu4As2W18-L2 described above except that Co4As2W18 was used and the product was a gray-green powder (0.34 g). Elemental analyses gave a ratio K:Co:Fe:W = 18.0:4.0:1.8:18.3, consistent with the formula. IR (KBr, cm-1): 2092 (v (CN)), 954, 881, 819, 759, 712.

K18[Ni4(L2)2(AsW9O34)2], Ni4As2W18-L2. The preparation procedure was the same as that for Cu4As2W18-L2 described above except that Ni4As2W18 was used and the product was a green powder (0.35 g). Elemental analyses gave a ratio K:Ni:Fe:W = 18.0:4.1:1.9:18.0, consistent with the formula. IR (KBr, cm-1): 2091 (v (CN)), 955, 881 , 763, 701.

K18[Fe4(L2)2(AsW9O34)2], Fe4As2W18-L2. The preparation procedure was the same as that for Cu4As2W18-L2 described above except that Fe4As2W18  was used and the product was a yellow-green powder (0.58 g). Elemental analyses gave a ratio K:Fe:As:W = 18.0:5.8:1.9:18.1, consistent with the formula. IR (KBr, cm-1): 2092 (v (CN)), 957, 883, 822, 730.

K10[Mn4(L3)2(AsW9O34)2], Mn4As2W18-L3. The preparation procedure was the same as that of Cu4As2W18-L3 described above except that Mn4As2W18 was used and the product was a white powder (0.32g). Elemental analyses gave a ratio K:Mn:C:N:W = 10.0:4.0:3.6:3.8:18.2, consistent with the formula. IR (KBr, cm-1): 1042 (v(C-N)), 1643 (δ(NH2)), 948, 882 , 819, 735.

K10[Co4(L3)2(AsW9O34)2], Co4As2W18-L3. The preparation procedure was the same as that of Cu4As2W18-L3 described above except that Co4As2W18 was used and the product was a pale-pink powder (0.42 g). Elemental analyses gave a ratio K:Co:C:N:W = 10.0:3.9:3.7:4.0:18.2, consistent with the formula. IR (KBr, cm-1): 1057 (v(C-N)), 1651 (δ(NH2)), 928, 880, 780, 728.

K10[Ni4(L3)2(AsW9O34)2], Ni4As2W18-L3. The preparation procedure was the same as that of Cu4As2W18-L3 described above except that Ni4As2W18 was used and the product was a flesh-colored powder (0.38 g). Elemental analyses gave a ratio K:Ni:C:N:W = 10.0:4.2:3.9:3.7:17.9, consistent with the formula. IR (KBr, cm-1): 1042 (v(C-N)), 1643 (δ(NH2)), 938, 872, 822, 725.

K10[Fe4(L3)2(AsW9O34)2], Fe4As2W18-L3. The preparation procedure was the same as that of Cu4As2W18-L3 described above except that Fe4As2W18 was used and the product was a brown-red powder (0.39 g). Elemental analyses gave a ratio K:Fe:C:N:W = 10.0:4.1:3.7:3.8:18.4, consistent with the formula. IR (KBr, cm-1): 1042 (v(C-N)), 1636 (δ(NH2)), 958, 881, 819, 745.

K14[Mn4(L4)2(AsW9O34)2], Mn4As2W18-L4.The preparation procedure was the same as that of Cu4As2W18-L4 described above except that Mn4As2W18 was used and the product was a white powder (0.35 g). Elemental analyses gave a ratio K:Mn:S:W = 14.0:4.1:1.8:17.8, consistent with the formula. IR (KBr, cm-1): 1123 (v(SO32-)), 945, 881, 819, 729.

K14[Co4(L4)2(AsW9O34)2], Co4As2W18-L4. The preparation procedure was the same as that of Cu4As2W18-L4 described above except that Co4As2W18 was used and the product was a pink powder (0.39 g). Elemental analyses gave a ratio K:Co:S:W = 14.0:4.1:2.1:18.3, consistent with the formula. IR (KBr, cm-1): 1126 (v(SO32-)), 943, 884, 820, 735.

K14[Ni4(L4)2(AsW9O34)2], Ni4As2W18-L4. The preparation procedure was the same as that of Cu4As2W18-L4 described above except that Ni4As2W18 was used and the product was a white powder (0.36 g). Elemental analyses gave a ratio K:Ni:S:W = 14.0:4.1:1.8:18.2, consistent with the formula. IR (KBr, cm-1): 1125 (v(SO32-)), 953, 881, 818, 735.

K14[Fe4(L4)2(AsW9O34)2], Fe4As2W18-L4. The preparation procedure was the same as that of Cu4As2W18-L4 described above except that Fe4As2W18 was used and the product was a brown-yellow powder (0.36 g). Elemental analyses gave a ratio K:Fe:S:W = 14.0:3.8:2.0:18.3, consistent with the formula. IR (KBr, cm-1): 1125 (v(SO32-)), 945, 880, 818, 758.

K12[Mn4(L5)2(AsW9O34)2], Mn4As2W18-L5. The preparation procedure was the same as that of Cu4As2W18-L5 described above except that Mn4As2W18 was used and the product was a yellow powder (0.42 g). Elemental analyses gave a ratio K:Mn:S:W = 12.0:4.2:2.3:18.1, consistent with the formula. IR (KBr, cm-1): 2071 (v(SCN-)), 955, 879, 820, 729.

K12[Co4(L5)2(AsW9O34)2], Co4As2W18-L5. The preparation procedure was the same as that of Cu4As2W18-L5 described above except that Co4As2W18 was used and the product was a purple powder (0.38 g). Elemental analyses gave a ratio K:Co:S:W = 12.0:4.0:1.8:18.2, consistent with the formula. IR (KBr, cm-1): 2069 (v(SCN-)), 959, 878, 818, 762.

K12[Ni4(L5)2(AsW9O34)2], Ni4As2W18-L5. The preparation procedure was the same as that of Cu4As2W18-L5 described above except that Ni4As2W18  was used and the product was a white powder (0.41 g). Elemental analyses gave a ratio K:Ni:S:W = 12.0:4.1:1.8:17.9, consistent with the formula. IR (KBr, cm-1): 2071 (v(SCN-)), 952, 890, 819, 748.

K12[Fe4(L5)2(AsW9O34)2], Fe4As2W18-L5. The preparation procedure was the same as that of Cu4As2W18-L5 described above except that Fe4As2W18  was used and the product was a yellow powder (0.35 g). Elemental analyses gave a ratio K:Fe:S:W = 12.0:4.2:1.7:18.5, consistent with the formula. IR (KBr, cm-1): 2070 (v(SCN-)), 960, 881, 829, 718.

- Tables and Figures.

- Table 1.  CV Data for M4As2W18 Compounds (V)a

| heteropoly- anions | Epa | Epc | ΔEp (mV) | heteropoly- anions | Epa | Epc | ΔEp (mV) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| α-AsW12O404- | 0.0078 | -0.0332 | 41 | Co4As2W18 | -0.6522 | -0.7762 | 124 |
|  | -0.1402 | -0.4276 | 286 |  | -0.8344 | -0.9074 | 73 |
|  | -0.3203 | -0.4443 | 124 | Zn4As2W18 | -0.6450 | -0.7797 | 135 |
|  | -0.5137 | -0.6595 | 146 |  | -0.7762 | -0.9147 | 139 |
|  | -0.6886 | -0.7943 | 106 | Cd4As2W18 | -0.6412 | -0.7822 | 141 |
| B-AsW9O349- | -0.5464 | -0.7835 | 237 |  | -0.7945 | -0.9475 | 153 |
| Cu4As2W18 | 0.1138 | -0.1643 | 278 | Fe4As2W18 | 0.1561 | -0.1677 | 324 |
|  | -0.2832 | -0.4269 | 144 |  | -0.5740 | -0.6947 | 121 |
|  | -0.6768 | -0.7742 | 97 |  | -0.7770 | -0.9045 | 127 |
| Mn4As2W18 | -0.6776 | -0.7723 | 95 |  |  |  |  |
|  | -0.7872 | -0.9001 | 113 |  |  |  |  |

a Epa, oxidation potential; Epc, reduction potential; ΔEp, the difference between the pair of redox potentials. Condition: pH 4.0 of a buffer solution of HAc-NaAc; 25℃; glassy carbon working electrode; scan rate 50mV·s-1; potentials recorded vs Ag/AgCl.

- Table 2. Colors and States of the Products Isolated from the Replacement Reactions in Aqueous Solutions a

| heteropoly- anions | ligands |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | [Fe(CN)6]3- | [Fe(CN)6]4- | C2H8N2 | SO32- | SCN- |
| Cu4As2W18 | yellow↓ (brown-yellow) | dark-red↓ (red-green↓) | violet↓ (blue) | white↓ (yellow↓) | pale-pink↓ (dark↓) |
| Mn4As2W18 | yellow↓ (brown) | pale-yellow↓ (white↓) | white↓ (yellowish↓) | white↓ (no reacn) | yellow↓ (no reacn) |
| Co4As2W18 | brown-black↓ (dark-red) | gray-green↓ (green↓) | pale-pink↓ (brown) | pink↓ (no reacn) | purple↓ (blue) |
| Ni4As2W18 | yellow-green↓ (yellow↓) | green↓ (greenish↓) | flesh↓ (blue) | white↓ (blue↓) | white↓ (no reacn) |
| Fe4As2W18 | dark-green↓ (dark-blue) | yellow-green↓ (blue) | Brown-red↓ (brown-black) | brown-yellow (khaki) | yellow↓ (orange) |

a The colors and states of the products isolated from aqueous solutions, in which only corresponding simple transition

metal ions and ligands present, are shown in the parentheses

Table 3 . Colors of M4As2W18 in Aqueous Solutions and in Benzene Containing 0.1M (tHA)Br.

|  | Cu4As2W18 | Mn4As2W18 | Co4As2W18 | Ni4As2W18 | Fe4As2W18 |
| --- | --- | --- | --- | --- | --- |
| H2O | green | orange | blue-purple | yellow | brown |
| before the loss of the coordinated water molecules | yellow-green | yellow | blue-purple | yellow | orange |
| after the loss of the coordinated water molecules | yellow | yellow | dark-blue | yellow | yellow |
| pyridine | yellow-green | yellow | purple | yellow | orange |
| acetone | yellow-green | yellow | purple | yellow | orange |
| lactic acid | yellow-green | yellow | purple-red | yellow | orange |
| acetonitrile | yellow-green | yellow | blue-purple | yellow | orange |
| chloroform | yellow-green | yellow | blue-purple | yellow | orange |
| pyrrole | orange | orange | purple-black | orange | orange-red |

Figure 1. General view of I.

Figure 2. Structure of the central tetrameric unit Cu4(H2O)2O14 in II.

Figure 3. General view of II.

Figure 4. Electronic spectra of Co4As2W18 in a aqueous solution (-·-·), in benzene / 0.1M   (tHA)Br (a) Co4As2W18-H2O. (b) Co4As2W18. (c) Co4As2W18-chloroform. (d) Co4As2W18-pyridine. (e) Co4As2W18-pyrrole. (f) Co4As2W18-acetone. (g)Co4As2W18-acetonitrile. (h) Co4As2W18-lactic acid.

Figure 5. Crystallographic morphologies of Co4As2W18 occupied by organic ligands isolated from benzene solutions: Co4As2W18 - chloroform (a), Co4As2W18 - acetonitrile (b), Co4As2W18 - pyridine (c), Co4As2W18 -acetone (d), Co4As2W18 - pyrrole (e), Co4As2W18 - lactic acid (f).