Synthesis and structural characterization of luminescent di- and trinuclear palladium(II) acetylide complexes as building blocks for metallodendrimers

# Vivian Wing-Wah Yam*, Lingjun Zhang, Chi-Hang Tao, Keith Man-Chung Wong, and Kung-Kai Cheung

# Department of Chemistry, The University of Hong Kong, Pokfulam Road, Hong Kong, P. R. China

### Supplementary Information

Crystal Structure Determination.  Crystals of 1 were obtained by recrystallisation from benzene-n-pentane.  Crystal Data.:  [C48H93P6Cl3Pd3], M = 1281.66, monoclinic, space group C2/c (No. 15), a = 11.233(7) Å, b = 31.389(6) Å, c = 19.214(4) Å,  = 103.60(3)o, V = 6584(4) Å3, Z = 4, Dc = 1.293 g cm3, (Mo-K) = 11.05 cm1, F(000) = 2640, T = 301 K.  A colourless crystal of dimensions 0.35  0.15  0.10 mm mounted on a glass fibre was used for data collection at 28oC on a Rigaku AFC7R diffractometer with graphite monochromatized Mo-K radiation ( = 0.71073 Å) using 2 scans with -scan angle (0.73 + 0.35 tan )o at a scan speed of 16.0 deg min1 (up to 6 scans for reflection with I < 15(I)).  Unit-cell dimensions were determined based on the setting angles of 25 reflections in the 2 range of 20.2 to 25.1°.  Intensity data (in the range of 2 max = 50°; h: 0 to 12; k: 0 to 37; l: 22 to 22 and 3 standard reflections measured after every 300 reflections showed decay of 4.49%) were corrected for decay and Lorentz and polarisation effects, and empirical absorption corrections based on the -scan of five strong reflections (minimum and maximum transmission factors 0.576 and 1.000).  5574 reflections were measured, of which 5249 were unique and Rint = 0.036.  2201 reflections with I > 3(I) were considered observed and used in the structural analysis.  The space group was determined based on a statistical analysis of intensity distribution and the successful refinement of the structure solved by direct methods (SIR92) and expanded by Fourier method and refined by full-matrix least-squares using the software package TeXsan on a Silicon Graphics Indy computer.  One crystallographic asymmetric unit consists of half of one formula unit with Pd(1), Cl(1), C(1), C(2), C(3) and C(6) at special positions.  In the least-squares refinement, the Pd, Cl and P atoms were refined anisotropically, all 26 C atoms were refined isotropically and 47 H atoms at calculated positions with thermal parameters equal to 1.3 times that of the attached C atoms were not refined.  Convergence for 152 variable parameters by least-squares refinement on F with w = 4Fo2/2(Fo2), where 2(Fo2) = [2(I) + (0.040 Fo2)2] for 2201 reflections with I > 3(I) was reached at R = 0.060 and wR = 0.088 with a goodness-of-fit of 2.50.  (/)max = 0.05 except for the H atoms.  The final difference Fourier map was featureless, with maximum positive and negative peaks of 0.84 and 0.53 eÅ3 respectively.

Crystals of 2 were obtained by recrystallisation from benzene-n-pentane.  Crystal Data.: [C45H84SiP4Cl2Pd2], M = 1060.85, monoclinic, space group P21/n (No. 14), a = 12.786(2) Å, b = 15.416(3) Å, c = 29.024(3) Å,  = 94.63(2)o, V = 5702(1) Å3, Z = 4, Dc = 1.236 g cm3, (Mo-K) = 8.84 cm1, F(000) = 2216, T = 301 K.  A colourless crystal of dimensions 0.4  0.1  0.1 mm mounted on a glass fibre was used for data collection at 28oC on a MAR diffractometer with a 300 mm image plate detector using graphite monochromatized Mo-K radiation ( = 0.71073 Å).  Data collections were made with 2o oscillation (96 images) at 120 mm distance and 600 s exposure.  The images were interpreted and intensities integrated using program DENZO.  7882 unique reflections were obtained from a total of 45846 measured reflections (Rint = 0.062).  3158 reflections with I > 3(I) were considered observed and used in the structural analysis.  These reflections were in the range of h: 0 to 15; k: 0 to 17; l: 34 to 33 with 2max = 50.8o.  The space group was determined based on systematic absences and the structure was solved by Patterson methods and expanded by Fourier methods (PATTY) and refinement by full-matrix least-squares using the software package TeXsanError: Reference source not found on a Silicon Graphics Indy computer.  A crystallographic asymmetric unit consists of one molecule.  In the least-squares refinement, 9 non-H atoms were refined anisotropically, all 45 C atoms were refined isotropically, and 84 H atoms at calculated position with thermal parameters equal to 1.3 times that of the attached C atoms were not refined.  Convergence for 262 variable parameters by least-squares refinement on F with w = 4Fo2/2(Fo2), where 2(Fo2) = [2(I) + (0.050Fo2)2] for 3158 reflections with I > 3(I) was reached at R = 0.095 and wR = 0.137 with a goodness of fit of 3.71.  (/)max = 0.05 for atoms refined anisotropically.  The final difference Fourier map was featureless, with maximum positive and negative peaks of 1.26 and 0.74 eÅ3 respectively.

. A. Altomare, M. Cascarano, C. Giacovazzo, A. Guagliardi, M. C. Burla, G. Polidori and M. Camalli, J. Appl. Cryst., 1994, 27, 435.

. TeXsan: Crystal Structure Analysis Package, Molecular Structure Corporation, 1985 and 1992, the Woodlands, Texas, U.S.A.

. In “The HKL manual – A description of programs DENZO, XDISPLAYF, and SCALEPACK” written by D. Gewirth, with the co-operation of the program authors Z. Otwinowski and W. Minor (1995), Yale University, New Haven, U.S.A.

. P. T. Beurskens, G. Admiraal, G. Beurskens, W. P. Bosman, S. Garcia-Granda, R. O. Gould, J. M. M. Smits and C. Smykalla, 1992, The DIRDIF program system, Technical Report of the Crystallography Laboratory, University of Nijimegen, The Netherlands.