##### Supplementary information

Crystal structures, magnetic and spectroscopic properties of manganese(II), cobalt(II), nickel(II) and zinc(II) dichloro complexes bearing two 2-pyridyl-substituted imino nitroxides

# Youhei Yamamoto, Takayoshi Suzuki and Sumio Kaizaki*

# Contents

Figure S1	Perspective drawings of (a) (OC-6-22)-[CoCl2(IM2py)2] 2, (b) (OC-6-22)-[NiCl2(IM2py)2] 3 and (c) (OC-6-22)-[ZnCl2(IM2py)2] 4.  Hydrogen atoms are omitted for clarity, and the thermal elipsoids are drawn at 50% probability level.

Figure S2	Temperature-dependence of vis-NIR absorption spectrum of complex 2 in dichloromethane: 300 K (• • • • • • •), 275 K (– • • – • • –), 250 K (— • — • —), 225 K (–  –  –  –) and 200 K (———).

Figure S3	Temperature-dependence of vis-NIR absorption spectrum of complex 1 in dichloromethane: 300 K (• • • • • • •), 275 K (– • • – • • –), 250 K (— • — • —), 225 K (–  –  –  –) and 200 K (———).

Equations S1–S4	Equations used in the analyses of magnetic susceptibitily data for complexes 4, 1, 3 and 2, respectively.

Figure S1	Perspective drawings of (a) (OC-6-22)-[CoCl2(IM2py)2] 2, (b) (OC-6-22)-[NiCl2(IM2py)2] 3 and (c) (OC-6-22)-[ZnCl2(IM2py)2] 4.  Hydrogen atoms are omitted for clarity, and the thermal elipsoids are drawn at 50% probability level.

Figure S2	Temperature-dependence of vis-NIR absorption spectrum of complex 2 in dichloromethane: 300 K (• • • • • • •), 275 K (– • • – • • –), 250 K (— • — • —), 225 K (–  –  –  –) and 200 K (———).

Figure S3	Temperature-dependence of vis-NIR absorption spectrum of complex 1 in dichloromethane: 300 K (• • • • • • •), 275 K (– • • – • • –), 250 K (— • — • —), 225 K (–  –  –  –) and 200 K (———).

Equations S1	Equation used in the analyses of magnetic susceptibitily data for complex 4.

2N2gR(bis)2            MW(bis)  N2gR(mono)2

M = ———————— • (1–) + ———— • —————— • 

kT{3 + exp(2J’/kT)}         MW(mono)    4kT

where J’ is a coupling constant between two IM2py (H = – 2J'SR1• SR2), gR(bis) and gR(mono) are g factors of IM2py radicals in [ZnCl2(IM2py)2] and [ZnCl2(IM2py)], respectively, MW(bis) and MW(mono) are molecular weight of [ZnCl2(IM2py)2] and [ZnCl2(IM2py)], respectively, and  is an impurity factor of comtamination with [ZnCl2(IM2py)].  Other symbols have their usual meanings.

Equations S2	Equation used in the analyses of magnetic susceptibitily data for complex 1.

N2   10g12 + 35g22e5x + 84g32e12x + 35g42e7x–2x’

M = —— • ———————————————————

4kT        2 + 3e5x + 4e12x + 3e7x–2x’

where x and x' denote J/kT and J’/kT (H = – 2J SMn•(SR1 + SR2) – 2J' SR1• SR2), respectively, and g1, g2, g3, and g4 express (7gMn – 2gR)/5, (31gMn + 4gR)/35, (5gMn + 2gR)/7, and gMn, respectively.  Other symbols have their usual meanings.

Equations S3	Equation used in the analyses of magnetic susceptibitily data for complex 3.

N2      (gNi + gR)2(5 + e–4x) + 4gNi2e–2x–2x’

M = ———— • ———————————————

2k(T–)      5 + 3e–4x + e–6x + 3e–2x–2x’

where x and x' denote J/kT and J’/kT (H = – 2J SNi•(SR1 + SR2) – 2J' SR1• SR2), respectively.  The parameter  is Weiss constant, and other symbols have their usual meanings.

Equations S4	Equation used in the analyses of magnetic susceptibitily data for complex 2.

N2    35g12 + 10g22e–5x + g32e–8x + 10g42e–3x–2x’

M = ———— • ———————————————————

4k(T–)        3 + 2e–5x + e–8x + 2e–3x–2x’

where x and x' denote J/kT and J’/kT (H = – 2J SCo•(SR1 + SR2) – 2J' SR1• SR2), respectively, and g1, g2, g3, and g4 express (3gCo + 2gR)/5, (11gCo + 4gR)/15, (5gCo – 2gR)/3, and gCo, respectively.  Other symbols including  have their usual meanings.