*******************************************************

*** PROGRAM FULLPROF (Version 3.2  - Jan97-LLB JRC) ***

*******************************************************

Rietveld, Profile Matching & Integrated Intensity

Refinement of X-ray and/or Neutron Data

Date & Time: 18-MAY-00 15:29:49

=> PCR file code: mnncobpa

=> DAT file code: mnncobpa

=> Title:  compound 2 [Mn(NCO)2bpa2]·bpa

==> CONDITIONS OF THIS RUN:

=> Global Refinement of X-ray powder diffraction data

Bragg-Brentano or Debye-Scherrer geometry

=> The    5th default profile function was selected

=> Data supplied in free format

=> Analysis of refinement at the end

=> Wavelengths:  1.54056 1.54433

=> Base of peaks: 2.0*HW*    7.50

=> Cos(Monochromator angle)=   0.7899

=> Absorption correction (muR-eff):   0.0000

==> Angular range, step and number of points:

2Thmin:   5.0000  2Thmax:  60.0000  Step:   0.0200  No. of points:   2751

=> Pattern Matching (fixed scale) for phase: 1

=> Scor: 2.3278

==> RESULTS OF REFINEMENT:

=> No. of fitted parameters:    9

------------------------------------------------------------------------------

=> Phase No.  1 compound 2 [Mn(NCO)2bpa2]·bpa                     C 2/c

------------------------------------------------------------------------------

=>  No. of reflections:   1060

==> PROFILE PARAMETERS:

=> Cell parameters      :

19.96724   0.00490

9.84135   0.00237

18.87326   0.00390

90.00000   0.00000

95.63611   0.00942

90.00000   0.00000

=> Overall scale factor :    1.000000000   0.000000000

=> ETA(p-V) or M(P-VII) :    1.30039   0.04578

=> Overall Tem. factor  :    0.00000   0.00000

=> Halfwidth parameters :    0.00000   0.00000

0.00000   0.00000

0.01524   0.00131

=> Preferred orientation:    0.00000   0.00000

0.00000   0.00000

=> Asymmetry parameters :    0.02483   0.00566

-0.00465   0.00136

0.00000   0.00000

0.00000   0.00000

=> X and Y parameters   :    0.00000   0.00000

0.00000   0.00000

=> Strain parameters    :    0.00000   0.00000

0.00000   0.00000

0.00000   0.00000

=> Size   parameters    :    0.00000   0.00000

0.00000   0.00000

==> GLOBAL PARAMETERS:

=> Zero-point:   0.0000  0.0000

=> Cos( theta)-shift parameter :   0.0529  0.0052

=> Sin(2theta)-shift parameter :   0.0000  0.0000

==> RELIABILITY FACTORS WITH ALL NON-EXCLUDED POINTS:

=> Cycle: 10 => MaxCycle: 10

=> N-P+C:  2741

=> Rp: 8.78     Rwp: 12.0     Rexp:    8.04 Chi2:  2.22      L.S. refinement

=> Conventional Rietveld R-factors ==>

=> Rp: 30.2     Rwp: 27.6     Rexp:   18.53 Chi2:  2.22

=> Deviance: 0.619E+04     Dev*  :  2.252

=> DW-Stat.:    0.9323     DW-exp:     1.8880

=> N-sigma of the GoF:   45.088

==> RELIABILITY FACTORS FOR POINTS WITH BRAGG CONTRIBUTIONS:

=> N-P+C:  2583

=> Rp: 9.40     Rwp: 12.6     Rexp:    8.33 Chi2:  2.29      L.S. refinement

=> Conventional Rietveld R-factors ==>

=> Rp: 28.3     Rwp: 27.3     Rexp:   18.01 Chi2:  2.29

=> Deviance: 0.603E+04     Dev*  :  2.330

=> DW-Stat.:    0.9574     DW-exp:     1.8848

=> N-sigma of the GoF:       46.430

=> Phase:  1

=> Bragg R-factor:  5.67       Vol:    3690.755   Fract(%):     0.00

=> Rf-factor= 3.11             ATZ:       0.000   Brindley:   1.0000