Supplementary material  (01/6/14)

Synthesis and characterization of tri-titanium(IV)-1,2,3-substituted -Keggin polyoxotungstates with heteroatoms P and Si.  Crystal structure of the dimeric, Ti-O-Ti bridged anhydride form K10H2[-P2W18Ti6O77]•17H2O and confirmation of dimeric forms in aqueous solution by ultracentrifugation molecular weight measurements

Kenji Nomiya, *a Mizuto Takahashi, a Katsunori Ohsawa a and Jason A. Widegren b

a Department of Materials Science, Faculty of Science, Kanagawa University, Hiratsuka, Kanagawa 259-1293, Japan.  E-mail: nomiya@chem.kanagawa-u.ac.jp

b Department of Chemistry, Colorado State University, Fort Collins, CO 80523, USA.

Received xxx xxxx 2001; accepted xxx xxxx 2001

Bond lengths and angles of compound 1, which are not listed in Table 2, are deposited in Table A.

# Table A  Bond lengths (Å) and angles (o) for the polyoxoanion 1

Distances(Å)

atom	atom	distance		atom	atom	distance

W(1)	O(9)	1.81(1)		W(1)	O(10)	1.95(1)

W(1)	O(15)	1.89(1)		W(1)	O(21)	2.00(1)

W(1)	O(25)	2.46(1)		W(1)	O(34)	1.73(2)

W(2)	O(4)	1.85(1)		W(2)	O(10)	1.93(1)

W(2)	O(11)	1.89(1)		W(2)	O(16)	1.96(1)

W(2)	O(25)	2.41(1)		W(2)	O(29)	1.72(1)

W(3)	O(6)	1.84(1)		W(3)	O(11)	1.93(1)

W(3)	O(12)	1.93(1)		W(3)	O(17)	1.96(1)

W(3)	O(26)	2.43(1)		W(3)	O(30)	1.71(1)

W(4)	O(5)	1.82(1)		W(4)	O(12)	1.91(1)

W(4)	O(13)	1.94(1)		W(4)	O(18)	1.97(1)

W(4)	O(26)	2.42(1)		W(4)	O(31)	1.71(2)

W(5)	O(8)	1.83(1)		W(5)	O(13)	1.88(1)

W(5)	O(14)	1.91(1)		W(5)	O(19)	1.94(1)

atom	atom	distance		atom	atom	distance

W(5)	O(27)	2.47(1)		W(5)	O(32)	1.70(1)

W(6)	O(7)	1.82(1)		W(6)	O(14)	1.94(1)

W(6)	O(15)	1.95(1)		W(6)	O(20)	1.98(1)

W(6)	O(27)	2.44(1)		W(6)	O(33)	1.74(1)

W(7)	O(20)	1.87(1)		W(7)	O(21)	1.87(1)

W(7)	O(22)	1.91(1)		W(7)	O(24)	1.91(1)

W(7)	O(28)	2.42(1)		W(7)	O(37)	1.73(1)

W(8)	O(16)	1.89(1)		W(8)	O(17)	1.89(1)

W(8)	O(22)	1.91(1)		W(8)	O(23)	1.92(1)

W(8)	O(28)	2.46(1)		W(8)	O(35)	1.72(1)

W(9)	O(18)	1.89(1)		W(9)	O(19)	1.90(1)

W(9)	O(23)	1.91(1)		W(9)	O(24)	1.92(1)

W(9)	O(28)	2.45(1)		W(9)	O(36)	1.70(1)

W(10)	O(44)	1.84(1)		W(10)	O(50)	1.94(1)

W(10)	O(51)	1.89(1)		W(10)	O(56)	1.96(1)

W(10)	O(65)	2.41(1)		W(10)	O(69)	1.70(2)

W(11)	O(45)	1.83(1)		W(11)	O(51)	1.93(1)

atom	atom	distance		atom	atom	distance

W(11)	O(52)	1.93(1)		W(11)	O(57)	1.99(1)

W(11)	O(66)	2.44(1)		W(11)	O(70)	1.73(1)

W(12)	O(46)	1.82(1)		W(12)	O(52)	1.93(1)

W(12)	O(53)	1.95(1)		W(12)	O(58)	1.97(1)

W(12)	O(66)	2.42(1)		W(12)	O(71)	1.70(1)

W(13)	O(47)	1.84(1)		W(13)	O(53)	1.89(1)

W(13)	O(54)	1.89(1)		W(13)	O(59)	1.94(1)

W(13)	O(67)	2.45(1)		W(13)	O(72)	1.71(2)

W(14)	O(48)	1.84(1)		W(14)	O(54)	1.97(1)

W(14)	O(55)	1.93(1)		W(14)	O(60)	1.94(1)

W(14)	O(67)	2.45(1)		W(14)	O(73)	1.73(1)

W(15)	O(49)	1.84(1)		W(15)	O(50)	1.93(1)

W(15)	O(55)	1.91(1)		W(15)	O(61)	1.95(1)

W(15)	O(65)	2.45(1)		W(15)	O(74)	1.73(2)

W(16)	O(56)	1.90(1)		W(16)	O(57)	1.87(1)

W(16)	O(62)	1.89(1)		W(16)	O(63)	1.90(1)

W(16)	O(68)	2.45(1)		W(16)	O(75)	1.71(1)

atom	atom	distance		atom	atom	distance

W(17)	O(58)	1.88(1)		W(17)	O(59)	1.89(1)

W(17)	O(63)	1.93(1)		W(17)	O(64)	1.92(2)

W(17)	O(68)	2.44(1)		W(17)	O(76)	1.71(1)

W(18)	O(60)	1.90(1)		W(18)	O(61)	1.90(1)

W(18)	O(62)	1.94(1)		W(18)	O(64)	1.90(2)

W(18)	O(68)	2.44(1)		W(18)	O(77)	1.73(2)

Ti(1)	O(1)	1.83(1)		Ti(1)	O(3)	1.90(1)

Ti(1)	O(4)	1.99(1)		Ti(1)	O(9)	2.04(1)

Ti(1)	O(25)	2.34(1)		Ti(1)	O(38)	1.85(1)

Ti(2)	O(1)	1.85(1)		Ti(2)	O(2)	1.87(1)

Ti(2)	O(5)	2.03(1)		Ti(2)	O(6)	2.01(1)

Ti(2)	O(26)	2.36(1)		Ti(2)	O(39)	1.86(1)

Ti(3)	O(2)	1.79(1)		Ti(3)	O(3)	1.92(1)

Ti(3)	O(7)	2.05(1)		Ti(3)	O(8)	2.01(1)

Ti(3)	O(27)	2.30(1)		Ti(3)	O(40)	1.83(1)

Ti(4)	O(38)	1.80(1)		Ti(4)	O(41)	1.87(1)

Ti(4)	O(43)	1.87(1)		Ti(4)	O(44)	2.00(1)

atom	atom	distance		atom	atom	distance

Ti(4)	O(49)	2.00(1)		Ti(4)	O(65)	2.39(1)

Ti(5)	O(39)	1.82(1)		Ti(5)	O(41)	1.88(1)

Ti(5)	O(42)	1.88(1)		Ti(5)	O(45)	2.01(1)

Ti(5)	O(46)	1.98(1)		Ti(5)	O(66)	2.37(1)

Ti(6)	O(40)	1.83(1)		Ti(6)	O(42)	1.81(1)

Ti(6)	O(43)	1.91(2)		Ti(6)	O(47)	2.00(1)

Ti(6)	O(48)	2.01(1)		Ti(6)	O(67)	2.32(1)

P(1)	O(25)	1.55(1)		P(1)	O(26)	1.55(1)

P(1)	O(27)	1.54(1)		P(1)	O(28)	1.53(1)

P(2)	O(65)	1.53(1)		P(2)	O(66)	1.53(1)

P(2)	O(67)	1.54(1)		P(2)	O(68)	1.52(1)

Angles(°)

atom	atom	atom	angle		atom	atom	atom	angle

O(9)	W(1)	O(10)	90.4(5)		O(9)	W(1)	O(15)	92.1(5)

O(9)	W(1)	O(21)	156.7(6)		O(9)	W(1)	O(25)	74.3(5)

O(9)	W(1)	O(34)	103.2(6)		O(10)	W(1)	O(15)	155.6(6)

O(10)	W(1)	O(21)	83.9(5)		O(10)	W(1)	O(25)	72.6(5)

O(10)	W(1)	O(34)	100.8(6)		O(15)	W(1)	O(21)	84.3(5)

O(15)	W(1)	O(25)	84.8(5)		O(15)	W(1)	O(34)	102.3(6)

O(21)	W(1)	O(25)	82.5(5)		O(21)	W(1)	O(34)	100.0(6)

O(25)	W(1)	O(34)	172.7(6)		O(4)	W(2)	O(10)	89.9(6)

O(4)	W(2)	O(11)	91.5(6)		O(4)	W(2)	O(16)	157.9(6)

O(4)	W(2)	O(25)	74.9(5)		O(4)	W(2)	O(29)	104.2(6)

O(10)	W(2)	O(11)	155.6(6)		O(10)	W(2)	O(16)	84.5(5)

O(10)	W(2)	O(25)	74.1(5)		O(10)	W(2)	O(29)	100.3(6)

O(11)	W(2)	O(16)	85.0(5)		O(11)	W(2)	O(25)	82.8(5)

O(11)	W(2)	O(29)	102.9(6)		O(16)	W(2)	O(25)	83.0(5)

O(16)	W(2)	O(29)	97.8(6)		O(25)	W(2)	O(29)	174.3(6)

atom	atom	atom	angle		atom	atom	atom	angle

O(6)	W(3)	O(11)	91.5(6)		O(6)	W(3)	O(12)	89.5(6)

O(6)	W(3)	O(17)	157.3(5)		O(6)	W(3)	O(26)	74.4(5)

O(6)	W(3)	O(30)	102.8(6)		O(11)	W(3)	O(12)	154.5(5)

O(11)	W(3)	O(17)	83.5(5)		O(11)	W(3)	O(26)	82.8(5)

O(11)	W(3)	O(30)	101.8(6)		O(12)	W(3)	O(17)	85.8(6)

O(12)	W(3)	O(26)	73.0(5)		O(12)	W(3)	O(30)	102.8(7)

O(17)	W(3)	O(26)	83.0(5)		O(17)	W(3)	O(30)	99.8(6)

O(26)	W(3)	O(30)	174.8(6)		O(5)	W(4)	O(12)	89.6(6)

O(5)	W(4)	O(13)	93.6(5)		O(5)	W(4)	O(18)	157.9(6)

O(5)	W(4)	O(26)	74.5(5)		O(5)	W(4)	O(31)	100.4(6)

O(12)	W(4)	O(13)	155.9(6)		O(12)	W(4)	O(18)	84.8(5)

O(12)	W(4)	O(26)	73.4(5)		O(12)	W(4)	O(31)	99.4(7)

O(13)	W(4)	O(18)	83.2(5)		O(13)	W(4)	O(26)	84.5(5)

O(13)	W(4)	O(31)	103.5(6)		O(18)	W(4)	O(26)	83.5(5)

O(18)	W(4)	O(31)	101.6(6)		O(26)	W(4)	O(31)	170.9(6)

O(8)	W(5)	O(13)	92.1(6)		O(8)	W(5)	O(14)	88.8(6)

O(8)	W(5)	O(19)	156.2(6)		O(8)	W(5)	O(27)	73.5(5)

atom	atom	atom	angle		atom	atom	atom	angle

O(8)	W(5)	O(32)	103.3(6)		O(13)	W(5)	O(14)	154.4(6)

O(13)	W(5)	O(19)	83.6(5)		O(13)	W(5)	O(27)	83.0(5)

O(13)	W(5)	O(32)	104.6(6)		O(14)	W(5)	O(19)	85.3(6)

O(14)	W(5)	O(27)	72.7(5)		O(14)	W(5)	O(32)	100.1(6)

O(19)	W(5)	O(27)	82.8(5)		O(19)	W(5)	O(32)	100.4(6)

O(27)	W(5)	O(32)	172.0(5)		O(7)	W(6)	O(14)	90.9(6)

O(7)	W(6)	O(15)	92.6(6)		O(7)	W(6)	O(20)	156.0(6)

O(7)	W(6)	O(27)	74.5(5)		O(7)	W(6)	O(33)	103.7(6)

O(14)	W(6)	O(15)	155.2(5)		O(14)	W(6)	O(20)	84.0(6)

O(14)	W(6)	O(27)	73.1(5)		O(14)	W(6)	O(33)	100.2(6)

O(15)	W(6)	O(20)	83.0(6)		O(15)	W(6)	O(27)	84.2(5)

O(15)	W(6)	O(33)	102.8(6)		O(20)	W(6)	O(27)	81.7(5)

O(20)	W(6)	O(33)	100.2(6)		O(27)	W(6)	O(33)	172.8(6)

O(20)	W(7)	O(21)	89.1(6)		O(20)	W(7)	O(22)	154.4(6)

O(20)	W(7)	O(24)	88.6(6)		O(20)	W(7)	O(28)	82.4(5)

O(20)	W(7)	O(37)	103.3(6)		O(21)	W(7)	O(22)	88.0(6)

O(21)	W(7)	O(24)	156.2(5)		O(21)	W(7)	O(28)	84.1(5)

atom	atom	atom	angle		atom	atom	atom	angle

O(21)	W(7)	O(37)	101.7(6)		O(22)	W(7)	O(24)	84.0(6)

O(22)	W(7)	O(28)	72.0(5)		O(22)	W(7)	O(37)	102.1(6)

O(24)	W(7)	O(28)	72.0(5)		O(24)	W(7)	O(37)	102.0(6)

O(28)	W(7)	O(37)	171.8(6)		O(16)	W(8)	O(17)	87.8(6)

O(16)	W(8)	O(22)	87.9(6)		O(16)	W(8)	O(23)	155.7(6)

O(16)	W(8)	O(28)	83.1(5)		O(16)	W(8)	O(35)	101.7(6)

O(17)	W(8)	O(22)	154.6(6)		O(17)	W(8)	O(23)	88.4(6)

O(17)	W(8)	O(28)	83.7(5)		O(17)	W(8)	O(35)	102.5(6)

O(22)	W(8)	O(23)	85.3(6)		O(22)	W(8)	O(28)	70.9(5)

O(22)	W(8)	O(35)	102.9(6)		O(23)	W(8)	O(28)	72.6(5)

O(23)	W(8)	O(35)	102.6(6)		O(28)	W(8)	O(35)	172.2(5)

O(18)	W(9)	O(19)	87.4(5)		O(18)	W(9)	O(23)	88.7(5)

O(18)	W(9)	O(24)	155.7(6)		O(18)	W(9)	O(28)	84.5(5)

O(18)	W(9)	O(36)	100.2(6)		O(19)	W(9)	O(23)	156.2(6)

O(19)	W(9)	O(24)	88.8(6)		O(19)	W(9)	O(28)	83.2(5)

O(19)	W(9)	O(36)	101.6(6)		O(23)	W(9)	O(24)	85.2(6)

O(23)	W(9)	O(28)	73.1(5)		O(23)	W(9)	O(36)	102.2(6)

atom	atom	atom	angle		atom	atom	atom	angle

O(24)	W(9)	O(28)	71.3(5)		O(24)	W(9)	O(36)	104.1(6)

O(28)	W(9)	O(36)	173.4(6)		O(44)	W(10)	O(50)	89.8(6)

O(44)	W(10)	O(51)	93.0(5)		O(44)	W(10)	O(56)	157.3(6)

O(44)	W(10)	O(65)	74.9(5)		O(44)	W(10)	O(69)	102.5(6)

O(50)	W(10)	O(51)	155.2(6)		O(50)	W(10)	O(56)	85.5(6)

O(50)	W(10)	O(65)	74.1(5)		O(50)	W(10)	O(69)	101.8(7)

O(51)	W(10)	O(56)	82.5(6)		O(51)	W(10)	O(65)	82.9(5)

O(51)	W(10)	O(69)	101.6(7)		O(56)	W(10)	O(65)	82.4(5)

O(56)	W(10)	O(69)	100.2(6)		O(65)	W(10)	O(69)	175.0(6)

O(45)	W(11)	O(51)	92.6(5)		O(45)	W(11)	O(52)	91.2(6)

O(45)	W(11)	O(57)	156.7(5)		O(45)	W(11)	O(66)	74.3(5)

O(45)	W(11)	O(70)	103.9(6)		O(51)	W(11)	O(52)	154.7(5)

O(51)	W(11)	O(57)	81.3(5)		O(51)	W(11)	O(66)	82.9(5)

O(51)	W(11)	O(70)	100.8(6)		O(52)	W(11)	O(57)	85.3(5)

O(52)	W(11)	O(66)	74.1(5)		O(52)	W(11)	O(70)	102.5(6)

O(57)	W(11)	O(66)	82.6(5)		O(57)	W(11)	O(70)	99.4(6)

O(66)	W(11)	O(70)	176.0(6)		O(46)	W(12)	O(52)	92.7(5)

atom	atom	atom	angle		atom	atom	atom	angle

O(46)	W(12)	O(53)	90.1(5)		O(46)	W(12)	O(58)	156.6(6)

O(46)	W(12)	O(66)	74.2(5)		O(46)	W(12)	O(71)	103.4(6)

O(52)	W(12)	O(53)	156.5(6)		O(52)	W(12)	O(58)	84.7(5)

O(52)	W(12)	O(66)	74.6(5)		O(52)	W(12)	O(71)	101.1(6)

O(53)	W(12)	O(58)	83.5(5)		O(53)	W(12)	O(66)	83.9(5)

O(53)	W(12)	O(71)	100.8(6)		O(58)	W(12)	O(66)	82.7(5)

O(58)	W(12)	O(71)	99.9(6)		O(66)	W(12)	O(71)	174.8(6)

O(47)	W(13)	O(53)	90.6(5)		O(47)	W(13)	O(54)	90.7(6)

O(47)	W(13)	O(59)	157.4(6)		O(47)	W(13)	O(67)	74.0(5)

O(47)	W(13)	O(72)	101.9(6)		O(53)	W(13)	O(54)	156.0(6)

O(53)	W(13)	O(59)	84.3(5)		O(53)	W(13)	O(67)	83.1(5)

O(53)	W(13)	O(72)	101.7(7)		O(54)	W(13)	O(59)	85.4(6)

O(54)	W(13)	O(67)	74.3(5)		O(54)	W(13)	O(72)	101.5(7)

O(59)	W(13)	O(67)	83.5(5)		O(59)	W(13)	O(72)	100.7(6)

O(67)	W(13)	O(72)	173.9(6)		O(48)	W(14)	O(54)	89.7(6)

O(48)	W(14)	O(55)	91.6(6)		O(48)	W(14)	O(60)	155.1(6)

O(48)	W(14)	O(67)	73.9(5)		O(48)	W(14)	O(73)	103.5(6)

atom	atom	atom	angle		atom	atom	atom	angle

O(54)	W(14)	O(55)	155.1(6)		O(54)	W(14)	O(60)	83.9(6)

O(54)	W(14)	O(67)	72.8(5)		O(54)	W(14)	O(73)	102.0(7)

O(55)	W(14)	O(60)	84.5(5)		O(55)	W(14)	O(67)	83.6(5)

O(55)	W(14)	O(73)	101.8(7)		O(60)	W(14)	O(67)	81.2(5)

O(60)	W(14)	O(73)	101.4(6)		O(67)	W(14)	O(73)	174.1(6)

O(49)	W(15)	O(50)	89.1(6)		O(49)	W(15)	O(55)	91.8(6)

O(49)	W(15)	O(61)	156.6(6)		O(49)	W(15)	O(65)	75.0(5)

O(49)	W(15)	O(74)	100.3(7)		O(50)	W(15)	O(55)	156.7(6)

O(50)	W(15)	O(61)	85.5(6)		O(50)	W(15)	O(65)	73.5(5)

O(50)	W(15)	O(74)	101.1(7)		O(55)	W(15)	O(61)	84.5(6)

O(55)	W(15)	O(65)	84.3(5)		O(55)	W(15)	O(74)	101.6(7)

O(61)	W(15)	O(65)	81.7(5)		O(61)	W(15)	O(74)	103.1(7)

O(65)	W(15)	O(74)	172.6(6)		O(56)	W(16)	O(57)	86.4(6)

O(56)	W(16)	O(62)	87.7(6)		O(56)	W(16)	O(63)	155.4(6)

O(56)	W(16)	O(68)	83.7(5)		O(56)	W(16)	O(75)	103.0(6)

O(57)	W(16)	O(62)	155.5(6)		O(57)	W(16)	O(63)	89.5(6)

O(57)	W(16)	O(68)	83.5(5)		O(57)	W(16)	O(75)	102.2(6)

atom	atom	atom	angle		atom	atom	atom	angle

O(62)	W(16)	O(63)	86.1(6)		O(62)	W(16)	O(68)	72.3(5)

O(62)	W(16)	O(75)	102.3(6)		O(63)	W(16)	O(68)	71.7(5)

O(63)	W(16)	O(75)	101.6(6)		O(68)	W(16)	O(75)	171.4(5)

O(58)	W(17)	O(59)	88.4(6)		O(58)	W(17)	O(63)	87.3(6)

O(58)	W(17)	O(64)	154.6(6)		O(58)	W(17)	O(68)	82.3(5)

O(58)	W(17)	O(76)	103.4(6)		O(59)	W(17)	O(63)	155.2(6)

O(59)	W(17)	O(64)	86.8(6)		O(59)	W(17)	O(68)	83.6(5)

O(59)	W(17)	O(76)	102.4(6)		O(63)	W(17)	O(64)	86.6(6)

O(63)	W(17)	O(68)	71.6(5)		O(63)	W(17)	O(76)	102.3(6)

O(64)	W(17)	O(68)	72.3(5)		O(64)	W(17)	O(76)	102.0(7)

O(68)	W(17)	O(76)	171.6(6)		O(60)	W(18)	O(61)	86.1(6)

O(60)	W(18)	O(62)	153.6(6)		O(60)	W(18)	O(64)	87.5(6)

O(60)	W(18)	O(68)	82.3(5)		O(60)	W(18)	O(77)	102.0(6)

O(61)	W(18)	O(62)	87.5(6)		O(61)	W(18)	O(64)	155.5(6)

O(61)	W(18)	O(68)	83.2(5)		O(61)	W(18)	O(77)	101.7(7)

O(62)	W(18)	O(64)	87.7(6)		O(62)	W(18)	O(68)	71.6(5)

O(62)	W(18)	O(77)	104.4(7)		O(64)	W(18)	O(68)	72.5(5)

atom	atom	atom	angle		atom	atom	atom	angle

O(64)	W(18)	O(77)	102.8(7)		O(68)	W(18)	O(77)	173.6(6)

O(1)	Ti(1)	O(3)	92.2(6)		O(1)	Ti(1)	O(4)	90.3(6)

O(1)	Ti(1)	O(9)	158.9(5)		O(1)	Ti(1)	O(25)	85.5(5)

O(1)	Ti(1)	O(38)	102.6(6)		O(3)	Ti(1)	O(4)	159.1(5)

O(3)	Ti(1)	O(9)	86.0(5)		O(3)	Ti(1)	O(25)	85.2(5)

O(3)	Ti(1)	O(38)	101.0(6)		O(4)	Ti(1)	O(9)	84.3(5)

O(4)	Ti(1)	O(25)	74.2(5)		O(4)	Ti(1)	O(38)	98.7(6)

O(9)	Ti(1)	O(25)	73.4(5)		O(9)	Ti(1)	O(38)	98.3(6)

O(25)	Ti(1)	O(38)	169.4(6)		O(1)	Ti(2)	O(2)	91.8(6)

O(1)	Ti(2)	O(5)	157.8(5)		O(1)	Ti(2)	O(6)	89.8(6)

O(1)	Ti(2)	O(26)	85.5(5)		O(1)	Ti(2)	O(39)	99.9(6)

O(2)	Ti(2)	O(5)	88.2(6)		O(2)	Ti(2)	O(6)	157.5(5)

O(2)	Ti(2)	O(26)	84.6(5)		O(2)	Ti(2)	O(39)	102.8(6)

O(5)	Ti(2)	O(6)	82.0(5)		O(5)	Ti(2)	O(26)	72.4(5)

O(5)	Ti(2)	O(39)	101.7(6)		O(6)	Ti(2)	O(26)	73.2(5)

O(6)	Ti(2)	O(39)	98.9(5)		O(26)	Ti(2)	O(39)	170.5(5)

O(2)	Ti(3)	O(3)	92.7(6)		O(2)	Ti(3)	O(7)	160.9(6)

atom	atom	atom	angle		atom	atom	atom	angle

O(2)	Ti(3)	O(8)	92.5(6)		O(2)	Ti(3)	O(27)	87.0(5)

O(2)	Ti(3)	O(40)	102.5(6)		O(3)	Ti(3)	O(7)	85.3(5)

O(3)	Ti(3)	O(8)	158.8(5)		O(3)	Ti(3)	O(27)	85.2(5)

O(3)	Ti(3)	O(40)	98.9(6)		O(7)	Ti(3)	O(8)	83.1(5)

O(7)	Ti(3)	O(27)	73.9(5)		O(7)	Ti(3)	O(40)	96.5(5)

O(8)	Ti(3)	O(27)	74.6(5)		O(8)	Ti(3)	O(40)	100.0(6)

O(27)	Ti(3)	O(40)	169.4(5)		O(38)	Ti(4)	O(41)	101.1(6)

O(38)	Ti(4)	O(43)	101.3(6)		O(38)	Ti(4)	O(44)	100.8(6)

O(38)	Ti(4)	O(49)	100.3(6)		O(38)	Ti(4)	O(65)	171.7(6)

O(41)	Ti(4)	O(43)	91.9(6)		O(41)	Ti(4)	O(44)	88.9(6)

O(41)	Ti(4)	O(49)	158.0(6)		O(41)	Ti(4)	O(65)	84.4(5)

O(43)	Ti(4)	O(44)	157.4(6)		O(43)	Ti(4)	O(49)	88.5(6)

O(43)	Ti(4)	O(65)	84.6(5)		O(44)	Ti(4)	O(49)	82.5(5)

O(44)	Ti(4)	O(65)	72.9(5)		O(49)	Ti(4)	O(65)	73.7(5)

O(39)	Ti(5)	O(41)	100.8(6)		O(39)	Ti(5)	O(42)	101.8(6)

O(39)	Ti(5)	O(45)	100.9(6)		O(39)	Ti(5)	O(46)	102.0(6)

O(39)	Ti(5)	O(66)	172.0(5)		O(41)	Ti(5)	O(42)	91.5(6)

atom	atom	atom	angle		atom	atom	atom	angle

O(41)	Ti(5)	O(45)	87.1(6)		O(41)	Ti(5)	O(46)	157.0(5)

O(41)	Ti(5)	O(66)	84.3(5)		O(42)	Ti(5)	O(45)	157.1(5)

O(42)	Ti(5)	O(46)	86.8(6)		O(42)	Ti(5)	O(66)	84.0(5)

O(45)	Ti(5)	O(46)	85.6(5)		O(45)	Ti(5)	O(66)	73.1(5)

O(46)	Ti(5)	O(66)	72.7(5)		O(40)	Ti(6)	O(42)	102.9(6)

O(40)	Ti(6)	O(43)	101.9(6)		O(40)	Ti(6)	O(47)	98.2(5)

O(40)	Ti(6)	O(48)	96.7(6)		O(40)	Ti(6)	O(67)	168.7(5)

O(42)	Ti(6)	O(43)	92.3(6)		O(42)	Ti(6)	O(47)	89.7(6)

O(42)	Ti(6)	O(48)	160.1(6)		O(42)	Ti(6)	O(67)	85.8(5)

O(43)	Ti(6)	O(47)	158.8(6)		O(43)	Ti(6)	O(48)	87.1(6)

O(43)	Ti(6)	O(67)	84.7(5)		O(47)	Ti(6)	O(48)	83.9(6)

O(47)	Ti(6)	O(67)	74.4(5)		O(48)	Ti(6)	O(67)	74.3(5)

O(25)	P(1)	O(26)	108.6(7)		O(25)	P(1)	O(27)	110.3(7)

O(25)	P(1)	O(28)	109.0(7)		O(26)	P(1)	O(27)	109.3(7)

O(26)	P(1)	O(28)	110.2(7)		O(27)	P(1)	O(28)	109.5(7)

O(65)	P(2)	O(66)	109.0(7)		O(65)	P(2)	O(67)	110.5(7)

O(65)	P(2)	O(68)	109.5(7)		O(66)	P(2)	O(67)	108.5(7)

atom	atom	atom	angle		atom	atom	atom	angle

O(66)	P(2)	O(68)	109.5(7)		O(67)	P(2)	O(68)	109.8(7)

Ti(1)	O(1)	Ti(2)	147.2(7)		Ti(2)	O(2)	Ti(3)	147.0(8)

Ti(1)	O(3)	Ti(3)	141.7(7)		W(2)	O(4)	Ti(1)	121.3(7)

W(4)	O(5)	Ti(2)	122.8(7)		W(3)	O(6)	Ti(2)	122.6(6)

W(6)	O(7)	Ti(3)	121.1(7)		W(5)	O(8)	Ti(3)	122.5(7)

W(1)	O(9)	Ti(1)	122.8(7)		W(1)	O(10)	W(2)	123.3(7)

W(2)	O(11)	W(3)	155.0(7)		W(3)	O(12)	W(4)	124.0(7)

W(4)	O(13)	W(5)	155.3(7)		W(5)	O(14)	W(6)	125.1(7)

W(1)	O(15)	W(6)	154.6(8)		W(2)	O(16)	W(8)	149.6(8)

W(3)	O(17)	W(8)	151.3(8)		W(4)	O(18)	W(9)	149.6(7)

W(5)	O(19)	W(9)	151.3(7)		W(6)	O(20)	W(7)	151.4(8)

W(1)	O(21)	W(7)	148.8(8)		W(7)	O(22)	W(8)	127.8(7)

W(8)	O(23)	W(9)	126.0(7)		W(7)	O(24)	W(9)	127.0(7)

W(1)	O(25)	W(2)	89.2(4)		W(1)	O(25)	Ti(1)	89.5(4)

W(1)	O(25)	P(1)	125.3(6)		W(2)	O(25)	Ti(1)	89.5(4)

W(2)	O(25)	P(1)	127.4(7)		Ti(1)	O(25)	P(1)	124.4(6)

W(3)	O(26)	W(4)	88.9(4)		W(3)	O(26)	Ti(2)	89.8(4)

atom	atom	atom	angle		atom	atom	atom	angle

W(3)	O(26)	P(1)	126.6(7)		W(4)	O(26)	Ti(2)	90.3(4)

W(4)	O(26)	P(1)	126.4(7)		Ti(2)	O(26)	P(1)	123.6(7)

W(5)	O(27)	W(6)	88.3(4)		W(5)	O(27)	Ti(3)	89.3(4)

W(5)	O(27)	P(1)	125.9(7)		W(6)	O(27)	Ti(3)	90.5(4)

W(6)	O(27)	P(1)	126.3(7)		Ti(3)	O(27)	P(1)	124.9(7)

W(7)	O(28)	W(8)	89.3(4)		W(7)	O(28)	W(9)	89.7(4)

W(7)	O(28)	P(1)	126.7(7)		W(8)	O(28)	W(9)	88.3(4)

W(8)	O(28)	P(1)	125.3(7)		W(9)	O(28)	P(1)	125.7(7)

Ti(1)	O(38)	Ti(4)	131.0(8)		Ti(2)	O(39)	Ti(5)	131.3(7)

Ti(3)	O(40)	Ti(6)	130.1(7)		Ti(4)	O(41)	Ti(5)	145.9(8)

Ti(5)	O(42)	Ti(6)	147.4(8)		Ti(4)	O(43)	Ti(6)	144.5(8)

W(10)	O(44)	Ti(4)	123.0(7)		W(11)	O(45)	Ti(5)	123.4(7)

W(12)	O(46)	Ti(5)	124.1(7)		W(13)	O(47)	Ti(6)	122.2(6)

W(14)	O(48)	Ti(6)	122.1(7)		W(15)	O(49)	Ti(4)	122.8(7)

W(10)	O(50)	W(15)	122.8(7)		W(10)	O(51)	W(11)	157.0(7)

W(11)	O(52)	W(12)	122.3(7)		W(12)	O(53)	W(13)	154.3(8)

W(13)	O(54)	W(14)	124.0(8)		W(14)	O(55)	W(15)	152.9(7)

atom	atom	atom	angle		atom	atom	atom	angle

W(10)	O(56)	W(16)	151.0(8)		W(11)	O(57)	W(16)	152.0(7)

W(12)	O(58)	W(17)	150.2(7)		W(13)	O(59)	W(17)	150.5(8)

W(14)	O(60)	W(18)	152.8(7)		W(15)	O(61)	W(18)	151.9(8)

W(16)	O(62)	W(18)	127.0(8)		W(16)	O(63)	W(17)	127.4(7)

W(17)	O(64)	W(18)	126.3(8)		W(10)	O(65)	W(15)	88.7(4)

W(10)	O(65)	Ti(4)	89.1(4)		W(10)	O(65)	P(2)	128.2(7)

W(15)	O(65)	Ti(4)	88.5(4)		W(15)	O(65)	P(2)	126.1(7)

Ti(4)	O(65)	P(2)	124.1(7)		W(11)	O(66)	W(12)	88.1(4)

W(11)	O(66)	Ti(5)	89.2(4)		W(11)	O(66)	P(2)	126.6(7)

W(12)	O(66)	Ti(5)	89.0(4)		W(12)	O(66)	P(2)	126.7(7)

Ti(5)	O(66)	P(2)	125.2(7)		W(13)	O(67)	W(14)	88.1(4)

W(13)	O(67)	Ti(6)	89.4(4)		W(13)	O(67)	P(2)	126.4(7)

W(14)	O(67)	Ti(6)	89.6(4)		W(14)	O(67)	P(2)	126.0(7)

Ti(6)	O(67)	P(2)	125.4(7)		W(16)	O(68)	W(17)	89.2(4)

W(16)	O(68)	W(18)	89.0(4)		W(16)	O(68)	P(2)	125.7(7)

W(17)	O(68)	W(18)	88.7(4)		W(17)	O(68)	P(2)	126.8(7)

W(18)	O(68)	P(2)	125.4(7)