Version: 30.07.2001

Porous poly(d,l-lactide) and poly(d,l-lactide-co-glycolide) produced by thermal salt elimination from halogenocarboxylates

Michael Siedler[a], Simon J. Kitchin[b], Kenneth D.M. Harris,[b]

Ana L. C. Lagoa,[c] Hermínio P. Diogo,[c] Manuel E.

Minas da Piedade,[c] and Matthias Epple[a],*

Supporting Information

# Combustion calorimetry

Detailed results of the combustion calorimetric experiments are shown in Tables A and B, where m(PLLA) and m(PDLLA) are the masses of poly(l-lactide) and poly(d,l-lactide), respectively; m(aux) is the mass of n-hexadecane used as combustion auxiliary; n(HNO3) is the amount of substance of nitric acid formed in the bomb process; ei and ef are the energy equivalents of the bomb contents in the initial and final states of the bomb process, respectively; Ti and Tf represent the initial and final temperatures of the experiment; DTc is the contribution to the observed temperature rise of the calorimeter due to the heat exchanged with the surroundings and the heat dissipated by the temperature sensor; DUign is the electrical energy supplied for ignition of the sample; DUIBP is the internal energy change associated with the bomb process under isothermal conditions, at 298.15 K; DU represents the sum of all corrections necessary to reduce UIBP to the standard state (Washburn corrections); DU(HNO3) is the energy change associated with the formation of nitric acid; DU(aux), DU(PLLA), and DU(PDLLA) are the contributions of n-hexadecane, poly(l-lactide) and poly(d,l-lactide), respectively, to the energy of the isothermal bomb process; and, finally, Δcuo(PLLA) and Δcuo(PDLLA) are the standard massic energies of combustion of poly(l-lactide) and poly(d,l-lactide), respectively.

The molar masses used in the calculation of molar quantities are based on the 1995 standard atomic masses.[1] The values of Ti, Tf , and DTc were calculated by using a computer program based on the Regnault-Pfaundler method,[2] and UIBP was derived from:[3]

UIBP=eo(Ti  Tf + DTc) + ei(Ti  298.15) +

ef(298.15  Tf + DTc) + DUign				(1)

The energy equivalent of the calorimeter and its standard deviation, eo=(1813.16±0.38) JK-1, was determined from the combustion of benzoic acid (B.D.H. thermochemical standard), whose energy of combustion under certificate conditions and standard deviation were (26433±2) Jg-1. The standard state corrections, DU, were derived as recommended in the literature,[3] by using the following massic heat capacity (cpo), density (r) and ∂u/∂pT data, at 298.15 K: for n-hexadecane cpo=2.215 JK-1g-1,[4] r=0.773 gcm-3,[5] and −∂u/∂pT= 0.347 JMPa-1g-1;[5] for PLLA: cpo=1.25 JK-1g-1 (estimated by a modified Kopp’s rule),[6] r=1.21 gcm-3 (obtained in this work by weighing several pellets of know dimensions), and −∂u/∂pT= 0.12 JMPa-1g-1;[7] for PDLLA: cpo=1.25 JK-1g-1 (estimated by a modified Kopp’s rule),[6] r=1.16 gcm-3 (obtained in this work by weighing several pellets of know dimensions), and −∂u/∂pT= 0.12 JMPa-1g-1.[7]

The value of DU(HNO3), corresponds to the process:

1/2H2O(l) + 1/2N2(g) + 5/4O2(g)  HNO3(aq, 0.1 mol.dm-3)	(2)

and was obtained from ΔfUmo(HNO3, aq, 0.1 mol.dm-3)=59.7 kJmol-1.[8] The calculation of DU(aux) was based on Δcuo(aux)=(47131.021.47) Jg-1.[2]

The standard massic energies of combustion of PLLA and PDLLA in Tables A and B refer to the reaction in equation 3

1/n(C3H4O2)n (cr) + 3O2 (g)  3CO2 (g) + 2H2O (l)		(3)

and were calculated from:

Δcuo(C3H4O2)=[UIBP + U  DU(HNO3)  DU(aux)]/m(C3H4O2)		(4)

References for supporting information

- IUPAC, J. Phys. Chem. Ref. Data 1997, 26, 1239–1253.

- H. P. Diogo, and M. E. Minas da Piedade, J. Chem. Thermodynamics 1995, 27, 197206.

- W. N. Hubbard, D. W. Scott, and G. Waddington, In Experimental Thermochemistry; Rossini, F. D., Ed.; Interscience: New York, 1956; Vol. 1, Chapter 5.

- Handbook of Chemistry and Physics, 74th ed.; Lide, D. R., Ed.; CRC Press: Boca Raton, 1993-94.

- N. B. Vargaftik, Tables on the Thermophysical Properties of Liquids and Gases, 2nd. ed.; John Wiley: New York, 1975.

- J. E. Hurst, Jr., and B. K. Harrison, Chem. Eng. Comm. 1992, 112, 2130.

- Assumed identical to the ∂u/∂pT value given for benzoic acid in W. H. Johnson, and E. J. Prosen, J. Res. Natl. Bur. Stand. (U. S.) 1975, 79A, 481486.

- D. D. Wagman, W. H. Evans, V. B. Parker, R. H. Schumm, I. Halow, S. M. Bailey, K. L. Churney, and R. L. Nuttall, The NBS Tables of Chemical Thermodynamics Properties, J. Phys Chem. Ref. Data 1982, 11; Supplement no. 2

- Table A. Results of the combustion experiments on PLLA

| m(PLLA)/mg | 44.6349 | 36.3884 | 45.4541 | 34.7062 | 30.1035 | 41.5620 |
| --- | --- | --- | --- | --- | --- | --- |
| m(aux)/mg | 5.0897 | 3.8999 | 3.1743 | 3.9704 | 3.6871 | 4.8849 |
| n(HNO3)105/mol | 2.16 | 1.61 | 1.79 | 1.99 | 1.24 | 2.41 |
| ei/Jmol-1K-1 | 1.213 | 1.200 | 1.210 | 1.198 | 1.192 | 1.209 |
| ef/Jmol-1K-1 | 1.282 | 1.256 | 1.274 | 1.252 | 1.239 | 1.273 |
| Ti/K | 298.16791 | 298.19262 | 298.11893 | 298.14479 | 298.12592 | 298.13499 |
| Tf/K | 298.82888 | 298.74679 | 298.74976 | 298.69851 | 298.63487 | 298.76153 |
| DTc/K | 0.06553 | 0.07499 | 0.07469 | 0.08933 | 0.10075 | 0.06775 |
| DTad/K | 0.59544 | 0.47917 | 0.55614 | 0.46439 | 0.40820 | 0.55880 |
| DUIBP/J | -1080.39 | -869.42 | -1009.07 | -842.59 | -740.63 | -1013.90 |
| DUign/J | 1.76 | 1.76 | 1.76 | 1.76 | 1.76 | 1.76 |
| DU(HNO3)/J | 1.29 | 0.96 | 1.07 | 1.19 | 0.74 | 1.44 |
| DU/J | 0.75 | 0.60 | 0.74 | 0.57 | 0.49 | 0.70 |
| DU(aux)/J | -239.88 | -183.81 | -149.61 | -187.13 | -173.78 | -230.23 |
| DU(PLLA)/J | -836.71 | -682.29 | -855.89 | -651.94 | -563.86 | -779.77 |
| Δcuo(PLLA)/Jg-1 | -18745.64 | -18750.21 | -18830.18 | -18784.54 | -18730.71 | -18761.61 |

Table B. Results of the combustion experiments on PDLLA

| m(PDLLA)/mg | 17.8563 | 19.4757 | 19.1329 | 20.6904 | 14.2466 | 19.8964 |
| --- | --- | --- | --- | --- | --- | --- |
| m(aux)/mg | 3.1384 | 3.1913 | 3.3534 | 3.7724 | 3.3345 | 4.4690 |
| n(HNO3)105/mol | 6.77 | 7.58 | 7.53 | 7.64 | 5.85 | 9.44 |
| ei/Jmol-1K-1 | 1.174 | 1.177 | 1.172 | 1.180 | 1.170 | 1.180 |
| ef/Jmol-1K-1 | 1.206 | 1.210 | 1.205 | 1.217 | 1.198 | 1.218 |
| Ti/K | 298.17803 | 298.14745 | 298.14677 | 298.17286 | 298.14255 | 298.28143 |
| Tf/K | 298.55845 | 298.54941 | 298.54880 | 298.59376 | 298.50217 | 298.69079 |
| DTc/K | 0.26957 | 0.11515 | 0.11370 | 0.10493 | 0.12309 | 0.08513 |
| DTad/K | 0.11085 | 0.28681 | 0.28832 | 0.31597 | 0.23653 | 0.32423 |
| DUIBP/J | -489.10 | -520.39 | -523.13 | -573.29 | -429.15 | -588.29 |
| DUign/J | 1.76 | 1.76 | 1.76 | 1.76 | 1.76 | 1.76 |
| DU(HNO3)/J | 0.40 | 0.45 | 0.45 | 0.46 | 0.35 | 0.56 |
| DU/J | 0.29 | 0.32 | 0.31 | 0.34 | 0.24 | 0.34 |
| DU(aux)/J | -147.91 | -150.41 | -158.05 | -177.80 | -157.16 | -210.63 |
| DU(PDLLA)/J | -338.74 | -367.45 | -362.56 | -392.93 | -269.64 | -375.00 |
| Δcuo(PLLA)/Jg-1 | -18970.33 | -18867.10 | -18949.56 | -18990.93 | -18926.62 | -18847.63 |