An Investigation of the Reaction of [RGa(3-Te)]4 with O2, SO2 and SeO2 Using a Combination of Experiment and Density Functional Theory

Bradley D. Fahlman,† Andrew Daniels, Gustavo Scusceria* and Andrew R. Barron*

Supplementary Materials

Table 3. Comparison of various DFT methods for [(Me)Ga(3-O)]4.

B3LYP/6-31G**	B3LYP/Stutt.	LSDA/Stutt.	B3LYP/LANL2DZ	Experiment

Ga-O (Å)	1.931	1.990	2.000	1.932	1.922a

Ga-C (Å) 	1.952	1.961	1.962	1.941	1.97 - 2.0b,c

Ga-O-Ga (°)	91.6	92.99	93.7	94.4	90.0a

O-Ga-O (°)	88.5	87.0	86.1	85.4	89.7a

a N. Wiberg, K. Amelunxen, H. -W. Lerner, H. Noth, W. Ponikwar, and H. Schwenk, J. Organomet. Chem., 1999, 574, 246.

b A. Keys, S. G. Bott, and A. R. Barron, Polyhedron, 1998, 17, 3121.

c A. Keys, T. Barbarich, S. G. Bott, and A. R. Barron, J. Chem. Soc., Dalton Trans., 2000, 577.

Table 4. Comparison of the structural parameters for the calculated [MeGa(3-O)]6 and empirical [(tBu)M(3-E)]6 structures.a

Compound	M-E	M-E-M	E-M-E

(Å)	(°)	(°)

[(Me)Ga(3-O)]6	1.92, 2.02	129.4, 94.9	110.3, 81.4

[(tBu)Al(3-O)]6	1.78, 1.91	127.6, 91.8	113.2, 87.9

[(tBu)Ga(3-S)]6	2.32, 2.39	117.5, 82.5	119.7, 97.4

a M. R. Mason, J. M. Smith, S. G. Bott, and, A. R. Barron, J. Am. Chem. Soc., 1993, 115, 4971; M. B. Power, J. W. Ziller, and A. R. Barron, Organometallics, 1992, 11, 2783.