Supporting Materials:

Palladium(II) salts containing [PdCl4]2- and [Pd2Cl6]2- ions as pre-catalysts for the vinyl-polymerization of norbornene — evidence for the in-situ formation of PdCl2 as the active species

Paul-Gerhard Lassahn, Vasile Lozan and Christoph Janiak*

Institut für Anorganische und Analytische Chemie, Universität Freiburg, Albertstr. 21, 79104 Freiburg, Germany. Fax: (int.) +49(0)761-2036147; E-mail: janiak@uni-freiburg.de

Table 1. 1H NMR data of pre-catalyst 2C and the ligands 6 and 7 in combination with different amounts of B(C6F5)3 (measured at room temperature)

| compound (molar ratio) | 1H NMR |
| --- | --- |
|  | [ppm (JPH Hz)] |
| 6 [a] | 2.41 (s, CH3 6a+6b), 4.50 (d, 19.4, CH 6b), 6.10 (d, 11.6, CH2 6a), 7.2-8.0 (m, Haromatic 6a+6b), 13.24 (s, OH 6b) |
| 6/B(C6F5)3 (1:1) [a] | 2.25 (d, 2.2, CH3 8), 4.50 (d, 12.2, CH2 8), 7.3-7.9 (m, Haromatic 8) |
| 6/B(C6F5)3 (1:1.5) [a] | 2.25 (d, 2.0, CH3 8), 4.41 (d, 12.2, CH2 8), 7.3-7.9 (m, Haromatic 8) |
| 6/B(C6F5)3 (1:2) [a] | 2.26 (d, 2.2, CH3 8), 4.42 (d, 12.2, CH2 8), 7.3-7.9 (m, Haromatic 8) |
| 6/B(C6F5)3 (1:3) [a] | 2.27 (d, 2.0, CH3 8), 4.41 (d, 12.2, CH2 8), 7.3-7.9 (m, Haromatic 8) |
| 6/B(C6F5)3 (1:5) [a] | 2.27 (d, 2.2, CH3 8), 4.40 (d, 12.0, CH2 8), 7.3-7.9 (m Haromatic 8) |
| 6/B(C6F5)3 (1:9) [a] | 2.28 (d, 2.0, CH3 8), 4.38 (d, 12.2, CH2 8), 7.3-7.9 (m, Haromatic 8) |
| 7 [a] | 1.92 (d, 1.8, CH3), 3.56 (d, br, 12.7, CH), 7.2-7.7 (m) |
| 7/B(C6F5)3 (1:1) [a] | 1.55 (s, CH3 9a), 1.79 (s, CH3 9b), 2.28 (d, 2.2, CH3 9c), 4.14 (d, 14.2, CH 9c), 4.28 (d, 12.2, CH 9a), 4.36 (d, 18.0, CH 9b), 7.1-7.9 (m, Haromatic 9a-c) |
| 7/B(C6F5)3 (1:9) [a] | 2.20 (d, 1.4, CH3 9c), 4.20 (d, 12.4, CH 9c), 7.2-7.9 (m, Haromatic 9c) |
| 2C [b] | 2.14 (d, 2.2, CH3), 5.32 (d, 12.6, CH2), 7.3-7.8 (m) |
| 2C/B(C6F5)3 (1:9) [a],[c] | 2.30 (d, 2.0, CH3 8), 4.32 (d, 12.2, CH2 8), 7.4-7.9 (m, Haromatic 8) |
| 2C/B(C6F5)3 (1:9) [b],[d] | n.s. |
| n.s. = no signals; [a] solvent: CD2Cl2; [b] solvent: [D6]DMSO; [c] soluble part in CD2Cl2; [d] insoluble in CD2Cl2, dissolved in [D6]DMSO |

Table 2. 31P NMR and 19F NMR data of pre-catalyst 2C and the ligands 6 and 7 in combination with different amounts of B(C6F5)3 (measured at room temperature)

| compound (molar ratio) | 31P NMR | 19F NMR [ppm (JFF Hz)] |
| --- | --- | --- |
|  | [ppm] | o-F | p-F | m-F |
| B(C6F5)3 [a] | n.s. | -130.24 (s, br) | -146.85 (s, br) | -161.94 (tdd, 20.7, 7.5, 2.8) |
| 6 [a] | 13.2 (6b), 19.6 (6a) | n.s. | n.s. | n.s. |
| 6/B(C6F5)3 [a] (1:1) | 19.5 (8) | -133.07 (dd, 23.5, 7.7) -135.97 (d, br, 22.4, 10) | -162.44 (t, 20.5) -160.37 (t, 19.9, 10) | -167.36 (m) -166.02 (td, br, 22.1, 7.0, 10) |
| 6/B(C6F5)3 [a] (1:1.5) | 19.5 (8) | -132.32 (d, 16.9) -133.84 (s, br, 10) | -158.65 (s, br) -160.23 (t, 20.1, 10) | -166.16 (s, br) -166.28 (t, 19.9, 10) |
| 6/B(C6F5)3 [a] (1:2) | 19.5 (8) | -131.23 (s, br) -133.93 (s, br, 10) | -154.07 (s, br) -160.14 (t, 20.2, 10) | -164.61 (s, br) -166.22 (t, 18.7, 10) |
| 6/B(C6F5)3 [a] (1:3) | 19.5 (8) | -130.46 (s, br) -133.94 (s, br, 10) | -150.63 (s, br) -160.17 (t, 20.2, 10) | -163.54 (s, br) -166.25 (t, 18.8, 10) |
| 6/B(C6F5)3 [a] (1:5) | 19.5 (8) | -129.84 (s, br) -133.95 (s, br, 10) | -148.39 (br) -160.20 (t, 20.2, 10) | -162.81 (s, br) -166.27 (t, 18.9, 10) |
| 6/B(C6F5)3 [a] (1:9) | 19.5 (8) | -129.62 (s, br) -133.93 (s, br, 10) | -147.31 (s, br) -160.21 (t, 20.3, 10) | -162.42 (s, br) -166.27 (t, 19.1, 10) |
| 7 [a] | 14.3 | n.s. | n.s. | n.s. |
| 7/B(C6F5)3 [a] (1:1) | 12.5 (9b), 15.6 (9a), 19.4 (9c) | -134.36 (s, br, 9b) -134.56 (m, br, 9a) -133.95 (s, br, 9c) | -161.42 (t, 19.0, 9b) -161.38 (t, 20.1, 9a) -160.13 (t, 20.2, 9c) | -166.73 (t, 21.6, 9b) -166.70(t, 21.3, 9a) -166.21 (t, 18.8, 9c) |
| 7/B(C6F5)3 [a] (1:9) | 19.4 (9c) | -131.82 (s, br) -134.96 (s, br, 9c) | -149.70 (s, br) -160.21 (t, 20.2, 9c) | -162.68 (m) -166.28 (t, 19.0, 9c) |
| 2C [b] | 19.5 | n.s. | n.s. | n.s. |
| 2C/B(C6F5)3 [a],[c] (1:9) | 19.4 (8) | -129.60 (s, br) -133.93 (s, br, 8) | -146.12 (s, br) -160.22 (t, 20.2, 8) | -161.90 -166.27 (t, 19.7, 8) |
| 2C/B(C6F5)3 [b],[d] (1:9) | n.s. | n.s. | n.s. | n.s. |
| Et4NCl/B(C6F5)3 [a] (1:9) | n.s. | -133.23 (dd, 23.3, 7.7) -135.85 (d, br, 20.9, 10) | -162.54 (t, 20.3) -160.62 (t, 20.2, 10) | -167.52 (m) -166.27 (td, 21.8, 6.7, 10) |
| Et4NCl/B(C6F5)3 [a] (1:9) | n.s. | -129.47 (s, br) -133.95 (s, br, 10) | -146.30 (s, br) -160.24 (t, 20.2, 10) | -162.03 (s, br) -166.31 (t, 18.7, 10) |
| n.s. = no signals; [a] solvent: CD2Cl2; [b] solvent: [D6]DMSO; [c] soluble part in CD2Cl2; [d] insoluble in CD2Cl2, dissolved in [D6]DMSO |

Table 3. 13C-NMR data of the compounds 6 and 7 in combination with different amounts of B(C6F5)3 (measured at room temperature)

| compound [a] (molar ratio) | 13C-NMR [ppm (JPC respectively JCF Hz)] |
| --- | --- |
| B(C6F5)3 [a] | 112.05 (ipso-C), 136.46 (dm, 249.5, m-C), 143.61 (dm, 260.7, p-C), 147.18 (dm, 249.9, o-C) |
| 6 [b] | 23.34 (d, 12.8, CH3 6b), 31.81 (d, 6.8, CH3 6a), 40.07 (d, 58.4, CH2 6a), 69.78 (d, 99.78, CH 6b), 118.69 (d, 89.0 Hz, ipso-C 6a), 121.63 (d, 92.2, ipso-C 6b), 129.43 (d, 12.6, m-C 6b), 129.68 (d, 12.8, m-C 6a), 133.95 (d, 10.6, o-C 6a), 133.68 (d, 10.7, o-C 6b), 133.64 (d, 3.0, p-C 6b), 134.33 (d, 3.0, p-C 6a), 181.14 (s, C(OH) 6b), 200.69 (d, 7.0, C(O) 6a) |
| 6/B(C6F5)3 [a] (1:1) | 31.09 (d, 5.9, CH3 8), 38.99 (d, 58.9, CH2 8), 116.65 (d, 89.3, ipso-C 8), 122.63 (m, br, ipso-C B), 129.71 (d, 13.2, m-C 8), 132.71 (d, 10.8, o-C 8), 134.76 (d, 3.0, p-C 8), 135.75 (dm, 243.1, m-C B), 138.11 (dm, 246.6, p-C B), 147.26 (dm, 246.6, o-C B), 197.5 (d, 7.0, C(O) 8) |
| 6/B(C6F5)3 [a] (1:2) | 31.16 (d, 5.8, CH3 8), 39.05 (d, 58.9, CH2 8), 116.54 (d, 89.3, ipso-C 8), 122.04 (m, br, ipso-C B), 129.79 (d, 13.1, m-C 8), 132.70 (d, 10.7, o-C 8), 134.88 (d, 3.1, p-C 8), 136.32 (dm, 244.9, m-C B), 138.69 (dm, 245.4, p-C B), 147.42 (dm, 241.2, o-C B), 197.38 (d, 6.3, C(O) 8) |
| 6/B(C6F5)3 [c] (1:9) | 31.30 (d, 5.8, CH3 8), 39.20 (d, 58.8, CH2 8), 113.06 (m, br, ipso-C, B), 116.36 (d, 89.4, ipso-C 8), 129.93 (d, 13.2, m-C 8), 132.69 (d, 10.7, o-C 8), 135.09 (d, 3.0, p-C 8), 136.81 (dm, 255.5, m-C B), 143.72 (dm, 255.6, p-C B), 147.56 (dm, 250.4, o-C B), 197.0 (s, C(O) 8) |
| 7 [b] | 26.77 (d, 16.0, CH3 7), 49.29 (d, 108.1, CH 7), 126.28 (d, 90.4, ipso-C 7), 127.44 (d, 12.2, m-C 7), 130.67 (d, 2.9, p-C 7), 131.77 (d, 10.2, o-C 7), 188.96 (d, 2.2, C(O) 7) |
| 7/B(C6F5)3 [a] (1:1) | 23.62 (d, 14.2, CH3 9b), 24.22 (d, 2.6, CH3 9a), 31.25 (d, 6.0, CH3 9c), 39.16 (d, 59.2, CH 9c), 68.46 (s, CH 9b), 70.49 (s, CH 9a), 116.28 (d, 89.3, ipso-C 9c), 121.44 (d, 91.5, ipso-C 9a), 121.75 (d, 92.2, ipso-C 9b), 128.43 (d, 12.8, m-C 9b), 129.22 (d, 12.8, m-C 9a), 129.92 (d, 13.2, m-C 9c), 132.02 (d, 10.4, o-C 9a), 132.54 (d, 10.4, o-C 9b), 132.65 (d, 10.0, o-C 9c), 133.38 (d, 2.9, p-C 9a), 135.10 (d, 3.0, p-C 9c), 135.86 (dm, 251.6, m-C B), 138.41 (dm, 247.2, p-C B), 146.97 (dm, 247.2, o-C B), 179.76 (d, 13.6, C(O) 9a), 182.35 (d, 1.9, C(O) 9b), 196.95 (s, weak, C(O) 9c), p-C of 9b overlayed by the signal group between 132.3-132.9 ppm |
| 7/B(C6F5)3 [c] (1:9) | 31.54 (d, 5.6, CH3 9c), 39.45 (d, 58.6, CH 9c), 113.99 (m, br, ipso-C B), 116.48 (d, 89.3, ipso-C 9c), 130.18 (d, 13.3, m-C 9c), 132.88 (d, 10.8, o-C 9c), 135.37 (d, 3.2, p-C 9c), 136.95 (dm, 255.3, m-C B), 142.87 (dm, 264.4, p-C B), 147.63 (dm, 244.1, o-C B), 197.23 (s, C(O) 9c) |
| B = B(C6F5)3; [a] 0.07 mmol B(C6F5)3 dissolved in 0.6 mL CD2Cl2; [b] 0.07 mmol compound dissolved in 0.6 mL CD2Cl2; [c] 0.007 mmol compound and 0.063 mmol B(C6F5)3 dissolved in 0.6 mL CD2Cl2; |

Table 4. IR data of the compounds 6 and 7 in combination with different amounts of B(C6F5)3 (measured in CD2Cl2 at room temperature)

| comp.[a] | molar ratio | IR [b] |
| --- | --- | --- |
|  | Pd/lig:B | [cm-1] |
| CD2Cl2 | 1:-- | 1751 |
| B(C6F5)3 | --:1 | 1751, 1647, 1522 |
| 6 | 1:-- | 1751, 1718, 1608 |
| 6 | 1:1 | 1751, 1725, 1644, 1589, 1516 |
| 6 [c] | 1:9 | 1751, 1727, 1647, 1520 |
| 7 | 1:-- | 1751, 1536 |
| 7 | 1:1 | 1751, 1727, 1644, 1553, 1515 |
| 7 [c] | 1:9 | 1751, 1727, 1648, 1520 |
| comp. = compound; lig = ligand; B = B(C6F5)3; [a] 0.07 mmol compound dissolved in 0.6 mL CD2Cl2; [b] IR signals between 1800 cm-1 and 1500 cm-1; [c] 0.007 mmol compound and 0.063 mmol B(C6F5)3 dissolved in 0.6 mL CD2Cl2; |