Supplementary Information for manuscript # B300698K.

Silsesquioxane-Bonded Zirconocene Complexes; Soluble Models for Silica-Tethered Olefin Polymerization Catalysts.

John R. Severn, Robbert Duchateau, Rutger A. van Santen,

Dianne D. Ellis, Anthony L. Spek and Glenn P.A. Yap

Contents:

Page 2:	Table S1. 1H, 13C{1H} and 29Si{1H} NMR Data of Silsesquioxane Compounds

(1-5a/b = CDCl3, 6-9 = C6D6).

Page 6: 	Table S2. Crystal data for 1, 5b, and 6b.

Page 7. 	Experimental Section for compounds 4, 5b and 6b and crystals structure analysis of 1, 5b and 6b.

Table S1. 1H, 13C{1H} and 29Si{1H} NMR Data of Silsesquioxane Compounds (1-5a/b = CDCl3, 6-9 = C6D6).

| # Complex | 1H | assignment | 13C{1H} | assignment | 29Si{1H} | assignment |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 7.86 (d, 2H) 7.70 (d, 2H) 7.37 (t, 2H) 7.34 (t, 2H) 3.90 (s, 1H) | Flu-CH (3JH-H = 8 Hz) Flu-CH (3JH-H = 8 Hz) Flu-CH (3JH-H = 8 Hz) Flu-CH (3JH-H = 8 Hz) Flu-CH-9 | 143.44 141.20 126.20 125.72 125.01 119.64 38.31 | Flu-C-ipso Flu-C-ipso Flu-CH Flu-CH Flu-CH Flu-CH Flu-C-9 | -67.16 (3) -67.99 (1) -68.34 (3) -71.63 (1) | (O)3SiC6H11 (O)3SiC6H11 (O)3SiC6H11 (O)3SiFlu |
| 2 | 7.78 (d, 2H) 7.73 (d, 2H) 7.39 (t, 2H) 7.32 (t, 2H) 4.13 (t, 1H) 1.24 (d, 2H) | Flu-CH (3JH-H = 7 Hz) Flu-CH (3JH-H = 8 Hz) Flu-CH (3JH-H = 7 Hz) Flu-CH (3JH-H = 8 Hz) Flu-CH-9 (3JH-H = 7 Hz) (O)3SiCH2Flu (3JH-H = 7 Hz) | 149.62 140.80 127.34 127.05 124.70 119.65 42.72 17.56 | Flu-C-ipso Flu-C-ipso Flu-CH Flu-CH Flu-CH Flu-CH Flu-C-9 (O)3SiCH2Flu | -65.73 (1) -65.77 (3) -65.82 (3) -70.17 (1) | (O)3SiC5H9 (O)3SiC5H9 (O)3SiC5H9 (O)3SiCH2Flu |
| 3 | 7.75 (d, 2H) 7.53 (d, 2H) 7.38 (t, 2H) 7.31 (t, 2H) 3.98 (t, 1H) 2.05 (m, 2H) 0.66 (m, 2H) | Flu-CH (3JH-H = 9 Hz) Flu-CH (3JH-H = 9 Hz) Flu-CH (3JH-H = 9 Hz) Flu-CH (3JH-H = 9 Hz) Flu-CH-9 (3JH-H = 8 Hz) (O)3SiCH2CH2CH2Flu (O)3SiCH2CH2CH2Flu | 147.79 141.28 127.46 126.98 124.81 119.99 47.55 36.77 26.46 10.83 | Flu-C-ipso Flu-C-ipso Flu-CH Flu-CH Flu-CH Flu-CH Flu-C-9 (O)3SiCH2CH2CH2Flu (O)3SiCH2CH2CH2Flu (O)3SiCH2CH2CH2Flu | -65.34 (3) -66.15 (3) -66.52 (1) -67.19 (1) | (O)3SiC5H9 (O)3SiC5H9 (O)3SiC5H9 (O)3SiCH2CH2CH2Flu |
| 4 | 7.75 (d, 2H) 7.63 (d, 2H) 7.29 (t, 2H) 7.27 (d. 2H) 7.21 (t, 2H) 7.15 (t, 2H) 4.25 (t, 1H) 3.09 (t, 2H) | aromatic-CH (3JH-H = 9 Hz) aromatic-CH (3JH-H = 8 Hz) aromatic-CH (3JH-H = 9 Hz) aromatic-CH (3JH-H = 9 Hz) aromatic-CH (3JH-H = 8 Hz) aromatic-CH (3JH-H = 9 Hz) Flu-CH-9 (3JH-H = 8 Hz) (O)3SiC6H4CH2Flu (3JH-H = 9 Hz) | 146.81 142.04 140.76 134.07 129.96 128.86 127.11 126.64 124.84 119.78 48.57 40.32 | aromatic-C-ipso aromatic-C-ipso aromatic-C-ipso aromatic-CH aromatic-C-ipso aromatic-CH aromatic-CH aromatic-CH aromatic-CH aromatic-CH Flu-C-9 (O)3SiC6H4CH2Flu | -66.45 (3) -65.91 (1) -65.63 (3) -81.72 (1) | (O)3SiC5H9 (O)3SiC5H9 (O)3SiC5H9 (O)3SiC6H4CH2Flu |

Table S1. continued.

| 5a | 7.76 (d, 2H) 7.45 (d, 2H) 7.27 (t, 2H) 7.25 (t, 2H) 1.76 (s, 2H) -0.28 (s, 9H) | Flu-CH (3JH-H = 8 Hz) Flu-CH (3JH-H = 8 Hz) Flu-CH (3JH-H = 8 Hz) Flu-CH (3JH-H = 8 Hz) (O)3SiCH2-Flu Flu-Si(CH3)3 | 149.16 139.67 125.51 124.82 123.53 119.24 44.09 13.88 -4.38 | Flu-C-ipso Flu-C-ipso Flu-CH Flu-CH Flu-CH Flu-CH Flu-C-9 (O)3SiCH2-Flu Flu-Si{CH3}3 | -5.89 (1) -65.76 (1) -65.80 (3) -65.87 (3) -70.15 (1) | Flu-SiMe3 (O)3Si-C5H9 (O)3Si-C5H9 (O)3Si-C5H9 (O)3Si-CH2Flu |
| --- | --- | --- | --- | --- | --- | --- |
| 5b | 7.83 (d, 2H) 7.29 (d, 2H) 7.25 (t, 2H) 7.23 (t, 2H) 2.02 (s, 2H) -0.22 (s, 9H) | Flu-CH (3JH-H = 8 Hz) Flu-CH (3JH-H = 8.Hz) Flu-CH (3JH-H = 8 Hz) Flu-CH (3JH-H = 8 Hz) (O)3SiCH2Flu Flu-Sn(CH3)3 | 149.52 136.74 125.44 123.44 121.18 119.45 45.84 14.72 -10.09 | Flu-C-ipso Flu-C-ipso Flu-CH Flu-CH Flu-CH Flu-CH Flu-C-9 CH2-Flu Flu-Sn{CH3}3 | -65.75 (1) -65.82 (3) -65.91 (3) -70.14 (1) | (O)3Si-C5H9 (O)3Si-C5H9 (O)3Si-C5H9 (O)3Si-CH2Flu |
| 6a | 7.93 (d, 2H) 7.62 (d, 2H) 7.04 (t, 2H) 6.99 (t, 2H) 3.47 (s, 2H) 1.55 (s, 45H) | Flu-CH (3JH-H = 11 Hz) Flu-CH (3JH-H = 10 Hz) Flu-CH (3JH-H = 11 Hz) Flu-CH (3JH-H = 10 Hz) (O)3SiCH2Flu C5(CH3)5 | 132.46 129.13 127.64 126.26 125.85 123.42 123.19 114.32 12.20 11.58 | Flu-C-ipso Flu-C-ipso C5{CH3}5 Flu-CH Flu-CH Flu-CH Flu-CH Flu-C-9 (O)3SiCH2Flu C5{CH3}5 | -66.70 (1) -66.94 (3) -67.13 (3) -70.42 (1) | (O)3SiC5H9 (O)3SiC5H9 (O)3SiC5H9 (O)3SiCH2Flu |
| 6b | 7.67 (d, 2H) 7.65 (d, 2H) 7.11 (t, 2H) 6.93 (t, 2H) 6.50 (t, 1H) 5.43 (d, 2H) 3.10 (s, 2H) 0.20 (s, 18H) | Flu-CH (3JH-H = 9 Hz) Flu-CH (3JH-H = 9 Hz) Flu-CH (3JH-H = 10Hz) Flu-CH (3JH-H = 10Hz) C5H3(SiMe3)2 (4JH-H = 2 Hz) C5H3(SiMe3)2 (4JH-H = 2 Hz) (O)3SiCH2-Flu C5H3(Si(CH3)3) 2 | 139.50 131.09 128.84 127.95 127.30 125.64 125.39 123.83 123.32 117.7 13.92 0.73 | Ipso-C5H3{SiMe3}2 Flu-C-ipso Flu-C-ipso C5H3(SiMe3)2 Flu-CH Flu-CH Flu-CH Flu-CH C5H3(SiMe3)2 Flu-C-9 (O)3SiCH2-Flu C5H3(Si(CH3)3)2 | 10.01 (2) -66.76 (1) -66.92 (3) -67.30 (3) -70.62 (1) | C5H3(SiMe3)2 (O)3SiC5H9 (O)3SiC5H9 (O)3SiC5H9 (O)3SiCH2Flu |

Table S1. continued.

| 7 | 7.82 (d, 2H) 7.69 (d, 2H) 7.41 (t, 2H) 7.33 (t, 2H) 3.52 (t, 2H) 1.92 (m, 2H) 1.63 (s, 15H) 0.89 (m, 2H) | Flu-CH (3JH-H = 9 Hz) Flu-CH (3JH-H = 9 Hz) Flu-CH (3JH-H = 9 Hz) Flu-CH (3JH-H = 9 Hz) (O)3SiCH2CH2CH2Flu (O)3SiCH2CH2CH2Flu C5(CH3)5 (O)3SiCH2CH2CH2Flu | 146.52 140.78 127.01 126.97 125.03 124.81 124.06 110.83 37.49 26.86 12.73 9.91 | Flu-C-ipso Flu-C-ipso Flu-CH C5{CH3}5 Flu-CH Flu-CH Flu-CH Flu-C-9 (O)3SiCH2CH2CH2Flu (O)3SiCH2CH2CH2Flu C5{CH3}5 (O)3SiCH2CH2CH2Flu | -65.61 (1) -66.52 (3) -66.58 (3) -66.87 (1) | (O)3SiC5H9 (O)3SiC5H9 (O)3SiC5H9 (O)3SiCH2CH2CH2Flu |
| --- | --- | --- | --- | --- | --- | --- |
| 8 | 7.87 (d, 2H) 7.76 (d, 2H) 7.35 (t, 2H) 7.31 (d, 2H) 7.25 (t, 2H) 7.22 (d, 2H) 4.19 (s, 2H) 1.67 (s, 15 H) | aromatic-CH (3JH-H = 8 Hz) aromatic-CH (3JH-H = 8 Hz) aromatic-CH (3JH-H = 9 Hz) aromatic-CH (3JH-H = 9 Hz) aromatic-CH (3JH-H = 8 Hz) aromatic-CH (3JH-H = 9 Hz) (O)3SiC6H4CH2Flu C5(CH3)5 | 143.37 141.97 140.83 133.59 130.85 128.32 128.11 127.59 124.78 125.54 101.45 42.71 12.55 | aromatic-C-ipso aromatic-C-ipso aromatic-C-ipso aromatic-CH aromatic-C-ipso aromatic-CH aromatic-CH aromatic-CH C5{CH3}5 aromatic-CH Flu-C-9 (O)3SiC6H4CH2Flu C5{CH3}5 | -65.74 (3) -66.56 (1) -66.63 (3) -74.82 (1) | (O)3SiC5H9 (O)3SiC5H9 (O)3SiC5H9 (O)3SiC6H4CH2Flu |
| 9 | 7.63 (d, 2H) 7.59 (d, 2H) 7.11 (t, 2H) 6.82 (t, 2H) 3.07 (s, 2H) | Flu-CH (3JH-H = 7 Hz) Flu-CH (3JH-H = 8 Hz) Flu-CH (3JH-H = 7 Hz) Flu-CH (3JH-H = 8 Hz) (O)3SiCH2Flu (3JH-H = 7 Hz) | 134.23 127.42 125.67 125.55 123.91 116.67 96.71 13.92 | Flu-C-ipso Flu-C-ipso Flu-CH Flu-CH Flu-CH Flu-CH Flu-C-9 (O)3SiCH2Flu | -66.30 (1) -66.97 (3) -68.56 (3) -70.62 (1) | (O)3SiC5H9 (O)3SiC5H9 (O)3SiC5H9 (O)3SiCH2Flu |

Table S1. continued.

| 10 | 7.71 (d, 2H) 7.68 (d, 2H) 7.29 (d, 2H) 6.99 (t, 2H) 6.41 (t, 1H) 5.57 (d, 2H) 3.73 (q, 2H) 2.78 (s, 2H) 1.44 (t, 3H) 0.16 (s, 18H) -0.11 (s, 6H) | Flu-CH (3JH-H = 9 Hz) Flu-CH (3JH-H = 9 Hz) Flu-CH (3JH-H = 9 Hz) Flu-CH (3JH-H = 9 Hz) C5H3(SiMe3)2 (4JH-H = 2 Hz) C5H3(SiMe3)2 (4JH-H = 2 Hz) OCH2CH3 (3JH-H = 8 Hz) Flu-9-CH2Si OCH2CH3, 3JH-H = 8 Hz) C5H3(Si(CH3)3)2 Si(CH3)2OEt | 140.13 129.87 127.33 126.88 125.72 125.14 122.68 121.32 118.53 106.34 57.94 19.84 18.39 0.68 -0.93 | Flu-C-ipso Flu-C-ipso C5H3(SiMe3)2-C-ipso Flu-CH Flu-CH Flu-CH Flu-CH C5H3(SiMe3)2 C5H3(SiMe3)2 Flu-C-9 OCH2CH3 OCH2CH3 Flu-9-CH2Si C5H3(Si(CH3)3)2 Si(CH3)2OEt |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| 11 | 6.46 (s, 5H) 3.41 (q, 2H) 1.92 (s, 6H) 1.75 (s, 6H) 1.47 (t, 3H) 0.93 (s, 6H) | C5H5 OCH2CH3 (3JH-H = 8 Hz) C5(CH3)4 C5(CH3)4 OCH2CH3 (3JH-H = 8 Hz) Si(CH3)2OEt | 136.41 135.95 116.86 50.10 39.27 14.11 10.37 4.43 | C5Me4SiMe2OEt C5Me4SiMe2OEt C5H5 OCH2CH3 OCH2CH3 C5(CH3)4 C5(CH3)4 Si(CH3)2OEt |  |  |

Table S2. Crystal data for 1, 5b and 6b.

|  | 1 | 5b(C6H14)0.25 | 6b(CH2Cl2)2.5 |
| --- | --- | --- | --- |
| formula | C55H86O12Si8 | C53.5H85.5O12Si8Sn | C62.50H99Cl7O12Si10Zr |
| formula weight (gmol-1) | 1163.96 | 1264.15 | 1662.71 |
| temperature (K) | 203 | 150(2) | 150(2) |
|  (Å) | 0.71073 | 0.71073 | 0.71073 |
| crystal system, space group | Monoclinic P2 (1)/n | Monoclinic, Pc | Triclinic, P-1 |
| unit cell dimensions a (Å) | 10.489(1) | 10.9320(3) | 11.3551(4) |
| b (Å) | 30.222(3) | 17.9730(4) | 18.1661(7) |
| c (Å) | 19.520(2) | 32.0160(7) | 19.8473(8) |
|  (deg) |  |  | 86.0297(17) |
|  (deg) | 91.441(2) | 94.0678(8) | 83.156(2) |
|  (deg) |  |  | 77.2346(18) |
| V (Å3) | 6186(1) | 6274.7(3) | 3960.5(3) |
| Z, Dcalcd (gcm-3) | 4, 1.250 | 4, 1.338 | 2, 1.394 |
| absorption coeff. (mm-1) | 0.230 | 0.615 | 0.580 |
| F(000) | 2496 | 2658 | 1738 |
| crystal size (mm) | 0.2  0.1  0.1 | 0.18  0.12  0.06 | 0.36  0.27  0.27 |
|  range (deg) min, max | 1.70, 20.82 | 1.71, 26.00 | 1.15, 25.00 |
| limiting indices | -10  h  10 | -13  h  13 | -13  h  13 |
|  | 0  k  30 | -21  k  20 | -21  k  20 |
|  | 0  l  19 | -39  l  39 | -23  l  22 |
| reflections collected, unique | 6485 3958 [R(int) = 0.1528] | 55788, 21590 [R(int) = 0.0606] | 30418, 13918 [R(int) = 0.0514] |
| completeness to  (%) | 100.0 ( =20.82) | 99.0 ( = 26) | 99.6 ( = 25) |
| absorption correction | semi-empirical from equivalents | semi-empirical from equivalents | semi-empirical from equivalents |
| Max, min transmission | 0.9281, 0.6596 | 0.9640, 0.8974 | 0.8591, 0.8184 |
| Refinement method | Full-matrix least-squares on F2 | Full-matrix least-squares on F2 | Full-matrix least-squares on F2 |
| data/restraints/parameters | 6485 / 204 / 890 | 21590 / 260 / 1349 | 13918 / 0 / 896 |
| Goodness-of-fit on F2 | 1.040 | 1.084 | 1.023 |
| Final R indices [I>2sigma(I)] | R1 = 0.0479 wR2 = 0.1302 | R1 = 0.0708, wR2 = 0.1643 | R1 = 0.0537, wR2 = 0.1135 |
| R indices (all data) | R1 = 0.0886 wR2 = 0.1191 | R1 = 0.0875, wR2 = 0.1738 | R1 = 0.0981, wR2 = 0.1304 |
| Largest diff. peak, hole (eÅ-3) | 0.312, -0.353 | 4.100, -0.843 | 0.836, -0.620 |

Experimental Section.

(c-C5H9)7Si8O12C6H4CH2-9-Flu(H) (4)

(a) (c-C5H9)7Si8O12(C6H4)-p-CH2Cl was prepared in a similar way as for 2, starting from (c-C5H9)7Si7O9(OH)3 (4.40 g. 5.0 mmol) and Cl3Si(C6H4)-p-CH2Cl (1.31 g, 5.0 mmol) and was isolated as a white powder (3.77 g, 3.8 mmol, 75 %). (b) (c-C5H9)7Si8O12C6H4CH2Flu(H) (4) was prepared in a similar way as 2, starting from (c-C5H9)7Si8O12C6H4CH2Cl (3.50 g, 3.5 mmol) and FluLi (prepared from fluorene (2 g, 12.0 mmol) and n-BuLi (4.8 mL, 2.5M, 12.0 mmol) and was isolated as a white powder (2.45 g, 2.2 mmol, 62 %). (Found: C, 57.14; H, 6.80. C55H78O12Si8 requires: C, 56.93; H, 6.87 %).

(c-C5H9)7Si8O12CH2-9-Flu(9-SnMe3) (5b)

Analogously as for 5a, 0.18 g (0.90 mmol) of trimethylstannylchloride was reacted with the product of the reaction between 2 (0.96 g, 0.89 mmol) and n-BuLi (0.35 mL, 2.5 M in hexanes, 0.9 mmol) to yield 5b (0.93 g, 0.77 mmol, 87 %) as a crystalline solid. Recrystalization from hexane produced a sample of 5b suitable for a single crystal X-ray diffraction study. (Found: C, 50.26; H, 6.65. C52H82O12Si8Sn requires: C, 49.89; H, 6.58 %).

Cp"[(c-C5H9)7Si8O12CH2-9-Flu]ZrCl2 (6b)

Using the same procedure as for 6a, with addition of Cp"ZrCl3 (0.40 g, 0.98 mmol) yielded 6b as an orange solid. Slow cooling to -30oC of a saturated dichloromethane solution yielded 6b as bright red rod like crystals suitable for a single crystal X-ray diffraction study. The crystals contained a considerable amount of solvent and were dried in vacuo for 3 h at room temperature, yielding 6b as an opaque orange powder (0.98 g, 0.66 mmol, 73 %). (Found: C, 49.69; H, 6.53. C60H94Cl2O12Si10Zr requires: C, 49.54; H, 6.81 %).

Crystal Structure Determination of (c-C6H11)7Si8O12-9-FluH (1)

A suitable crystal was selected, mounted on a thin, glass fiber using paraffin oil and cooled to the data collection temperature.  Data were collected on a Bruker AXS SMART 1k CCD diffractometer using 0.3° -scans at 0, 90, and 180° in . Initial unit-cell parameters were determined from 60 data frames collected at different sections of the Ewald sphere. Semi-empirical absorption corrections based on equivalent reflections were applied. Systematic absences in the diffraction data and unit-cell parameters were uniquely consistent with the reported space group. The structure was solved by direct methods, completed with difference Fourier syntheses and refined with full-matrix least-squares procedures based on F2. One cyclohexyl ring was found disordered in two conformations with a roughly 60/40 refined site occupancy distribution. All non-hydrogen atoms were refined with anisotropic displacement coefficients. All hydrogen atoms were treated as idealized contributions. All scattering factors are contained in the SHELXTL 6.12 program library.

Crystal Structure Determination of (c-C5H9)7Si8O12CH2-9-Flu(9-SnMe3)(C6H14)0.25 (5b).

A colorless crystal measuring (0.18  0.12  0.06 mm) was mounted under the liquid nitrogen stream (150 K), on a Nonius Kappa CCD area detector with a graphite monochromator ( = 0.71073 Å), with a rotating anode source. The crystal contained one disordered hexane solvent molecule per unit cell. Lorentz, polarisation and absorption corrections were applied. The molecule was refined in the acentric space group Pc with two independent molecules in the asymmetric unit, and half a molecule of hexane. The PLATON/ADDSYM tool did not show any indication for missing symmetry. The distances and angles in all cyclopentyl groups were restrained using the SAME command, and one group (C241–C245) was equally disordered across two sites, with two atoms (C240/C241, C243/C247) sharing common positional and displacement parameters. One carbon atom in the hexane molecule was not located so no hydrogen atoms were placed on the two outer most carbons (C400/C404). A large residual difference peak of 4.1 e.Å-3 was located close to one of the methyl groups on the tin which was refined with isotropic displacement parameters. The likely substitutional disorder CH3/Cl was not included in the model. Three other atoms (O221, C221 and C247) and all atoms in the solvent were refined with isotropic parameters. Several atoms in the second molecule had unusual anisotropic displacement parameters, and most of the residual density was located around these atoms. Refinement was carried out using full matrix least-squares on F2 (SHELXL-97).

Crystal Structure Determination of Cp"[(c-C5H9)7Si8O12CH2-9-Flu]ZrCl2(CH2Cl2)2.5 (6b).

An orange crystal measuring (0.36  0.27  0.27 mm) was mounted under the liquid nitrogen stream (150 K), on a Nonius Kappa CCD area detector with a graphite monochromator ( = 0.71073 Å), with a rotating anode source. The crystal contained five dichloromethane solvent molecules per unit cell. Lorentz, polarisation and absorption corrections were applied. Two of the cyclopentyl groups (C71–C75 / C81–C85) were disordered across two sites, the major and minor components being in a ratio of 0.52:0.48. Three pairs of atoms in the disordered groups (C71/C71A, C74/C74A, C84/C84A) share positional and displacement ellipsoid parameters. Half a molecule of dichloromethane was located close to an inversion centre, and is possibly disordered, but no additional restraints were applied. Refinement was carried out using full matrix least-squares on F2 (SHELXL-97).

References.

R. Blessing,  Acta Cryst., 1995, A51, 33.

G. M. Sheldrick, Bruker AXS, Madison, WI, 2001.