Table S1. Elemental analysis of the product of  W(CO)6  sonication in diphenylmethane.

| Element | As – prepared (wt. %) | ### Heated at 550oC in Ar, (wt. %) | Heated at 1000 oC in Ar (wt. %) | Heated at 1000 oC in Air ( wt. %) |
| --- | --- | --- | --- | --- |
| Nitrogen | 1.8 | 0.3 | 0 | 0 |
| Carbon | 18.8 | 4.1 | 0.3 | < 0.1 |
| Hydrogen | 3.4 | 0.4 | 0 | 0 |

Fig. S1 TEM image of the product heated at 1000 ºC