Modification of the solid-state structure of bis(1-hydroxy-2(1H)-pyridinethiolato-S2,O)zinc(II): synthesis and characterisation of a molecular solid solution incorporating 3-hydroxy-4-methyl-2(3H)-thiazolethione

## Andrew D. Bond,* Francesca Benevelli and William Jones

# Supplementary Material

Indexed PXRD data (2 < 35 ) for the single phase Zn(PT)x(MTT)2-x(H2O) products (shown in Figure 4)

x = 2.00

Refined cell parameters: orthorhombic, a = 15.621(8), b = 11.927(6), c = 7.137(4) Å.

Cell volume: 1329.7(8) Å3.

| 2(obs) /  | h | k | l | 2(calc) /  | 2(obs) – 2(calc) /  | I / % | d(obs) / Å | d(calc) / Å |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 9.289 | 1 | 1 | 0 | 9.322 | -0.0328 | 75.6 | 9.5132 | 9.4798 |
| 11.277 | 2 | 0 | 0 | 11.320 | -0.0426 | 25.9 | 7.8399 | 7.8105 |
| 13.512 | 2 | 1 | 0 | 13.541 | -0.0285 | 25.4 | 6.5479 | 6.5341 |
| 15.512 | 1 | 1 | 1 | 15.529 | -0.0168 | 100.0 | 5.7077 | 5.7016 |
| 16.798 | 2 | 0 | 1 | 16.814 | -0.0161 | 54.5 | 5.2736 | 5.2685 |
| 18.388 | 2 | 1 | 1 | 18.395 | -0.0066 | 44.3 | 4.8210 | 4.8193 |
| 19.380 | 0 | 2 | 1 | 19.381 | -0.0011 | 16.8 | 4.5764 | 4.5762 |
| 20.191 | 1 | 2 | 1 | 20.204 | -0.0129 | 25.0 | 4.3944 | 4.3916 |
| 22.641 | 3 | 2 | 0 | 22.652 | -0.0112 | 69.3 | 3.9242 | 3.9223 |
| 23.930 | 4 | 1 | 0 | 23.958 | -0.0274 | 10.0 | 3.7156 | 3.7114 |
| 25.941 | 3 | 2 | 1 | 25.899 | 0.0413 | 31.7 | 3.4320 | 3.4374 |
|  | 4 | 0 | 1 | 25.988 | -0.0471 |  |  | 3.4259 |
| 27.104 | 4 | 1 | 1 | 27.058 | 0.0463 | 14.9 | 3.2872 | 3.2927 |
| 28.473 | 2 | 1 | 2 | 28.477 | -0.0041 | 7.7 | 3.1322 | 3.1318 |
| 29.148 | 0 | 2 | 2 | 29.140 | 0.0076 | 8.1 | 3.0613 | 3.0620 |
| 29.705 | 1 | 2 | 2 | 29.707 | -0.0024 | 10.6 | 3.0051 | 3.0049 |
| 30.050 | 4 | 2 | 1 | 30.058 | -0.0083 | 12.4 | 2.9714 | 2.9706 |
| 30.499 | 1 | 4 | 0 | 30.496 | 0.0032 | 9.3 | 2.9286 | 2.9289 |
| 30.939 | 3 | 3 | 1 | 30.924 | 0.0150 | 8.4 | 2.8880 | 2.8894 |
| 31.331 | 2 | 2 | 2 | 31.353 | -0.0217 | 12.7 | 2.8527 | 2.8508 |
| 32.171 | 5 | 1 | 1 | 32.137 | 0.0331 | 6.7 | 2.7802 | 2.7830 |
| 33.042 | 1 | 4 | 1 | 33.032 | 0.0096 | 6.8 | 2.7088 | 2.7096 |
| 33.956 | 3 | 2 | 2 | 33.936 | 0.0202 | 12.5 | 2.6380 | 2.6395 |
|  | 4 | 0 | 2 | 34.005 | -0.0490 |  |  | 2.6343 |
| 34.572 | 4 | 3 | 1 | 34.532 | 0.0402 | 17.0 | 2.5923 | 2.5953 |
|  | 2 | 4 | 1 | 34.536 | 0.0368 |  |  | 2.5950 |

Figure of Merit F(23) = 18.3 ( 0.019, 65 ).

Modification of the solid-state structure of bis(1-hydroxy-2(1H)-pyridinethiolato-S2,O)zinc(II): synthesis and characterisation of a molecular solid solution incorporating 3-hydroxy-4-methyl-2(3H)-thiazolethione

## Andrew D. Bond,* Francesca Benevelli and William Jones

# Supplementary Material

Indexed PXRD data (2 < 35 ) for the single phase Zn(PT)x(MTT)2-x(H2O) products (shown in Figure 4)

x = 1.67

Refined cell parameters : orthorhombic, a = 15.805(20), b = 11.781(20), c = 7.128(16) Å.

Cell volume: 1327.3(49) Å3.

| 2(obs) /  | h | k | l | 2(calc) /  | 2(obs) – 2(calc) /  | I / % | d(obs) / Å | d(calc) / Å |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 9.379 | 1 | 1 | 0 | 9.355 | 0.0237 | 52.0 | 9.4218 | 9.4456 |
| 11.151 | 2 | 0 | 0 | 11.187 | -0.0361 | 16.1 | 7.9282 | 7.9027 |
| 13.476 | 2 | 1 | 0 | 13.481 | -0.0053 | 16.2 | 6.5654 | 6.5628 |
| 15.565 | 1 | 1 | 1 | 15.561 | 0.0042 | 100.0 | 5.6884 | 5.6900 |
| 16.730 | 2 | 0 | 1 | 16.736 | -0.0059 | 51.4 | 5.2951 | 5.2932 |
| 18.378 | 2 | 1 | 1 | 18.360 | 0.0177 | 41.0 | 4.8236 | 4.8282 |
|  | 3 | 1 | 0 | 18.433 | -0.0547 |  |  | 4.8094 |
| 18.794 | 2 | 2 | 0 | 18.774 | 0.0197 | 12.5 | 4.7179 | 4.7228 |
| 19.506 | 0 | 2 | 1 | 19.534 | -0.0279 | 7.2 | 4.5472 | 4.5408 |
| 20.370 | 1 | 2 | 1 | 20.332 | 0.0382 | 17.3 | 4.3561 | 4.3642 |
| 22.648 | 0 | 3 | 0 | 22.625 | 0.0235 | 61.3 | 3.9229 | 3.9269 |
|  | 3 | 2 | 0 | 22.625 | 0.0233 |  |  | 3.9269 |
| 25.789 | 4 | 0 | 1 | 25.758 | 0.0313 | 25.0 | 3.4518 | 3.4559 |
| 26.483 | 1 | 3 | 1 | 26.499 | -0.0159 | 7.0 | 3.3629 | 3.3609 |
| 26.840 | 4 | 1 | 1 | 26.863 | -0.0237 | 8.5 | 3.3191 | 3.3162 |
| 29.252 | 5 | 1 | 0 | 29.228 | 0.0242 | 6.5 | 3.0506 | 3.0531 |
|  | 0 | 2 | 2 | 29.263 | -0.0114 |  |  | 3.0494 |
| 29.939 | 4 | 2 | 1 | 29.953 | -0.0141 | 11.9 | 2.9821 | 2.9808 |
| 30.932 | 5 | 0 | 1 | 30.920 | 0.0120 | 7.3 | 2.8886 | 2.8897 |
| 33.907 | 0 | 3 | 2 | 33.939 | -0.0320 | 9.8 | 2.6416 | 2.6392 |
|  | 3 | 2 | 2 | 33.939 | -0.0321 |  |  | 2.6392 |
| 34.489 | 4 | 3 | 1 | 34.545 | -0.0562 | 14.4 | 2.5984 | 2.5943 |
|  | 5 | 2 | 1 | 34.545 | -0.0563 |  |  | 2.5943 |

Figure of Merit F(18) = 12.9 ( 0.022, 63 ).

Modification of the solid-state structure of bis(1-hydroxy-2(1H)-pyridinethiolato-S2,O)zinc(II): synthesis and characterisation of a molecular solid solution incorporating 3-hydroxy-4-methyl-2(3H)-thiazolethione

## Andrew D. Bond,* Francesca Benevelli and William Jones

# Supplementary Material

Indexed PXRD data (2 < 35 ) for the single phase Zn(PT)x(MTT)2-x(H2O) products (shown in Figure 4)

x = 1.60

Refined cell parameters : orthorhombic, a = 15.837(15), b = 11.762(14), c = 7.114(9) Å.

Cell volume: 1325.2(35) Å3.

| 2(obs) /  | h | k | l | 2(calc) /  | 2(obs) – 2(calc) /  | I / % | d(obs) / Å | d(calc) / Å |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 9.388 | 1 | 1 | 0 | 9.359 | 0.0292 | 50.8 | 9.4132 | 9.4425 |
| 11.168 | 2 | 0 | 0 | 11.165 | 0.0039 | 16.0 | 7.9160 | 7.9187 |
| 13.493 | 2 | 1 | 0 | 13.469 | 0.0236 | 17.0 | 6.5572 | 6.5687 |
| 15.560 | 1 | 1 | 1 | 15.583 | -0.0222 | 100.0 | 5.6902 | 5.6821 |
| 16.707 | 2 | 0 | 1 | 16.739 | -0.0317 | 49.2 | 5.3022 | 5.2922 |
| 18.337 | 2 | 1 | 1 | 18.368 | -0.0308 | 40.8 | 4.8342 | 4.8262 |
| 18.772 | 2 | 2 | 0 | 18.780 | -0.0082 | 11.4 | 4.7233 | 4.7213 |
| 19.585 | 0 | 2 | 1 | 19.569 | 0.0161 | 8.9 | 4.5290 | 4.5327 |
| 20.382 | 1 | 2 | 1 | 20.363 | 0.0192 | 15.3 | 4.3537 | 4.3578 |
| 22.646 | 3 | 2 | 0 | 22.616 | 0.0299 | 59.2 | 3.9234 | 3.9285 |
|  | 0 | 3 | 0 | 22.662 | -0.0166 |  |  | 3.9205 |
| 23.334 | 1 | 3 | 0 | 23.356 | -0.0221 | 4.6 | 3.8092 | 3.8056 |
| 23.664 | 4 | 1 | 0 | 23.692 | -0.0277 | 3.0 | 3.7568 | 3.7525 |
| 25.754 | 4 | 0 | 1 | 25.729 | 0.0250 | 21.7 | 3.4564 | 3.4597 |
| 26.550 | 1 | 3 | 1 | 26.541 | 0.0093 | 8.0 | 3.3546 | 3.3557 |
| 26.845 | 4 | 1 | 1 | 26.839 | 0.0056 | 9.9 | 3.3184 | 3.3191 |
| 29.175 | 5 | 1 | 0 | 29.174 | 0.0010 | 5.4 | 3.0584 | 3.0585 |
| 29.936 | 4 | 2 | 1 | 29.941 | -0.0050 | 10.3 | 2.9824 | 2.9819 |
| 33.863 | 4 | 0 | 2 | 33.848 | 0.0150 | 9.4 | 2.6450 | 2.6461 |
| 34.526 | 5 | 2 | 1 | 34.517 | 0.0087 | 14.2 | 2.5957 | 2.5964 |
|  | 4 | 3 | 1 | 34.549 | -0.0228 |  |  | 2.5941 |

Figure of Merit F(19) = 17.9 ( 0.017, 63 ).

Modification of the solid-state structure of bis(1-hydroxy-2(1H)-pyridinethiolato-S2,O)zinc(II): synthesis and characterisation of a molecular solid solution incorporating 3-hydroxy-4-methyl-2(3H)-thiazolethione

## Andrew D. Bond,* Francesca Benevelli and William Jones

# Supplementary Material

Indexed PXRD data (2 < 35 ) for the single phase Zn(PT)x(MTT)2-x(H2O) products (shown in Figure 4)

x = 1.50

Refined cell parameters: orthorhombic, a = 15.861(12), b = 11.771(9), c = 7.154(4) Å.

Cell volume: 1335.6(24) Å3.

| 2(obs) /  | h | k | l | 2(calc) /  | 2(obs) – 2(calc) /  | I / % | d(obs) / Å | d(calc) / Å |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 9.347 | 1 | 1 | 0 | 9.349 | -0.0018 | 42.8 | 9.4539 | 9.4521 |
| 11.124 | 2 | 0 | 0 | 11.148 | -0.0240 | 15.6 | 7.9475 | 7.9305 |
| 13.449 | 2 | 1 | 0 | 13.452 | -0.0034 | 15.6 | 6.5786 | 6.5770 |
| 15.530 | 1 | 1 | 1 | 15.521 | 0.0084 | 100.0 | 5.7014 | 5.7044 |
| 16.675 | 2 | 0 | 1 | 16.676 | -0.0008 | 52.6 | 5.3123 | 5.3121 |
| 18.307 | 2 | 1 | 1 | 18.308 | -0.0014 | 40.0 | 4.8422 | 4.8418 |
| 18.773 | 2 | 2 | 0 | 18.761 | 0.0121 | 6.8 | 4.7230 | 4.7261 |
| 19.512 | 0 | 2 | 1 | 19.515 | -0.0031 | 7.4 | 4.5457 | 4.5450 |
| 20.345 | 1 | 2 | 1 | 20.309 | 0.0358 | 12.4 | 4.3616 | 4.3692 |
| 22.608 | 3 | 2 | 0 | 22.589 | 0.0183 | 53.0 | 3.9299 | 3.9330 |
|  | 0 | 3 | 0 | 22.645 | -0.0373 |  |  | 3.9235 |
| 23.328 | 1 | 3 | 0 | 23.337 | -0.0089 | 2.3 | 3.8101 | 3.8087 |
| 25.679 | 4 | 0 | 1 | 25.666 | 0.0135 | 20.2 | 3.4664 | 3.4682 |
| 26.782 | 4 | 1 | 1 | 26.776 | 0.0061 | 9.6 | 3.3260 | 3.3268 |
| 27.324 | 2 | 0 | 2 | 27.329 | -0.0052 | 7.8 | 3.2613 | 3.2607 |
| 28.363 | 2 | 1 | 2 | 28.379 | -0.0161 | 4.7 | 3.1441 | 3.1424 |
| 29.162 | 5 | 1 | 0 | 29.132 | 0.0302 | 4.7 | 3.0598 | 3.0629 |
|  | 0 | 2 | 2 | 29.192 | -0.0298 |  |  | 3.0568 |
| 29.884 | 4 | 2 | 1 | 29.879 | 0.0042 | 12.4 | 2.9875 | 2.9879 |
| 30.967 | 3 | 3 | 1 | 30.989 | -0.0223 | 8.8 | 2.8855 | 2.8835 |
| 31.344 | 2 | 2 | 2 | 31.337 | 0.0070 | 8.4 | 2.8516 | 2.8522 |
| 33.851 | 3 | 2 | 2 | 33.846 | 0.0049 | 9.2 | 2.6459 | 2.6463 |
|  | 6 | 0 | 0 | 33.883 | -0.0320 |  |  | 2.6435 |
|  | 0 | 3 | 2 | 33.884 | -0.0334 |  |  | 2.6434 |
| 34.476 | 5 | 2 | 1 | 34.450 | 0.0259 | 13.9 | 2.5994 | 2.6013 |
|  | 4 | 3 | 1 | 34.488 | -0.0118 |  |  | 2.5985 |

Figure of Merit F(21) = 28.8 ( 0.011, 64 ).

Modification of the solid-state structure of bis(1-hydroxy-2(1H)-pyridinethiolato-S2,O)zinc(II): synthesis and characterisation of a molecular solid solution incorporating 3-hydroxy-4-methyl-2(3H)-thiazolethione

## Andrew D. Bond,* Francesca Benevelli and William Jones

# Supplementary Material

Indexed PXRD data (2 < 35 ) for the single phase Zn(PT)x(MTT)2-x(H2O) products (shown in Figure 4)

x = 1.33

Refined cell parameters: orthorhombic, a = 15.971(13), b = 11.732(11), c = 7.191(9) Å.

Cell volume: 1347.3(31) Å3.

| 2(obs) /  | h | k | l | 2(calc) /  | 2(obs) – 2(calc) /  | I / % | d(obs) / Å | d(calc) / Å |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 9.343 | 1 | 1 | 0 | 9.346 | -0.0032 | 60.1 | 9.4581 | 9.4549 |
| 11.072 | 2 | 0 | 0 | 11.071 | 0.0007 | 17.7 | 7.9849 | 7.9855 |
| 13.405 | 2 | 1 | 0 | 13.402 | 0.0029 | 19.8 | 6.5998 | 6.6013 |
| 15.469 | 1 | 1 | 1 | 15.469 | -0.0004 | 100.0 | 5.7237 | 5.7235 |
| 16.571 | 2 | 0 | 1 | 16.577 | -0.0053 | 39.7 | 5.3453 | 5.3435 |
| 18.242 | 2 | 1 | 1 | 18.229 | 0.0139 | 36.5 | 4.8592 | 4.8629 |
| 19.510 | 0 | 2 | 1 | 19.514 | -0.0047 | 9.0 | 4.5464 | 4.5453 |
| 20.300 | 1 | 2 | 1 | 20.297 | 0.0025 | 13.5 | 4.3711 | 4.3717 |
| 22.554 | 3 | 2 | 0 | 22.536 | 0.0181 | 59.6 | 3.9390 | 3.9421 |
| 23.383 | 1 | 3 | 0 | 23.402 | -0.0184 | 6.1 | 3.8013 | 3.7983 |
| 25.487 | 4 | 0 | 1 | 25.497 | -0.0096 | 11.0 | 3.4920 | 3.4907 |
| 25.768 | 3 | 2 | 1 | 25.752 | 0.0160 | 19.4 | 3.4546 | 3.4568 |
| 26.592 | 4 | 1 | 1 | 26.622 | -0.0299 | 12.4 | 3.3494 | 3.3457 |
| 29.777 | 4 | 2 | 1 | 29.759 | 0.0174 | 10.9 | 2.9980 | 2.9997 |
| 30.984 | 3 | 3 | 1 | 30.955 | 0.0290 | 9.4 | 2.8839 | 2.8865 |
|  | 1 | 4 | 0 | 30.976 | 0.0082 |  |  | 2.8846 |
| 33.680 | 6 | 0 | 0 | 33.643 | 0.0372 | 7.5 | 2.6590 | 2.6618 |
|  | 3 | 2 | 2 | 33.713 | -0.0328 |  |  | 2.6565 |
| 34.405 | 4 | 1 | 2 | 34.398 | 0.0067 | 8.9 | 2.6046 | 2.6051 |
|  | 4 | 3 | 1 | 34.411 | -0.0062 |  |  | 2.6041 |

Figure of Merit F(17) = 23.7 ( 0.011, 64 ).

Modification of the solid-state structure of bis(1-hydroxy-2(1H)-pyridinethiolato-S2,O)zinc(II): synthesis and characterisation of a molecular solid solution incorporating 3-hydroxy-4-methyl-2(3H)-thiazolethione

## Andrew D. Bond,* Francesca Benevelli and William Jones

# Supplementary Material

Indexed PXRD data (2 < 35 ) for the single phase Zn(PT)x(MTT)2-x(H2O) products (shown in Figure 4)

x = 1.00

Refined cell parameters: orthorhombic, a = 15.960(11), b = 11.699(7), c = 7.205(4) Å.

Cell volume: 1345.4(21) Å3.

| 2(obs) /  | h | k | l | 2(calc) /  | 2(obs) – 2(calc) /  | I / % | d(obs) / Å | d(calc) / Å |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 9.362 | 1 | 1 | 0 | 9.365 | -0.0035 | 40.9 | 9.4393 | 9.4357 |
| 11.087 | 2 | 0 | 0 | 11.078 | 0.0087 | 15.6 | 7.9740 | 7.9802 |
| 13.423 | 2 | 1 | 0 | 13.420 | 0.0035 | 15.9 | 6.5909 | 6.5926 |
| 15.455 | 1 | 1 | 1 | 15.461 | -0.0058 | 100.0 | 5.7286 | 5.7265 |
| 16.555 | 2 | 0 | 1 | 16.563 | -0.0080 | 35.9 | 5.3504 | 5.3479 |
| 18.229 | 2 | 1 | 1 | 18.225 | 0.0035 | 33.9 | 4.8629 | 4.8638 |
| 18.806 | 2 | 2 | 0 | 18.794 | 0.0123 | 9.9 | 4.7148 | 4.7179 |
| 19.509 | 0 | 2 | 1 | 19.531 | -0.0227 | 7.6 | 4.5466 | 4.5414 |
| 20.307 | 1 | 2 | 1 | 20.315 | -0.0080 | 11.2 | 4.3697 | 4.3680 |
| 22.574 | 3 | 2 | 0 | 22.573 | 0.0010 | 50.0 | 3.9356 | 3.9358 |
| 23.485 | 1 | 3 | 0 | 23.464 | 0.0211 | 5.5 | 3.7849 | 3.7883 |
| 25.332 | 1 | 0 | 2 | 25.324 | 0.0079 | 5.8 | 3.5131 | 3.5141 |
| 25.778 | 3 | 2 | 1 | 25.772 | 0.0064 | 18.4 | 3.4532 | 3.4541 |
| 26.612 | 4 | 1 | 1 | 26.628 | -0.0166 | 16.4 | 3.3469 | 3.3449 |
| 27.024 | 4 | 2 | 0 | 27.029 | -0.0046 | 4.0 | 3.2968 | 3.2963 |
| 28.235 | 2 | 1 | 2 | 28.206 | 0.0293 | 1.9 | 3.1581 | 3.1613 |
| 29.067 | 0 | 2 | 2 | 29.087 | -0.0207 | 2.9 | 3.0696 | 3.0675 |
| 29.783 | 4 | 2 | 1 | 29.782 | 0.0010 | 11.3 | 2.9974 | 2.9975 |
| 31.057 | 1 | 4 | 0 | 31.061 | -0.0044 | 9.7 | 2.8773 | 2.8769 |

Figure of Merit F(19) = 14.4 ( 0.010, 148 ).