Table S1 Activities of iron and boron in the Fe-B melts at 1823 K determined in different ways (reference states are pure liquid components)

| x(B) | a(B)102(I) | a(B)102(II) | a(B)102(III) | a(Fe)10(I) | a(Fe)10(III) |
| --- | --- | --- | --- | --- | --- |
| 0.097 |  | 0.239 | 0.239 | 8.92 | 8.89 |
| 0.150 |  | 0.442 | 0.443 | 8.12 | 8.16 |
| 0.201 |  | 0.720 | 0.718 | 7.44 | 7.36 |
| 0.250 | 1.08 | 1.12 | 1.10 | 6.47 | 6.51 |
| 0.302 | 1.70 | 1.74 | 1.70 | 5.43 | 5.51 |
| 0.347 | 2.47 | 2.53 | 2.50 | 4.62 | 4.58 |
| 0.395 | 3.88 | 3.84 | 3.90 | 3.53 | 3.52 |
| 0.456 | 3.97 |  | 4.01 | 3.45 | 3.45 |
| 0.548 | 36.5 |  | 36.2 | 0.377 | 0.382 |
| 0.610 | 37.8 |  | 38.3 | 0.347 | 0.350 |
| 0.649 | 47.5 |  | 47.3 | 0.245 | 0.246 |
| 0.730 | 48.4 |  | 47.9 | 0.241 | 0.239 |

Note: I, calculated from experimental Fe and В vapour pressures; II, found by integrating the Gibbs-Duhem equation; III, calculated by the suggested model with optimised parameters for formation of associated complexes. The a(B) and a(Fe) values calculated by method III at x(B)=0.456, 0.548 and at x(B)=0.730 correspond to equilibria between melts and iron monoboride and crystalline boron, respectively.

Table S2 Comparison of (I) experimental activities of the Fe-B melt components chosen at random from the experimental data array with (II) a(Fe) and a(B) values calculated according to the suggested model

| x(B) | T/К | a(Fe) |  | а(В) |  |
| --- | --- | --- | --- | --- | --- |
|  |  | I | II | I | II |
| 0.097 | 1603 | 0.893 | 0.887 | 0.00103 | 0.00101 |
| 0.907 | 1703 | 0.879 | 0.888 | 0.00152 | 0.0154 |
| 0.097 | 1753 | 0.895 | 0.889 | 0.00187 | 0.00187 |
| 0.097 | 1830 | 0.885 | 0.889 | 0.00241 | 0.00245 |
| 0.150 | 1453 | 0.792 | 0.804 | 9.0210-4 | 9.1110-4 |
| 0.150 | 1553 | 0.814 | 0.809 | 0.00156 | 0.00153 |
| 0.150 | 1653 | 0.817 | 0.812 | 0.00237 | 0.00238 |
| 0.150 | 1753 | 0.809 | 0.815 | 0.00354 | 0.00349 |
| 0.150 | 1830 | 0.823 | 0.816 | 0.00458 | 0.00454 |
| 0.201 | 1553 | 0.719 | 0.723 | 0.00257 | 0.00259 |
| 0.201 | 1753 | 0.732 | 0.732 | 0.00485 | 0.00478 |
| 0.201 | 1827 | 0.744 | 0.737 | 0.00730 | 0.00727 |
| 0.250 | 1623 | 0.641 | 0.638 | 0.00551 | 0.00550 |
| 0.250 | 1703 | 0.638 | 0.644 | 0.00749 | 0.00740 |
| 0.250 | 1834 | 0.661 | 0.652 | 0.0112 | 0.0113 |
| 0.302 | 1658 | 0.543 | 0.537 | 0.00991 | 0.00995 |
| 0.302 | 1753 | 0.550 | 0.546 | 0.0136 | 0.0137 |
| 0.302 | 1824 | 0.548 | 0.551 | 0.0170 | 0.0170 |
| 0.347 | 1703 | 0.441 | 0.446 | 0.0177 | 0.0174 |
| 0.347 | 1753 | 0.458 | 0.451 | 0.0201 | 0.0204 |
| 0.347 | 1833 | 0.457 | 0.459 | 0.0256 | 0.0257 |
| 0.395 | 1821 | 0.346 | 0.351 | 0.0394 | 0.0388 |
| 0.610 | 1809 | 0.0342 | 0.0337 | 0.379 | 0.382 |
| 0.610 | 1834 | 0.0360 | 0.0361 | 0.388 | 0.384 |
| 0.649 | 1818 | 0.0245 | 0.0242 | 0.466 | 0.472 |
| 0.649 | 1829 | 0.0254 | 0.0250 | 0.471 | 0.473 |