# Supplementary Information

IR spectrum of Cd(2,2’-bipy)(H2PO4)2

Experimental powder X-ray diffraction pattern of Cd(2,2’-bipy)(H2PO4)2

2θ/˚

Simulated powder X-ray diffraction pattern based on the single crystal solution

TGA curve of Cd(2,2’-bipy)(H2PO4)2 under air (10℃/min)

Table 1 Hydrogen bonds for Cd(2,2’-bipy)(H2PO4)2a

| D-H···A | d(D-H)/Å | D(H···A)/Å | D(D···A)/ Å | Angle D-H/º |
| --- | --- | --- | --- | --- |
| O(4)-H(1)···O(2) #1 | 0.82 | 1.87 | 2.675(8) | 166.8 |
| O5-H2···O8#2 | 0.82 | 1.84 | 2.640(8) | 166.1 |
| O6-H3···O8#3 | 0.82 | 1.80 | 2.601(8) | 166.1 |
| O7-H4···O1 | 0.82 | 1.78 | 2.600(7) | 175.8 |
| aSymmetry transformations used to generate equivalent atoms: #1 -x, y, -z+1/2 #2 -x+1/2, -y+3/2, -z+1 #3 x, -y+1, z-1/2 |