New silica-based hybrid organic-inorganic solids containing oligoarylene-vinylene fluorophore terminated phosphonates.

Céline Carbonneau, Richard Frantz, Jean-Olivier Durand*, Michel Granier,

Gérard F. Lanneau*, Robert J.P. Corriu

Precursor 3: Diethyl 4-(4-trimethoxysilylstyr-1-yl) benzylphosphonate

Diethyl 4-bromobenzylphosphonate (5g, 16.28 mmol), 4-styryltrimethoxysilane (3.83 g, 17.09 mmol), Pd(OAc)2 (36.7 mg, 0.16 mmol), triorthotolylphosphine (298 mg, 0.98 mmol), Et3N (6.87 mL, 48.84 mmol), are dissolved in MeCN (27 mL). The mixture is heated in a sealed tube at 110°C for 4h. Dry toluene is added with stirring to induce precipitation of triethylammonium salts. After decantation, the liquid is filtered over toluene-wetted silanized silica. Volatiles are evaporated and a brown oily liquid is obtained (6.61 g, 90%).

1HNMR (200 MHz, CDCl3,  ppm): 7.70-7.15 (m, 10H), 4.06 (m, 4H), 3.66 (s, 9H), 3.20 (d, 2J = 21.8 Hz, 2H), 1.29 (t, 3J = 7.1 Hz, 6H). 13C NMR (50 MHz, CDCl3,  ppm): 139.8 (s, 1C), 136.2 (sd, 5J = 3.8 Hz, 1C), 135.6 (d, 2C), 131.6 (sd, 2J = 9.3 Hz, 1C), 130.5 (dd, 3J = 6.2 Hz, 2C), 129.7 (d, 1C), 128.9 (s, 1C), 128.7 (d, 1C), 127.2 (d, 2C), 126.4 (d, 2C), 62.6 (td, 1J = 137.2 Hz, 2C), 33.9 (td, 1J = 137.2 Hz, 1C), 16.79 (d, 3J = 5.9 Hz, 2C). 31P NMR, (120 MHz, CDCl3,  ppm): 27.57. 29Si NMR, (60 MHz, CDCl3,  ppm): -54.8. IR (NaCl pellets), 3020, 2980, 2840, 1599, 1541, 1400, 1246, 1082, 1163, 1030, 980-860. HRMS: calc. 451.1706, obs. 451.1793.

Table S1. Gelation of precursor 3

| solid | Precursor 3 Quantity(g) mmol |  | y NH4F(%) | TMOS (x) Quantity (g) mmol |  |  | H2O (l) | Solvant (mL) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ## X3-2 | 0.70 | 1.554 | 2 | 2 | 0.473 | 3.108 | 155 | 2*3.10 |
| ### X3-3 | 0.70 | 1.554 | 2 | 3 | 0.710 | 4.662 | 212 | 2*4.13 |
| X3-4 | 0.70 | 1.554 | 2 | 4 | 0.946 | 6.216 | 268 | 2*5.16 |
| X3-10 | 0.70 | 1.554 | 2 | 10 | 2.366 | 15.540 | 607 | 2*171 |
| ### X3-100 | 0.01 | 2.2*10-2 | 4 | 100 | 0.338 | 2.220 | 80 | 2*2.24 |
| X3-1000 | 0.01 | 2.2*10-2 | 10 | 1000 | 3.379 | 22.20 | 800 | 2*22.0 |
| X3-5000 | 0.02 | 4.4*10-2 | 5000 | 5000 | 33.793 | 221.998 | 8000 | 2*222 |

Table S2. Data for xerogels X3

| Solid |  | Solid state NMR, d (ppm) 29Si 31P 13C |  |  |  |  |  | Density |  | SBET (m2/g) |  | EDX, Si/P(th) Si/P(exp) |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ## X3-2 |  | -68.2 (T2) -77.4 (T3) -100.3 (Q3) -108.7 (Q4) |  | 26.9 |  | 135.2-130.4 (C. ar.) 62.8 (OCH2) 16.4 (OCH2CH3) |  | 1.45 |  | <5 |  | 3 |  | 2.6 |
| X3-3 |  | -71.3 (T2) -78.5 (T3) -91.4 (Q2) -100.5 (Q3) -109.5 (Q4) |  | 26.6 |  | 139.0-129.9 (C. ar.) 62.6 (OCH2) 16.8 (OCH2CH3) |  | 1.50 |  | <5 |  | 4 |  | 3.2 |
| X3-4 |  | -70.7 (T2) -78.6 (T3) -91.5 (Q2) -101.1 (Q3) -107.9 (Q4) |  | 26.1 |  | 139.0-130.0 (C. ar.) 62.5 (OCH2) 16.2 (OCH2CH3) |  | 1.61 |  | <5 |  | 5 |  | 3.6 |
| ###### X3-10 | -63.2 (T1) -72.0(T2) -103.3 (Q3) |  | 27.9 |  | 138.5-129.7 (C. ar.) 62.4 (OCH2) 15.9 (OCH2CH3) |  | 1.63 |  | <5 |  | 11 |  | 9.3 |  |
| ##### X3-100 |  |  |  |  |  |  |  | 2.0 |  | 451 |  |  |  |  |
| X3-1000 |  |  |  |  |  |  |  | 2.1 |  | 710 |  |  |  |  |
| X3-5000 |  |  |  |  |  |  |  | 2.1 |  | 749 |  |  |  |  |

Table S3. Gelation of precursor 1a

| Solid | Precursor 1a Quantity(g) mmol |  | y NH4F (% ) | TMOS (x) Quantity (g) mmol |  |  | H2O l) | Solvant (mL) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ## X1a-0 | 1.0 | 1.809 | 3 | 0 | 0 | 0 | 50 | 1.81 |
| X1a-2 | 1.06 | 1.918 | 2 | 2 | 0.584 | 3.836 | 192 | 2*5.75 |
| X1a-3 | 0.70 | 1.266 | 2 | 3 | 0.578 | 3.798 | 172 | 2*5.06 |
| X1a-4 | 0.70 | 1.266 | 2 | 4 | 0.771 | 5.064 | 218 | 2*6.33 |
| X1a-5 | 0.70 | 1.266 | 2 | 5 | 0.964 | 6.330 | 264 | 2*7.60 |
| X1a-6 | 0.70 | 1.266 | 2 | 6 | 1.156 | 7.596 | 310 | 2*8.86 |
| X1a-7 | 0.70 | 1.266 | 2 | 7 | 1.349 | 8.862 | 354 | 2*10.1 |
| X1a-10 | 0.70 | 1.266 | 2 | 10 | 1.927 | 12.660 | 495 | 2*13.9 |
| X1a-15 | 0.70 | 1.266 | 2 | 15 | 2.890 | 18.990 | 725 | 2*20.3 |
| X1a-17.5 | 0.70 | 1.266 | 2 | 17.5 | 3.373 | 22.155 | 840 | 2*23.5 |
| X1a-20 | 0.70 | 1.266 | 2 | 20 | 3.854 | 25.320 | 955 | 2*26.6 |
| X1a-100 | 0.02 | 3.6*10-2 | 4 | 100 | 0.551 | 3.620 | 130 | 2*3.65 |
| X1a-1000 | 0.02 | 3.6*10-2 | 10 | 1000 | 5.511 | 36.20 | 1300 | 2*36.0 |
| ## X1a-5000 | 0.02 | 3.6*10-2 | 1 | 5000 | 27.552 | 181.0 | 6540 | 2*181 |

Table S4. Data for xerogels X1a

| Solid | Solid state NMR d (ppm) 29Si 31P 13C |  |  |  |  |  |  | Density |  |  | SBET (m2/g) |  |  | EDX Si/P (th) Si/P (exp) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ## X1a-0 |  |  | -70.0 (T2) -78.1 (T3) |  | 26.7 |  | 135.8-130.0 (C. ar.) 63.0 (OCH2) 16.8 (OCH2CH3) |  |  | 1.20 |  |  | <5 |  |  | 1 |  | 0.8 |
| ## X1a-2 |  | -71.4 (T2) -77.8 (T3) -100.3 (Q3) -108.5 (Q4) |  | 26.5 |  | / |  |  | 1.36 |  |  | <5 |  |  | 3 |  | 3.2 |  |
| ## X1a-3 |  | -65.5 (T2) -77.0 (T3) -90.0 (Q2) -100.3 (Q3) -108.4 (Q4) |  | 27.0 |  | 136.0-128.5 (C. ar.) 63.2 (OCH2) 16.5 (OCH2CH3) |  |  | 1.43 |  |  | <5 |  |  | 4 |  | 2.9 |  |
| ## X1a-4 |  | -68.2 (T2) -77.8 (T3) -100.6 (Q3) -110.4 (Q4) |  | 27.3 |  | / |  |  | / |  |  | <5 |  |  | 5 |  | 3.4 |  |
| ## X1a-5 |  | -68.0 (T2) -78.4 (T3) -101.0 (Q3) -109.7 (Q4) |  | 28.1 |  | 136.8-129.7 (C. ar.) 62.9 (OCH2) 16.6 (OCH2CH3) |  |  | 1.55 |  |  | 5 |  |  | 6 |  | 5.3 |  |
| ## X1a-6 |  | / |  | 27.2 |  |  |  |  | 1.46 |  |  | <5 |  |  | 7 |  | 4.1 |  |
| ## X1a-7 |  | / |  | 28.1 |  |  |  |  | 1.48 |  |  | <5 |  |  | 8 |  | 5.5 |  |
| ## X1a-10 |  | -78.3 (T3) -101.6 (Q3) -109.9 (Q4) |  | 28.6 |  | 136.7-126.8 (C. ar.) 63.6 (OCH2) 16.0 (OCH2CH3) |  |  | 1.60 |  |  | <5 |  |  | 11 |  | 6.3 |  |
| ## X1a-15 |  | / |  | 29.1 |  | 136.6-126.6 (C. ar.) 63.6 (OCH2) 50.8 (OCH3) 15.1 (OCH2CH3) |  |  | 1.71 |  |  | 330 |  |  | 16 |  | 11 |  |
| ## X1a-17.5 |  | / |  | 29.2 |  | 136.7-126.5 (C. ar.) 63.1 (OCH2) 14.7 (OCH2CH3) |  |  | 1.68 |  |  | 70 |  |  | 18.5 |  | 12 |  |
| ## X1a-20 |  | -77.8 (T3) -93.0 (Q2) -101.3(Q3) -109.8 (Q4) |  | 29.3 |  | 136.7-126.3 (C. ar.) 63.6 (OCH2) 51.0 (OCH3) 15.1 (OCH2CH3) |  |  | 1.76 |  |  | 306 |  |  | 21 |  | 13 |  |
| ## X1a-100 |  |  |  |  |  |  |  |  | 1.96 |  |  | 304 |  |  |  |  |  |  |
| ## X1a-1000 |  |  |  |  |  |  |  |  | 2.08 |  |  | 470 |  |  |  |  |  |  |
| ## X1a-5000 |  |  |  |  |  |  |  |  | 2.10 |  |  | 464 |  |  |  |  |  |  |

Table S5. Gelation of precursor 1b

| Solid | Precursor 1b Quantity(g) mmol |  | y NH4F (% ) | TMOS (x) quantity (g) mmol |  |  |  | H2O l) | Solvant (mL) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ## X1b-5 | 0.52 | 0.8224 | 3 | 5 | 0.650 | 4.112 | 179 |  | 2*5.2 |
| ## X1b-7 | 0.225 | 0.370 | 3 | 7 | 0.393 | 2.590 | 104 |  | 2*3 |
| ## X1b-9 | 0.38 | 0.625 | 3 | 9 | 0.8552 | 5.625 | 221 |  | 2*10 |
| ## X1b-12 | 0.154 | 0.253 | 3 | 12 | 0.462 | 3.036 | 117 |  | 2*3.5 |
| ## X1b-15 | 0.100 | 0.164 | 3 | 15 | 0.374 | 2.467 | 94 |  | 2*5 |

Table S6. Data for xerogels X1b

| Solid |  | Solid state NMR, d (ppm) 29Si 31P 13C |  |  |  |  |  | EDX, % Si and P Si/P(th) Si/P(exp) |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ## X1b-5 | -68.1 (T2) -77.5 (T3) -92 (Q2) -101 (Q3) -109.3 (Q4) |  | 17.6 |  | 139.2-129.1 (C. ar.) 82.1 (OC) 30.5 (OC(CH3)3) |  | 6 |  | 5.7 |  |
| ## X1b-9 |  | -70.7 (T2) -78.6 (T3) -91.5 (Q2) -101.1 (Q3) -107.9 (Q4) |  | 17.3 |  | 139.2-129.1 - ar.) 82.1 (OC) 30.4 (OC(CH3)3) |  | 10 |  | 8 |

Table S7. Gelation of precursor 2

| Solid | # Precursor 2 Quantity (g) mmol |  | y NH4F(%) | TMOS x Quantity (g) mmol |  |  | H2O l) | Solvant (mL) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ## X2-0 | 0.70 | 1.113 | 3 | 0 | 0 | 0 | 31 | 2.20 |
| ## X2-2 | 0.78 | 1.241 | 2 | 2 | 0.378 | 2.481 | 124 | 2*3.72 |
| ## X2-5 | 0.34 | 5.34*10-1 | 2 | 5 | 0.407 | 2.672 | 111 | 2*3.20 |
| ## X2-100 | 0.02 | 3.6*10-2 | 4 | 100 | 0.551 | 3.620 | 130 | 2*3.65 |
| ## X2-1000 | 0.02 | 3.6*10-2 | 10 | 1000 | 5.511 | 36.20 | 1300 | 2*36.0 |
| ## X2-5000 | 0.02 | 3.6*10-2 | 5000 | 5000 | 27.552 | 181.0 | 6500 | 2*181 |

Table S8. Data for xerogels X2

| Solid |  | Solid state NMR d (ppm) 29Si 31P 13C |  |  | Density |  | SBET (m2/g) |  | EDX Si/P(th) Si/P(exp) |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ## X2-0 | -72.0 (T2) -79.1 (T3) |  | 26.9 | 135.2-129.9 (C. ar.) 61.2 (OCH2) 16.1 (OCH2CH3) |  | / |  | / |  | 1 | 0.9 |
| ## X2-2 | -68.0 (T2) -79.5 (T3) -100.1 (Q3) -110.4 (Q4) |  | 26.5 | / |  | 1.42 |  | / |  | 3 | 2.9 |
| ## X2-5 | -67.5 (T2) -77.2 (T3) -91.5 (Q2) -101.2 (Q3) -110.0 (Q4) |  | 28.0 | 134.6-126.2 (C. ar.) 62.3 (OCH2) 14.7 (OCH2CH3) |  | 1.60 |  | / |  | 6 | 7.5 |
| ## X2-100 |  |  |  |  |  | 1.98 |  | 509 |  |  |  |
| ## X2-1000 |  |  |  |  |  | 2.00 |  | 579 |  |  |  |
| ## X2-5000 |  |  |  |  |  | 2.04 |  | 725 |  |  |  |

Figure S1. 29Si cpmas NMR (39.5 MHz) of xerogel X2-0

Figure S2. 29Si cpmas NMR (39.5 MHz) of xerogel X1b-5