Figures captions for Electronic supplementary information

Fig. S1. 1H NMR (D2O) for dried 1 (showing traces of DMF in 1).

Fig. S2. 1H NMR (D2O) for dried 1, immersed in a mixture of acetoneCH3CNCH3OHC2H5OH (1:1:1:1), then dried in air, indicating that only ethanol molecules were absorbed.

Fig. S3. 1H NMR (D2Oacetone-d6 = 4:1) for dried 1, immersed in a mixture of benzenetolueneTHFC2H5OH (1:1:1:1), then dried in air, indicating only ethanol molecules were absorbed (the trace of toluene is due to its higher boiling point, and it disappeared after a longer period of drying in air (over 2 h).

Fig. S1

Fig. S2

Fig. S3